## Slide 1
Influence of slag mineralogy on possibilities for use in alternative applications
Fredrik Engström, Ida Strandkvist, Caisa Samuelsson and Bo Björkman
Minerals and Metals Research Laboratory (MiMeR)
Luleå, Sweden
Notes: <number>

## Slide 2: Outline
Background
Case studies/Discussion
Conclusions
Notes: <number>

## Slide 3: Background
2010: ~ 45 million tonnes slag
External use: ~ 80 %
Europe
Sweden
2010: 1.4 million tonnes slag
External use: ~ 38 %
Landfilling: ~ 20 %
---------------------------------------------------------------------------------------------------
Europe
Notes: <number>
<number>
Enter speaker notes here.

## Slide 4: Conditions in Sweden
40 million tonne virgin material used in construction annually
Good access to high quality natural stone material
Criteria for use in building applications and road construction are missing for these materials
High availability of land for land filling
“Fear” of using by-products
---------------------------------------------------------------------------------------------------
---------------------------------------------------------------------------------------------------
Notes: <number>
Good building environment
By 2010, extraction of natural gravle not exceed 12 million ton.
The total quantity of waste generated will not increase and maximum use will be made of it’s resource potential

## Slide 5
Background
Leaching tests used today!

## Slide 6
Background
Black Box!
Why?

## Slide 7: Slags
Multi-crystalline materials !
EAF slag from black steel
EAF slag from stainless steel

## Slide 8
Minerals commonly found in slags
Mineral name |  | Chemical name | 
Akermanite |  | Ca2MgSi2O7 | X
Merwinite |  | Ca3MgSi2O8 | X
Gehlenite |  | Ca2Al2SiO7 | X
Melilite |  | Ca2MgSi2O7-Ca2Al2SiO7 | 
Wollastonite |  | CaSiO3 | X
Monticellite |  | CaMgSiO4 | X
Ingesonite |  | γ-Ca2SiO4 | X
Larnite |  | β-Ca2SiO4 | X
Bredegite |  | Ca14Mg2(SiO4)8 | 
Tricalcium silicate |  | Ca3SiO5 | 
Spinel (Fe,Mg,Mn,Al) |  | Me2+Me3+2O4 | 
Wustite |  | FeO | X
Lime |  | CaO | 
Periclase |  | MgO | X
Srebrodolskite |  | Ca2Fe2O5 | X
Brownmillerite |  | Ca2(Al,Fe)O5 | X
Mayenite |  | Ca12Al14O33 | X
Tricalcium aluminate |  | Ca3Al2O6 | X
X has been synthetic manufactured by us in order to evaluate it’s properties!
The behaviour of the slags depends on what minerals that are available in the slag!

## Slide 9
Case study 1, Cr leaching
In order to explain the chromium leaching occurring from slags, at least two questions have to be answered.
How is chromium distributed!
How is the chromium containing phase reacting with water.

## Slide 10
Dissolves Chromium(Cr+3)
Merwinite Yes
Akermanite No
B-Ca2SiO4 No
MgO Yes
Gehlenit No
Ca2Fe2O5 Yes
3CaO*Al2O3 No
Distribution of Cr in slag mineral

## Slide 11: Synthetic slag minerals/ titration
20-38 μm size, 0.1 M HNO3, 50 mg mineral / 100 ml H2O

## Slide 12: Minerals responsible for Cr leaching
MgO (ss)
Ca2(Fe,Al)2O5 (ss)
EAF slag from black steel

## Slide 13: Minerals responsible for Cr leaching
MgO-FeO (ss)

## Slide 14: Minerals responsible for Cr leaching
Ca2Fe2O5 - Ca2(Fe,Al)O5 (ss)
X-ray diffraction p

## Slide 15: CASE STUDY 2-PHOSPHORUS CAPACITY
Company's were asked to submit slag sample for P-screening
  22 samples from industry
  Were evaluated using chemical analysis and XRD
4 Cluster + 2 outliers

## Slide 16: RESULTS-PHOSPHORUS
Cluster 1 and 2 best!
Cluster
pH
Degree of P removal % and pH
P removal %

## Slide 17: RESULTS-PHOSPHORUS
0.01 g mineral, 20-38um, 10 ml solution, konc 10 mg/L

## Slide 18: RESULTS-OTHER METALS
0.01g mineral, 20-38um, 10 ml solution, Cu=15ug/L, Ni=4ug/L

## Slide 19: Conclusions
=
The properties of the slags is influenced:

## Slide 20: Acknowledgement
Notes: <number>