## Slide 1
Recent experimental and modelling research on the thermodynamics and phase equilibria of multi-component oxide systems
Evgueni Jak and Peter Hayes
PYROSEARCH, Pyrometallurgy Innovation Centre, The University of Queensland,
Brisbane, Australia.

## Slide 2
Introduction
Experimental Methodology
Thermodynamic Models and Databases
Applications to Industry

## Slide 3: Introduction - The slag valorisation process
NEW MATERIALS
Cements
Geopolymers
Slag structural materials
Slag manufactured materials
RAW MATERIALS
Slags
Stoichiometric compounds
Complex wastes
PROCESS AND CHEMICAL MODIFICATION
Complex solid solutions
Amorphous (glassy) materials
Partially crystallised materials
Chemical separations
PROPERTIES TO BE ACHIEVED
High/Low reactivity
Stabilisation of hazardous elements
Low impurity levels
How we can help!!!

## Slide 4
INTRODUCTION - CaO-FeO-Fe2O3-SiO2-Common slag chemistry Al2O3-MgO……
Fe sinter
Iron and
steelmaking
slags
Cement
production
Inorganic-polymer materials
Fe ore
Structural
materials
CaO
|
FeO
|
Fe2O3
|
SiO2
|
Al2O3
|
MgO
Non-ferrous
metallurgical
slags
Manufactured
materials
Slag
valorisation
Industrial wastes

## Slide 5
INTRODUCTION - Information needed
- Phases present
- Chemical compositions of the phases
- Relative fractions of the phases
- Thermodynamic activities of the chemical components
- Physico-chemical properties of chemical components (e.g. viscosity)

## Slide 6: ● Thermodynamic modelling - assess existing data and plan experiments
METHODOLOGY needed for complex systems – Integrated and iterative thermodynamic modelling and experimental studies
● Experiments on low order systems - fundamental knowledge
● Experiments on multi-component systems - usually in support of industrial processes
● Thermodynamic modelling - final database development

## Slide 7
INTEGRATED
  EXPERIMENTAL AND
  THERMODYNAMIC MODELLING
STUDIES
PYROSEARCH METHODOLOGY
New advanced micro-analytical tools and experimental methodologies,
EPMA, LA-ICP-MS
New advanced computational and theoretical tools

## Slide 8
Chart: Analysis spot size (micron)
| 15 | 30 | 60 | 80
Ag | 10.1 | 0.03 | 0.011 | 0.002
Au | 9.8 | 0.02 | 0.005 | 0.001
Pb | 18.9 | 0.55 | 0.13 | 0.05
Examples of Laser Ablation ICP-MS microanalysis of minor elements in slag
EXPERIMENTAL METHODOLOGY
– microanalysis for minor elements in multi-phase systems

## Slide 9
METHODOLOGY FOR ACCURATE PHASE EQUILIBRIA MEASUREMENTS
Independent of original bulk composition/Crucible interaction/Vaporisation
  Enables metal/slag/matte/ gas equilibration
  Allows use of substrates
  Tests achievement of
  equilibria
  Enables phase analysis and identification
  Defines limits of solid and liquid solutions for thermodynamic modelling
  Applicable to multi-
  component systems
High Temperature Equilibration
>>> Quenching
>>> Electron Probe X-ray Microanalysis (EPMA)

## Slide 10
METHODOLOGY FOR ACCURATE PHASE EQUILIBRIA MEASUREMENTS
The lever rule applies in multi-phase space, e.g.
At T1 the proportion of liquid at bulk composition, X
= bc/ac

## Slide 11
Evolution of sample support types for slag phase equilibria determination.
Sample mass /Systems
0.05 – 0.2 g
No silica systems
Chemical Analysis Techniques
Wet chemical/
SEM-EDS
EPMA
EPMA/LA-ICP-MS
Increasing cooling rate
5 – 20 g/ High silica systems
0.1 – 1 g/ Low silica systems
EXPERIMENTAL APPROACHES
Previous
10 yrs ago
Now

## Slide 12
Projections and sections in compositional space.
METHODOLOGY
for representation of phase equilibria –
Phase diagrams
There are many different ways to explore compositional space and to make it easier to apply thermodynamics to practice

## Slide 13
10-6
PO2 10-5
10-7
10-8
10-9
T = 1300oC
References:
(1) S. Nikolic, P.C. Hayes and E. Jak: Metall. Trans. B, 39B(2008), 179-188.
(2) T. Hidayat, P.C. Hayes and E. Jak: Metall. Mater. Trans. B, 43(2012), 14-26.
(3) T. Hidayat, P.C. Hayes and E. Jak: Metall. Mater. Trans. B, 43(2012), 27-38.
FeOx-CaO-SiO2 at fixed PO2

## Slide 14
a’-Ca2SiO4-Fe2SiO4
Solid Solution
New experimental
liquid / solid tie-lines
– essential for the accurate revision of thermodynamic databases
References:
(4) B. Zhao, P. Hayes and E. Jak: Unpublished Work: Pyrometallurgy Research Centre, The University of Queensland, (2003), (5) W.C. Allen and R.B. Snow: J. Am. Ceram. Soc., 38(1955), 264-280.
(6) N.L. Bowen, J.F. Schairer and E. Psnjak: Am. J. Sci., 26(1933), 193-284.
(7) E. Görl, F. Oeters and R. Scheel: Arch. Eisenhuettenwes., 37(1966), 441-445.
(8) S.A. Decterov, I.-H. Jung, E. Jak, Y.-B. Kang, P. Hayes and A.D. Pelton: Proc. of VII Int. Conf. on Molten Slags, Fluxes & Salts. SAIMM, South Africa, 2004, 839-850.
S.A. Decterov, I.-H. Jung, E. Jak, Y.-B. Kang, P. Hayes and A.D. Pelton: Proc. of VII Int. Conf. on Molten Slags, Fluxes & Salts. SAIMM, South Africa, (2004), 839-850.
CaO-“FeO”-SiO2 in equilibrium with metallic iron

## Slide 15
“FeO”-CaO-SiO2 at fixed PO2 - effect of Al2O3
References:
T. Hidayat, H.M. Henao, P.C. Hayes and E. Jak: Proc. of the 7th International Copper-Cobre Conference 2010. GDMB, Hamburg, Germany, 2010, 761-778.

## Slide 16
“FeO”-CaO-SiO2 at fixed PO2 - effect of MgO
References:
T. Hidayat, H.M. Henao, P.C. Hayes and E. Jak: Proc. of the 7th International Copper-Cobre Conference 2010. GDMB, Hamburg, Germany, 2010, 761-778.

## Slide 17
17
Microanalysis of multi-phase systems for complex feeds - partitioning of elements between solutions
Cu-Pb-Fe-O-S-Si system
Notes: 17

## Slide 18: ● Thermodynamic modelling - assess existing data and plan experiments
Integrated thermodynamic modelling and experimental studies
● Experiments on low order systems - fundamental knowledge
● Experiments on multi-component systems - usually in support of industrial processes
● Thermodynamic modelling - final database development

## Slide 19
Pyramid effect: e.g. change in Fe-O
requires re-evaluation of all these systems
THERMODYNAMIC DATABASE DEVELOPMENT

## Slide 20
What does it mean when we say build a database?
Quantitatively define the relationship between
Composition and Gibbs Free Energy for each and every possible phase.
THERMODYNAMIC DATABASE DEVELOPMENT

## Slide 21
THERMODYNAMIC DATABASE DEVELOPMENT
For accurate description of a condensed phase system at least 6 types of data are needed to describe the system unambiguously, S298 Cp ∆H298 ∆Hfusion Liquidus, Component Activities.
For systems having extensive solid solutions then crystal structure and site occupancy of elements must also be added.
Solids data S298 and Cp (then ∆H298) are usually the most accurate – liquid data are invariably the least accurate.
S298, Cp, ∆H298
S298, Cp, ∆H298
Liquid
∆Hfusion Liquidus, Activities
solubilities
Its important to get the foundations right!

## Slide 22
THERMODYNAMIC DATABASE DEVELOPMENT
Modern Thermodynamic Computer Platforms
contain
------------------------------------
GIBBS FREE ENERGY
MINIMISATION SOFTWARE
+
THERMODYNAMIC DATABASES
+
INPUT/OUTPUT WINDOWS - BASED

## Slide 23
FactSage thermodynamic databases describe the Gibbs Free Energies of
      Over 5000 stoichiometric compounds
      Advanced solution models
      Evaluated complex solutions
----------------------------------------------
Enabling the prediction of the thermochemical properties of Multi-component, Multi-phase equilibria for systems containing
GASES / SLAG (molten oxides) / MOLTEN SALTS (Cl, F, S, SO3, .) / METAL ALLOYS / SOLIDS / AQUEOUS SOLUTIONS
THERMODYNAMIC DATABASE DEVELOPMENT
FactSage developed by Centre for Computational Thermochemistry, (CRCT ), Ecole Polytechnique de Montreal, Canada

## Slide 24
LIQUID SLAG – RECENT MODEL IMPROVEMENTS:
- Modified Quasi-chemical Model, GUTS model
- Flexible acid / basic grouping
- Flexible maximum ordering composition
- Flexible combination of models for binaries and ternaries
SOLID SOLUTIONS:
- Compound energy formalism - 2 and 3 sub-lattice models
THERMODYNAMIC DATABASES DEVELOPMENT
Models provide the structure

## Slide 25
THERMODYNAMIC DATABASES - Example
Quasi-chemical model for slags and molten salts
Quasichemical Thermodynamic Model (FactSage)
SNNB – Second Nearest Neighbour Bond
(Si-O-Si) + (Me-O-Me) = 2 (Me-O-Si), DgSi-Me= w-hT

## Slide 26
Slag
Matte/Metal
Spinel
Olivine [Ca2+, Fe2+, Mg2+, Zn2+]M2(Ca2+, Fe2+, Mg2+, Zn2+)M1SiO4
Melilite [Ca2+, Pb2+]2(Fe2+, Zn2+, Al3+, Fe3+)[Al3+, Fe3+, Si4+]2
Pyroxenes (Ca, Fe2+, Mg)M2 (Fe2+, Fe3+, Mg, Al )M1 (Fe3+, Al, Si)B SiA O6
Monoxide CaO - MgO - MnO - CoO - NiO - FeO
(+ Fe2O3 - Al2O3 - ZnO - Cr2O3)
a-Ca2SiO4 a-Ca2SiO4 ( + Fe2SiO4, Mg2SiO4, Mn2SiO4)
a’-Ca2SiO4 a’-Ca2SiO4 ( + Fe2SiO4, Mg2SiO4, Mn2SiO4 , Pb2SiO4 , Zn2SiO4)
Wollastonite CaSiO3 ( + FeSiO3, MgSiO3, MnSiO3)
Corundum Al2O3 - Cr2O3 - Fe2O3
.
THERMODYNAMIC DATABASES - Advanced thermodynamic models / self consistent databases
Pyroxenes (Ca, Fe2+, Mg)M2 (Fe2+, Fe3+, Mg, Al )M1 (Fe3+, Al, Si)B SiA O6
Monoxide CaO - MgO - MnO - CoO - NiO - FeO
(+ Fe2O3 - Al2O3 - ZnO - Cr2O3)
a-Ca2SiO4 a-Ca2SiO4 ( + Fe2SiO4, Mg2SiO4, Mn2SiO4)
a’-Ca2SiO4 a’-Ca2SiO4 ( + Fe2SiO4, Mg2SiO4, Mn2SiO4 , Pb2SiO4 , Zn2SiO4)
Wollastonite CaSiO3 ( + FeSiO3, MgSiO3, MnSiO3)
Corundum Al2O3 - Cr2O3 - Fe2O3

## Slide 27
Recent data shows that early measurements were not always correct
a’-Ca2SiO4-Fe2SiO4
Solid Solution
In equilibrium with metallic iron
References:
(4) B. Zhao, P. Hayes and E. Jak: Unpublished Work: Pyrometallurgy Research Centre, The University of Queensland, (2003),
(5) W.C. Allen and R.B. Snow: J. Am. Ceram. Soc., 38(1955), 264-280.
(6) N.L. Bowen, J.F. Schairer and E. Psnjak: Am. J. Sci., 26(1933), 193-284.
(7) E. Görl, F. Oeters and R. Scheel: Arch. Eisenhwes., 37(1966), 441-445.
(8) S.A. Decterov, I.-H. Jung, E. Jak, Y.-B. Kang, P. Hayes and A.D. Pelton: Proc. VII Int. Conf. on Molten Slags, Fluxes & Salts. SAIMM (2004), 839-850.
(10) F. Abbattista, A. Burdese and M. Maja: Rev. Int. Hautes Temp. Refract., 12(1975), 337-342.
(11) H. Larson and J. Chipman: Trans. AIME, J. Met., 197(1953), 1089-1096.
(12) Y. Takeda, S. Nakazawa and A. Yazawa: Can. Metall. Q., 19(1980), 297-305.
(13) M. Timucin and A.E. Morris: Metall. Trans., 1(1970), 3193-3201.
S.A. Decterov, I.-H. Jung, E. Jak, Y.-B. Kang, P. Hayes and A.D. Pelton: Proc. VII Int. Conf. Molten Slags, Fluxes & Salts. SAIMM, South Africa, (2004), 839-850.
THERMODYNAMIC DATABASES – why we need to re-evaluate base systems

## Slide 28
THERMODYNAMIC DATABASES– why we need to re-evaluate base systems

## Slide 29
THERMODYNAMIC DATABASES– why we need to re-evaluate base systems

## Slide 30
THERMODYNAMIC DATABASES – why we need to re-evaluate base systems

## Slide 31
Effect of P on phase distribution in the system CaO-2CaO.SiO2-3CaO.P2O5
B. Hokfors, PhD thesis, Umea 2014, “Cementa” “Phase Chemistry in process models for cement clinker and lime production”
Minor elements in solid solutions can significantly change the polymorph that is stable
2CaO.SiO2
3CaO.P2O5
CaO

## Slide 32
FactSage THERMODYNAMIC DATABASES
for slags developed by PYROSEARCH
(in collaboration with CRCT Ecole Polytechnique de Montreal)
PbO - ZnO- CaO - FeO -Fe2O3 - Al2O3 - SiO2
SiO2 - Al2O3 - CaO - FeO - Fe2O3 - MgO - Na2O - K2O
“Cu2O”- S -SiO2 - FeO - Fe2O3 - CaO - Al2O3 - MgO
Now extending these to integrated slag/ matte/ metal databases to include
Cu-S-O-FeO-Fe2O3-SiO2-Al2O3-CaO-MgO-Pb
… As-Pb-Zn-Sn-Sb-Bi-Ag-Au … Ni, Se, Te, Pd …

## Slide 33
DATABASES THE NEXT GENERATION - Integration of
experimental results, models and modelling tools
EXPERIMENTS
AND MODELLING
OF VISCOSITIES
Liquid and
partially crystallised
slag systems
CUSTOMISED SOFTWARE
INDUSTRIAL APPLICATIONS
- Slag liquidus / fluxing / blending
- Slag viscosity / flow
    Activity / vapour pressure / enthalpy changes
    Multi-phase equilibrium predictions
PHASE
EQUILIBRIA
EXPERIMENTS
AND
THERMODYNAMIC
MODELLING
- % Liquid
- % Solids
- Slag composition

## Slide 34
Example: Application of thermodynamics to Cement chemistry - FactSage equilibrium predictions
Proportions of phases formed under equilibrium cooling of an “idealised cement mix” in the CaO-SiO2-Al2O3-Fe2O3 system.
B. Hokfors, PhD thesis, Umea, 2014, “Cementa”, “Phase Chemistry in process models for cement clinker and lime production”.

## Slide 35
B. Hokfors, PhD thesis, Umea 2014, “Cementa”, “Phase Chemistry in process models for cement clinker and lime production”.
Example: Application of thermodynamics to Cement chemistry - FactSage predictions Scheil non-equilibrium cooling
Proportions of phases formed under non-equilibrium cooling of an “idealised cement mix” in the CaO-SiO2-Al2O3-Fe2O3 system

## Slide 36
SUMMARY
Experimental studies of phase equilibria
New experimental techniques make it possible to accurately measure
- Phase equilibria in complex oxide systems.
- Elemental partitioning between liquid and solid oxides, sulphides, alloys at controlled temperatures and compositions.
FactSage thermodynamic databases
are available for the prediction of equilibrium and metastable states in systems containing complex oxides, sulphides, alloys.
Slag Viscosities
Experimental measurement can be undertaken at controlled temperatures and compositions.
Quasi-chemical models can accurately predict slag viscosities in complex oxide systems, e.g. CaO-FeO-Fe2O3-SiO2-Al2O3-MgO….

## Slide 37
CONCLUDING STATEMENT
Modern computer platforms enable complex calculations of mass balance, energy balance, thermodynamic calculations (chemical outcomes), process modelling, simulation, optimisation and control.
Underpinning these tools are key fundamental property data on thermochemistry, physico-chemical and chemical thermodynamic properties.
We have the predictive tools but ….
to have accurate tools we need accurate and comprehensive thermodynamic databases
…. this is what we do!!