## Slide 1
Selective Recovery of Phosphorus and Manganese by Carbothermic Reduction
Presenter : Shin Dong-Jun1
Xu Gao2, Shigeru Ueda2, Shin-ya Kitamura2
1 Tohoku University, Graduate School of Engineering
2 Tohoku University, IMRAM

## Slide 2
1. Introduction
2. Experimental
3. Result & Discussion
4. Conclusion
Contents
3.1 Influence of Slag Basicity (CaO/SiO2)
3.2 Influence of Temperature
3.3 Thermodynamic discussion

## Slide 3
Iron Ore
Lime
Stone
Coke
C〮C
Sintering
Ironmaking
Steelmaking
2nd Refining
1. Introduction
Recycling into sintering process…
Al2O3
MgO
SiO2
P2O5
FeO
MnO
CaO
Steelmaking Slag
Fe Source
Accumulation
P2O5 and MnO are necessary to be separated.
Structure raw materials
Cement
Ladle Slag (2nd Refining)
Ironmaking Slag
Dephosphorization Slag
Recycle into steelmaking
P2O5, MnO
Continuous
Casting
3

## Slide 4
r
S. Shiomi et al[1]
- Recovery of Fe and P by carbon reduction
Li et al[2]
- Slag resurrection (P removal by carbon reduction)
Kazuki Mortia et al[3]
- P and Fe recovery by microwave heating processing
Removal of phosphorus by Carbothermic reduction
Removal of Mn is not paid attention
Phosphorus
– Essential nutrients in agricultural production.
Manganese
– Resource for improving mechanic properties of steel
Investigate the possibility of separation of P and Mn by carbothermic reduction
Research Purpose
1. Introduction
Mn Ore
High Carbon
Fe-Mn (303)
Low Carbon
Fe-Mn (48)
Si-Mn (186)
LD Slag
EF Slag
Kton/year
Mineral
resources
Steelmaking
Slag
410
110
Imported
(537)
Dumped
(520)
Steel
Industry
(112)
(156)
Dumped
(93)
Imported
(110)
Phosphate Ore
Fertilizer
(110)
Food, Plant
Recycling Mn and P in Steelmaking Slag
– Alternative Resource
Steelmaking
process
Steelmaking
process
Reference;
[1] S. Shiomi, N. Sano and Y. Matsushita: Tetsu-to-Hagané 63 (1977) 1520–1528, [2] Li, H-J. et al, ISIJ international 35.9 (1995): 1079-1088. [3] Morita Kazuki et al, Journal of Material Cycles and Waste Management 4.2 (2002): 93-101
4

## Slide 5
1. Introduction
Thermodynamic background
Chart: 
| 0.7 | 1 | 1.5
Mn | 0 | 0 | 0.2
P | -14.8 | -16.7 | -18.8
P
Activity coefficient
Basicity (CaO/SiO2)
Chart: 
| 1625 | 1700 | 1925
Mn | 5.1 | 4.3 | 2.8
P | -14.9 | -17.5 | -22.5
Mn
Temperature (K)
Equilibrium Constant (K)
Influence of Slag basicity
Influence of Temperature
Coke
SiO2
Coke
CaO
Scrap
(FeO)
Steelmaking Slag
Fe-C-P
H: MnO
L: P2O5
High: MnO
Low: P2O5
Slag
Fe-Mn-C
Selective Reduction
(Phosphorus)
High Temp.
Low Basicity
Selective Reduction
(Manganese)
Low Temp.
High Basicity
Cleaned Slag
Fertilizer
Source
Ferromanganese
Source
Recycle
Sintering Process
Fig. 1 Effect of slag basicity and temperature
for phosphorus and manganese oxidation
Reduced Slag
5

## Slide 6
 | FeO | CaO | SiO2 | P2O5 | MnO | MgO | Al2O3 | Basicity (CaO/SiO2) | Note
Slag A | 23.36 | 29.87 | 20.07 | 4.06 | 5.61 | 3.43 | 13.60 | 1.49 | High C/S
Slag B | 26.27 | 25.70 | 25.54 | 3.77 | 6.02 | 3.67 | 9.03 | 1.01 | Middle C/S
Slag C | 25.10 | 23.10 | 30.43 | 3.91 | 5.54 | 3.71 | 8.22 | 0.76 | Low C/S
2.1 Sample Preparation
Table. 1 Synthesized slag compositions (mass %)
Crush &
Mixing
Synthesis
Carbothermic
Reduction
Analysis
Crucible : Al2O3
Atmosphere : Ar gas
Temperature : 1400 ℃ (1 hour)
Slag Powder Size : Less than (500 μm)
Mixing slag with graphite
2. Experimental
6

## Slide 7
2.2 Carbothermic Reduction Condition
Table. 2 Carbothermic Reduction Condition | 
Temperature (K) | 1673, 1773, 1873
Reduction Time (min) | 20, 40, 80
Ar gas flow (ml/min) | 500
Graphite amount | 200 % (Stoichiometry)
2.3 Mass Balance Calculation
Total mass of Slag(g) = CaO mass (g) initial in slag / (CaO %) after reduction * 100 ························· (1)
Total mass of Metal(g) = Iron mass (g) reduced mass from slag / [Fe %] after reduction* 100 ················ (2)
Phosphorus mass (g) in Metal = Total metal mass (g) x [P %] after reduction * 100
Manganese mass (g) in Metal = Total metal mass (g) x [Mn %] after reduction * 100
Sample Analysis
ICP-AES (inductively coupled plasma)
CIP (combustion infrared spectrometer)
2. Experimental
Gas Inlet
(Al2O3 tube)
Ceramic
Reaction
Tube
Gas
Outlet
Gas Flow Controller
Sample
Ar Gas
Mixed with Graphite
Crucible
Al2O3
3g slag + Graphite
MaOb + bC = aM + bCO
7

## Slide 8
Fig. 3 Slag and metal composition changes analyzed
by ICP with reduction time
Chart: 
| 0 | 20 | 40 | 80
Mn | 0 | 1.5125 | 2.6854 | 5.98
P | 0 | 6.2966 | 7.2857 | 8.1056
C | 0 | 2.0346 | 2.011 | 1.7431
Chart: 
| 0 | 20 | 40 | 80
Al2O3 | 9.0292 | 29.4666 | 36.8727 | 40.8275
CaO | 25.6999 | 27.1997 | 26.5719 | 26.2775
FeO | 26.2725 | 5.6409 | 1.5033 | 0.47626
MgO | 3.6674 | 3.6486 | 3.7251 | 3.2097
MnO | 6.0238 | 5.5991 | 4.5049 | 2.4904
P2O5 | 3.7724 | 1.34 | 0.47727 | 0.090837
SiO2 | 25.5395 | 27.1101 | 26.3493 | 26.6278
Slag B (C/S=1.01)
Slag Composition (Mass %)
Reduction time (min)
Fig. 2 Sample image after 20 mins reduction
3.1 Influence of Slag Basicity (CaO/SiO2)
Al2O3 concentration
Dissolution from Al2O3 crucible
General reduction tendency
Fe P Mn
Al2O3 Crucible
Reduced Slag
Metal
10 mm
Metal Composition (Mass %)
Metal & Slag Separation
Residual graphite
Carbon composition in metal = saturated
8

## Slide 9
Fig. 4 Slag and metal composition changes analyzed by ICP with reduction time
(Influence of slag basicity)
3.1 Influence of Slag Basicity (CaO/SiO2)
Chart: MnO Contents in Slag
| 0 | 20 | 40 | 80
Slag C | 5.6135 | 2.4448 | 1.9233 | 0.80547
Slag D | 6.0238 | 5.5991 | 4.5049 | 2.4904
Slag E | 5.5382 | 6.2651 | 4.9264
Chart: P2O5 Contents in Slag
| 0 | 20 | 40 | 80
Slag C | 4.0567 | 2.7568 | 2.2155 | 1.6751
Slag D | 3.7724 | 1.34 | 0.47727 | 0.090837
Slag E | 3.9124 | 0.16165 | 0.0616
Chart: Mn Contents in Metal
| 0 | 20 | 40 | 80
Slag C | 0 | 12.5696 | 13.4557 | 16.161
Slag D | 0 | 1.5125 | 2.6854 | 5.98
Slag E | 0 | 0.95344 | 2.2661
Chart: P Contents in Metal
| 0 | 20 | 40 | 80
Slag C | 0 | 3.2424 | 3.7459 | 4.2238
Slag D | 0 | 6.2966 | 7.2857 | 8.1056
Slag E | 0 | 7.9921 | 8.0447
Slag Composition (Mass %)
Metal Composition (Mass %)
1773K
1773K
1773K
1773K
9

## Slide 10
Chart: Mass Balance of Manganese
| Total | 20 | 40 | Total | 20 | 40 | Total | 20 | 40
Metal | 0.13042 | 0.071728 | 0.087815 | 0.13995 | 0.0081937 | 0.017664 | 0.12867 | 0.0060475 | 0.014811
Slag | 0.043802 | 0.033857 | 0.12292 | 0.10123 | 0.12263 | 0.11415
Unknown | 0.014893 | 0.0087505 | 0.0088454 | 0.021059 | 0 | 0
Chart: Mass Balance of Phosphorus
| Total | 20 | 40 | Total | 20 | 40 | Total | 20 | 40
Metal | 0.053114 | 0.018503 | 0.024446 | 0.049392 | 0.032815 | 0.043348 | 0.051225 | 0.049164 | 0.050421
Slag | 0.027833 | 0.021979 | 0.016577 | 0.0060437 | 0.002061 | 0.00080433
Unknown | 0.0067782 | 0.0066884 | 0 | 0 | 0 | 0
Fig. 5 Mass balance results of Slag A (C/S= 1.49), Slag B (C/S=1.01) and Slag C (C/S=0.76)
(Left : Manganese, Right : Phosphorus)
3.1 Influence of Slag Basicity (CaO/SiO2)
Decreasing slag basicity
Reduction of manganese - suppressed
Reduction of phosphorus - promoted
Slag E(C/S=0.76) 20 mins reduction
Separation of P and Mn was achieved
10
55.00
33.58
11.42
67.33
25.96
6.71
12.62
72.33
15.05
5.85
87.83
6.32
11.51
88.71
4.70
95.30

## Slide 11
3.2 Influence of Temperature (Slag C, C/S=0.76)
Slag Composition (Mass %)
Metal Composition (Mass %)
Chart: MnO Content in Slag
| 0 | 20 | 40
1673K | 5.5382 | 6.2521 | 5.1074
1773K | 5.5382 | 6.2651 | 4.9264
1873K | 5.5382 | 5.3561 | 4.3759
Chart: P2O5 Content in Slag
| 0 | 20 | 40
1673K | 3.9124 | 1.6412 | 0.4569
1773K | 3.9124 | 0.16165 | 0.0616
1873K | 3.9124 | 0.12656 | 0.031604
Chart: Mn Content in Metal
| 0 | 20 | 40
1673K | 0 | 0.41197 | 1.7662
1773K | 0 | 0.95344 | 2.2661
1873K | 0 | 0.99844 | 3.9375
Chart: P Content in Metal
| 0 | 20 | 40
1673K | 0 | 5.6744 | 6.5838
1773K | 0 | 7.9921 | 8.0447
1873K | 0 | 7.667 | 8.0727
1773K
1673K
1873K
1773K
1673K
1873K
1773K
1673K
1873K
1773K
1673K
1873K
Fig. 6 Slag C (C/S = 0.76) composition changes analyzed by ICP with reduction time
(Influence of temperature)
11

## Slide 12
Fig. 7 Slag C (C/S = 0.76) mass balance result with different temperature
(Left : Manganese, Right : Phosphorus)
3.2 Influence of Temperature (Slag C, C/S=0.76)
Increasing temperature promotes reduction of phosphorus and manganese simultaneously
Reduction of phosphorus at higher temperature is more favorable than manganese
Chart: Mass Balance of Manganese
| Total | 20 | 40 | 20 | 40 | 20 | 40
Metal | 0.12867 | 0.0023877 | 0.011316 | 0.0060475 | 0.014811 | 0.0063666 | 0.026386
Slag | 0.12012 | 0.094364 | 0.12263 | 0.11415 | 0.12298 | 0.10279
Unknown | 0.0061642 | 0.022994 | 0 | 0 | 0 | 0
Chart: Mass Balance of Phosphorus
| Total | 20 | 40 | 20 | 40 | 20 | 40
Metal | 0.051225 | 0.032888 | 0.042182 | 0.049164 | 0.050421 | 0.049587 | 0.050807
Slag | 0.017769 | 0.004757 | 0.002061 | 0.00080433 | 0.0016375 | 0.00041834
Unknown | 0.00056757 | 0.0042857 | 0 | 0 | 0 | 0
12

## Slide 13
Chart: aP2O5 (Initial Composition)
| 0.76 | 1.01 | 1.49
aP2O5 | 3.5202e-14 | 3.2827e-15 | 1.7604e-16
aP2O5 (10mass% Al2O3) | 3.5589e-14 | 3.311e-15 | 1.5569e-16
Basicity (CaO/SiO2)
Chart: aMnO (Initial Composition)
| 0.76 | 1.01 | 1.49
aMnO | 0.022905 | 0.034439 | 0.041945
aMnO (10mass % Al2O3) | 0.021337 | 0.033167 | 0.049085
Basicity (CaO/SiO2)
Chart: aP2O5 (Initial Composition)
| 1673 | 1773 | 1873
aP2O5 | 5.2621e-15 | 3.5202e-14 | 1.9142e-13
aP2O5 (10mass% Al2O3) | 5.302e-15 | 3.5589e-14 | 1.9389e-13
Temperature (K)
Chart: aMnO (Initial Composition)
| 1673 | 1773 | 1873
aMnO | 0.019423 | 0.022905 | 0.026416
aMnO (10mass % Al2O3) | 0.018082 | 0.021337 | 0.024619
Temperature (K)
3.3 Thermodynamic discussion
Fig. 8 Activities changes by basicity and temperature calculated by Factsage
13

## Slide 14
Influence of slag basicity
- Decreasing slag basicity increased reduction of phosphorus while
suppressing that of manganese.
- Separation of phosphorus and manganese was achieved at 0.76 slag
basicity after 20 min carbothermic reduction
Influence of temperature
- Higher temperature carbothermic reduction promotes both P and Mn
than low temperature
- Reduction of phosphorus at higher temperature is more favorable than manganese
4. Conclusion
THANK YOU FOR LISTENING
Shin Dong Jun
E-mail : Shindj@mail.tagen.tohoku.ac.jp
14