## Slide 1
<number>
PRODUCTION OF CEMENT EXTENDER FROM MANGANESE SLAGS
W. K. Banda, H. Lagendijk
Leuven, April 5th 2017

## Slide 2: OUTLINE
Introduction
Processing concepts
Objectives
Technical results
Thermodynamic simulation
Summary
Acknowledgements
<number>
http://www.dailymail.co.uk

## Slide 3: INTRODUCTION
<number>
Products from the manganese ferroalloy industry include alloy and slag:
Alloy has monetary value
Slag is classified as a hazardous product due to the MnO content
20 Mt of HCFeMn and SiMn slag has accumulated over the years on dumps in South Africa1
On average 0.5 Mt are added to these dumps each year1
[1] Steenkamp, J.D. & Basson, J., 2013. The manganese ferroalloys industry in southern Africa. Journal of The Southern African Institute of Mining and Metallurgy, 113, pp.667–676.
Tilting pot
Electrode
Slag
Silicomanganese
© Joalet Steenkamp
© Joalet Steenkamp
Notes: Mn leaches from the slag and potentially to ground water, most of all takes up land space for
<number>

## Slide 4: PROCESSING CONCEPT
<number>
Initial approach:
Conditioning of manganese waste slag for the utilization as a cement extender
Dilution of the manganese content using fluxes, including calcined lime, silica sand and alumina
Uneconomical due to the ratio of slag: flux = 1:4
New concept:
Metallothermic reduction of the manganese waste slag
Mintek’s Pyrosim thermodynamic simulation
Experimental trial tests using a 40 kW DC “tilting” pot
Lower flux requirements and two commercial products
Metal box
Tilting pot
Electrode
© Puso Ntikang
Notes: The initial approach to reusing manganese ferroalloy slag, cement producers condition the manganese waste slag for the utilization as a cement extender
<number>

## Slide 5: OBJECTIVES
<number>
Conditioned slag target specifications:
Parameter | Specification
Basicity (B3) = [(MgO+CaO)/SiO2] | ≥ 1*
∑ MgO+CaO+SiO2 | ≥ 66.7%*
MnO | < 8%
Glass (amorphous) content | > 95%*
Test leachability of the conditioned slag
Economic viability analysis
Strength tests
*From specifications of GGBFS EN-197
MnO specification was based on previous leaching test results.
Notes: <number>

## Slide 6: TECHNICAL RESULTS
<number>
The modified granulated slag met the Ground Granulated Blast Furnace Slag (GGBFS) specifications (EN-197)
Parameter | GGBFS specs | Modified slag
∑ MgO+CaO+SiO2 | > 67% | 80%
B3 = [(MgO+CaO)/SiO2] | ≥ 1 | 0.9 to 1.05
Glass content | > 95% | 99%
MnO | N/A | 8 ± 2%
1-5mm particles

## Slide 7: TECHNICAL RESULTS
<number>
SiMn alloy produced met the ASTM specifications:
Element | SiMn specs | Alloy produced
Si | Grade C1: 12.5 - 16 | 18 ± 5%
 | Grade B1: 16 – 18.5 | 
 | Grade A1: 18.5 – 21 | 
Mn | 65 to 68 | 70 ± 5%
1 ASTM Standards A483 / A483M - 10, “Standard Specification for Silicomanganese.” ASTM International, West Conshohocken, PA, 2003, pp. 1–2, 2010.
Entrained alloy product
10 mm
Alloy product
50 mm
Products:

## Slide 8: TECHNICAL RESULTS
<number>
Leaching stability tests
TCLP#
SPLP*
Environmental conditions
Landfill conditions
  * Synthetic Precipitation Leaching Procedure #Toxicity Characteristic Leaching Procedure

## Slide 9: TECHNICAL RESULTS
<number>
Leaching stability tests
TCLP#
SPLP*
Environmental conditions
Landfill conditions
Not tested
  World Health Organization (WHO) standards were met with respect to Mg, Al, As, Co, Cr, Cu, Fe, Mn, Mo, Ni, Pb, V, Zn , Cd, and Hg.

## Slide 10: THERMODYNAMIC SIMULATION
<number>
* Average composition from 6 taps
# Average composition from 4 bags of slag
Composition in mass %
The compositions of the slags produced in the actual tests were similar to the compositions predicted by Pyrosim
Notes: <number>

## Slide 11: THERMODYNAMIC SIMULATION
<number>
Significant decrease!!!
31% to 8%
* Average composition from 6 taps
# Average composition from 4 bags of slag
Notes: <number>

## Slide 12: THERMODYNAMIC SIMULATION
The compositions of the slags produced in the actual tests were similar to the compositions predicted by Pyrosim (results in wt%)
<number>
 | Basicity (CaO+MgO)/SiO2 | ΣCaO+MgO+SiO2
Actual test results (average)* | 1 | 80
Standard deviation | 0.03 | 0.88
Pyrosim | 1 | 77
*Average composition from 6 taps
Notes: <number>

## Slide 13: THERMODYNAMIC SIMULATION
<number>
Test | Components |  |  | 
 | Fe | Mn | Si | Total
Actual test results (average)* | 6 | 74 | 17 | 98
Standard deviation | 0.93 | 0.93 | 3.40 | 2.57
Pyrosim | 6 | 74 | 20 | 100
*Average composition from 6 taps
The compositions of the alloys produced in the actual tests were similar to the compositions predicted by Pyrosim (results in wt%)
Notes: <number>

## Slide 14: SUMMARY
Technical evaluations:
The production of a cleaner slag with low MnO, concurrently with SiMn alloy was successful
There were minor deviations between the Pyrosim simulations and the actual averaged results
Slag met the specifications for the GGBFS (EN-197)
Very stable slag under aggressive acid leaching conditions
Slag can be used as a cement extender
<number>
Notes: <number>

## Slide 15: SUMMARY
Techno-economic evaluations:
Dumped HCFeMn can be processed profitably by remelting and slag treatment in an EAF
SiMn slag would need to be modified in the molten state using a ladle/ladle furnace, in order for the process to be economically viable
It is more profitable to use silicon and FeSi than aluminium as the reductant and bauxite as a flux
The processing of manganese waste slag according to the new concept was found to be economically feasible
<number>
Notes: A high level techno-economic evaluation was conducted on six conceptual flowsheets for a plant modifying 355 kt/annum of waste slag. Because of different MnO levels in the starting waste slag, it was found that
<number>

## Slide 16: ACKNOWLEDGEMENTS
<number>
Herman Lagendijk
This work is published by permission of Mintek. Mintek acknowledges the support of NIPMO (South Africa’s National Intellectual Property Management Office) in the ongoing maintenance of its IP portfolio.
Notes: <number>

## Slide 17
<number>
THANK YOU
www.mintek.co.za
wesleyb@mintek.co.za
hl@mintek.co.za
© Joalet Steenkamp
© Joalet Steenkamp