## Slide 1: INVESTIGATION ON THE MECHANISMS OF BIO-PROCESSING VANADIUM SLAGS
By DR Willie Nheta 05 April 2017

## Slide 2
Content
Introduction and Back ground
Research Justification
Methodology
Results and Discussion
Conclusion

## Slide 3: INTRODUCTION AND BACK GROUND
Highveld Process – South Africa
New Zealand Process – New Zealand
Pan steel Process – China
NTMK Duplex Process – Russia
Source -Metal Bulletin

## Slide 4: INTRODUCTION AND BACK GROUND
SLAG
Sybit.com

## Slide 5: INTRODUCTION AND BACK GROUND

## Slide 6: INTRODUCTION AND BACK GROUND
Vanadium slag
Na2CO3
Alkaline
Roasting
Leaching
NaOH + Na2CO3
Roasted slag
ɳ V = 80%

## Slide 7: RESEARCH JUSTIFICATION
Photograph by Greg Girard
COST
COMPLEX
POLLUTION

## Slide 8: RESEARCH JUSTIFICATION
Beolichni, 2009 – Bioleaching of iron from exhaust catalyst.
Mohamad, 2011 – Recovery of vanadium using heterotrophic bacteria Pseudomonas Putida
Mirazimi 2015 – Vanadium recovery using Fungi
- Bacteria
Vale.com

## Slide 9: RESEARCH JUSTIFICATION
Microorganisms can mobilise metals by:
Formation of organic acids
Oxidation and reduction reaction,
Extraction by complexion,
Chelate formation

## Slide 10: AIM
To simulate the bioleaching of vanadium from slags using organic acids produced by Pseudomonas putida and Aspergellius niger.

## Slide 11: METHODOLOGY
CHARACTERISATION
PRE-TREATMENT OF THE SAMPLE
Roasting
800ºC 10% Na2CO3
SAMPLE COLLECTION
XRD, XRF, SEM/EDX
LEACHING WITH ORGANIC ACIDS (Gluconic, Citric, Oxalic)
S/L
Separation
AAS

## Slide 12: RESULTS AND DISCUSSION
Table 1. Chemical composition of the slag sample
Component | MgO | Al2O3 | SiO2 | CaO | V2O5 | Fe2O3
% Wt | 7.2 | 60.3 | 1.6 | 23.8 | 4.3 | 1.07
% Elemt | 4.3 | 31.9 | 0.7 | 17 | 2.4 | 0.7

## Slide 13: RESULTS AND DISCUSSION
Fig 1. XRD pattern of the slag sample

## Slide 14: RESULTS AND DISCUSSION
 | Percentage |  |  |  |  |  | 
POINT | V205 | MgO | CaO | Al203 | SiO2 | FeO | Phase Mineral
a | 11.47 |  | 3.54 | 76.95 | 6.13 | 1.02 | Spinel
b | 91.18 | 3.63 | 4.17 |  | 0.76 | 0.37 | Vanadium oxide
c |  | 6.05 | 5.79 | 38.89 | 4.94 | 43.30 | Grossite
d | 0.33 |  | 12.15 | 86.62 | 0.90 |  | Calcium aluminium oxide
Fig 2. SEM photomicrograph of the slag sample

## Slide 15: RESULTS AND DISCUSSION
Fig 3. XRD pattern of raw and roasted slag

## Slide 16: RESULTS AND DISCUSSION
Fig 4. Effect of acid concentration on recovery of vanadium from raw slag
Chart: Acid concentration, mM
| 0 | 50 | 100 | 150
Gluconic acid | 0 | 2.4991 | 2.8897 | 3.1454
Citric acid | 0 | 3.966 | 3.8352 | 4.3486
Oxalic acid | 0 | 6.2656 | 6.3392 | 6.8392

## Slide 17: RESULTS AND DISCUSSION
Fig 5. Effect of acid concentration on vanadium recovery – roasted slag
Chart: Acid concentration, mM
| 0 | 50 | 100 | 150
Gluconic acid | 0 | 90.8183 | 81.6394 | 85.0685
Citric acid | 0 | 34.2144 | 54.3317 | 62.3183
Oxalic acid | 0 | 15.1622 | 54.1972 | 55.8111

## Slide 18: RESULTS AND DISCUSSION
Chart: Time , min
| 0 | 20 | 40 | 60 | 80 | 100 | 120 | 140 | 160 | 180
Gluconic acid | 0 | 77.4239 | 80.975 | 85.1578 | 81.9167 | 82.0911 | 75.4306 | 92.1239 | 83.8922 | 85.0685
Citric acid | 0 | 67.4117 | 70.3994 | 65.1117 | 68.0528 | 67.3417 | 63.81 | 64.2911 | 66.8317 | 62.3183
Oxalic acid | 0 | 53.7083 | 45.9733 | 79.0061 | 77.4667 | 85.0922 | 73.1078 | 70.48 | 57.9194 | 55.8111
Fig 6. Effect of leaching time on vanadium recovery

## Slide 19: CONCLUSION
Vanadium can be leached from roasted V- bearing slag using very low concentrations of gluconic, oxalic and citric acid.
The results suggest that gluconic acid is the best leachate followed by citric acid and then oxalic acid.
Optimum leaching time using all acids is 60mins.
Further studies needs to target bacteria that produces more of gluconic acid as compared to the other two.

## Slide 20: THANK YOU

## Slide 21: REFERENCES
Song, W.C., Li, H., Fu-xing, Z.H., Li, K., Zheng, Q, 2004. Extraction of Vanadium from molten Vanadium bearing slag by oxidation with pure Oxygen in the presence of CaO. Transactions of Nonferrous Metals Society of China, vol. 24. pp. 2687−2694.
Mirazimi, M., Rashchi E, 2011. Optimization of bioleaching of a Vanadium containing slag using RSM. 7th International Chemical Engineering Congress & Exhibition. pp. 21-24.
Bayraktar, O, 2005. Bioleaching of Nickel from equilibrium fluid catalytic cracking catalysts. World Journal of Microbiology & Biotechnology, vol. 21, pp. 661–665.
Behera, S.K., Panda S.K., Pradhan N., Sukla L.B., Mishra B.K, 2012. Extraction of Nickel by microbial reduction of lateritic chromite overburden of Sukinda, India. Bioresource Technology, Vol 125. pp. 17–22.
Zhang, G., Zhang, T., Lü, G., Zhang Y., Liu, Y., and Liu, Z., 2015. Extraction of Vanadium from Vanadium slag by high pressure oxidative acid leaching. International Journal of Minerals, Metallurgy and Materials, vol 22. pp. 21.
Biswas, S., Dey, R., Mukherjee, S., Banerjee, C.P., 2013. Bioleaching of Nickel and Cobalt from Lateritic Chromite Overburden Using the Culture Filtrate of Aspergillus niger. Appl Biochem Biotechnol, vol. 170, pp. 1547–1559.