## Slide 1
Yanling Zhang Ph.D
State Key Laboratory of Advanced Metallurgy
University of Science and Technology Beijing, China
Thermodynamic prediction for chromium reduction behavior from molten slag

## Slide 2
1.Background
 18-33 kg/t dust produced in stainless steel making process;
 Capital of Cr/Ni-bearing raw materials, ≥ 50% production cost.
Annual out put of stainless steel, million ton
Year
35
30
25
20
15
10
5
0
China
Worldwide

## Slide 3
1.Background
 18-33 kg/t dust produced in stainless steel making process;
 Capital of Cr/Ni-bearing raw materials, ≥ 50% production cost.
Stainless steel slag wt.%
From | CaO | SiO2 | MgO | Cr2O3 | Al2O3 | Fe2O3 | TiO2 | MnO | NiO | CaF2 | other
Baosteel Co., Ltd. | 44.5 | 28.0 | 9.3 | 8.3 | 3.2 | 3.1 | 2.1 | 0.7 | — | — | 0.8
Jiuquan iron and steel company (JISCO) | 35.7 | 25.6 | 12.3 | 13.4 | 2.1 | 2.5 | 0.8 | 1.6 | — | 3.7 | 2.3
Stainless steel dust wt.%
From | Fe2O3 | Cr2O3 | NiO | CaO | SiO2 | MgO | Al2O3 | MnO | other | Σ(Fe+Cr+Ni+Mn)
Baosteel Co., Ltd. | 20.9 | 28.1 | 0.1 | 31.3 | 5.3 | 10.6 | 2.4 | — | 1.3 | 33.9
Jin hui stainless steel Co., Ltd. | 41.9 | 9.3 | 0.7 | 26.7 | 2 | 2.2 | — | 7.7 | 9.5 | 42.2

## Slide 4
stainless steel dust
Fe-Cr-Ni-C (-Si/Al) melt
CaO-SiO2-MgO-Al2O3 based
slag
Smelting treatment
 Smelting is a promising method to recovery Fe/ Cr/Ni resources from stainless steel dust;
 Compared to Fe2O3 and NiO, Cr2O3 is much more difficult to be reduced;
 Behaviors of Cr in Fe-Cr-Ni-C (-Si/Al) melt and CaO-SiO2-MgO-Al2O3 based slag are necessary knowledge；

## Slide 5
2.Thermodynamic predictions
2.1 Activity coefficient of Cr in Fe-Cr-Ni-C(-Si/Al) melt
Redlich-Kister polynomial:
In Fe-Cr-C melts:

## Slide 6
(b)
(a)
(c)
(d)

## Slide 7
2.2 Activity coefficient of CrO in CaO-SiO2-MgO-Al2O3-3%CrO
 T , PO2 , 
 It was assumed that the oxides state of chromium in residual slag is CrO during smelting treatment of stainless steel dust.
 Liquid areas of 1823–1923K in CaO-SiO2-Al2O3/MgO-3%CrO systems were predicted by using of Phase Diagram Module of FactSage software; Iso-activity coefficient lines of CrO at1873 K in the above systems were predicted by using FactSage software based on a modified quasichemical model.
by L.J. Wang and S. Seetharaman

## Slide 9
2.3 Final (%Cr) in CaO-SiO2-Al2O3-MgO-CrO slag when equilibrating with different melts
Effect of [%C] on (%Cr)
a
c
b

## Slide 10
Influence of [%Si] on %Cr
Influence of temperature on (%Cr)
in melt phase increases with increasing temperature, which means high T does not benefit the reduction of CrO in slag when it equilibrates with high Cr melt.

## Slide 11
3.Experiments
成分 | CaO | SiO2 | Al2O3 | MgO | Cr2O3 | CaF2 | FeO | MnO | TiO2 | other | R
% | 35.7 | 25.6 | 2.1 | 12.3 | 13.4 | 3.7 | 3.2 | 1.6 | 0.8 | 1.6 | 1.4
(Fe+Cr+Mn)%=12.8%，Direct discharge or improper management will lead to the pollution of environment and the waste of valuable metal, especially Cr.
3.1 Materials

## Slide 12
Slag pretreatment：Crashing—Fine grinding—Removing Iron particle—Screening to 60 mesh——Drying
Procedure：20g metal (Pig iron or Fe-xC) was set in the bottom of MgO crucible and 20g the slag block containing reductant (C, 78%SiFe, or Aluminum) and flux (SiO2,CaO, or Al2O3) was pressed under the 20MPa and then was charged above the metal.
3.2 Apparatus
MgO Crucible

## Slide 13
3.3 Results
Fig.1 Effect of [%C] in Fe-C melts on (%Cr) and ƞCr
ηCr—Reduction ratio of Cr
Mf,m—Final weight of metal, g
Wf,Cr—The content of Cr in the final metal, wt.%
Mi,m—Inital weight of metal, g
Wi,Cr—The content of Cr in the inital metal, wt.%
Mi,s—The initial weight of slag,g
Wi,Cr—The content of Cr in the inital slag, wt.%
20g Fe-xC and 20g stainless steel slag, 1550℃, 20min

## Slide 14
Fig.2 Different C/SiFe/Al-containing slag pellets reduced by Fe-5.0C melts
Fig.3 Different C/SiFe/Al-containing slag pellets reduced by Fe-1.9C melts
Experiment condition
20g Fe-xC and 20g stainless steel slag
The addition quantity of reductant is based on the oxygen combined with Fe, Cr, and Mn in the slag
The sample was kept at 1550℃ for 20min

## Slide 15
Fig.4 Time dependent of Cr in slag and metal
Experiment condition
20g pig iron (C: 4.61%, Si: 0.42%, Cr: 0.014%) and 20g stainless steel slag
The addition quantity of high-pure graphite is based on the oxygen combined with Fe, Cr, and Mn in the slag
A little SiO2 (about 1g ) was added to the pellets to adjust the final basicity to 1.1
The sample was kept at 1550℃ for 5, 10, 20, 40 min to find the proper holding time
Fig.5 Effect of time on (%Cr) and ƞCr

## Slide 16
Metal | Reductant | Flux | [C]final % | η % | (Cr)slag %
Fe-5.0C | — | — | 4.08 | 40.6 | 6.14
Fe-5.0C | nC:nO=1.0 | — | 5.07 | 80.7 | 0.55
Fe-5.0C | nC:nO=1.0,nSi:nO=0.1 | — | 5.42 | 89.7 | 0.39
Fe-5.0C | nC:nO=1.0,nAl:nO=0.1 | — | 5.39 | 88.8 | 0.42
Fe-1.9C | nC:nO=1.0 | — | 2.41 | 81.2 | 1.04
Fe-1.9C | nC:nO=1.0,nSi:nO=0.1 | — | 2.71 | 83.0 | 0.63
Fe-1.9C | nSi:nO=0.5 | — | 2.04 | 92.6 | 0.33
Fe-1.9C | nSi:nO=0.75 | — | * | * | 0.12
Fe-1.9C | nAl:nO=2:3 | — | * | * | 0.12
Fe-1.9C | nC:nO=1.0,nSi:nO=0.1 | SiO2 | * | * | 0.59
Fe-1.9C | nC:nO=1.0,nSi:nO=0.1 | CaO | * | * | 0.88
Pig iron | nC:nO=1.0 | SiO2 | 4.46 | 87.8 | 0.38
Table Comparison of chromium oxides reduction by different melts
* The [C], [Cr] in metal has not been detected.

## Slide 17
4.1 Conclusions
γCr decreases with Increasing [%C], increasing [%Si], and decreasing [%Al] in metal phase. And, γCr increases with increasing temperature.
Activity of CrO in CaO-SiO2-MgO(Al2O3)-3%CrO increases with increasing basicity (%CaO/%SiO2). %Al2O3 gives little influence on aCrO, while it was helpful to increase the ratio of the liquid phase.
Thermodynamically, (%Cr) of slag greatly decreases as the [%C] of a metal increases. For the high [%Cr] and low [%C] metal melt, Si has limited reducibility for CrO in slag. Temperature has different effects on the reduction of CrO in slag and depends on the effective reductant in the melt.
The effective reduction of high Cr-containing slag must rely on self-reduction and proper addition of C, SiFe, and Al increases the ηCr extensively. High [C] pool is beneficial to keep the low [Cr] in the metal, which is consistent with the calculation from Factsage equilib module.
Compared with C, SiFe and Al have stronger reducibility. Considering the economy, a little addition of SiFe or Al will promote the reduction of CrOx once the C was chosen as the main reductant. The final slag composition has remarkable influence on the (Cr)slag and the work will be carried out.

## Slide 18
Thanks for your attention!