## Slide 1: Utilization of activated GGBS for non-reinforced concrete applications
Ludovic ANDRE, Laurent STEGER, Diane ACHARD, Laurent FROUIN, Martin CYR
3-5 April 2017, 5th Slag Valorisation Symposium, Leuven, Belgium

## Slide 2
Introduction
Industrial trials (low GGBS content)
Laboratory development (increasing GGBS content)
Conclusion
Summary

## Slide 3
Non-reinforced concrete applications: dry concrete
  Blocks, kerbs, pavers, slabs, pool coping…
  Without standards on concrete (NF EN 206)
  Immediate or delayed demoulding
Interest of GGBS in the products
  Reduction of carbon footprint
  Cost/cement (CEM I ; CEM II)
  Reduction or elimination of efflorescence
Introduction

## Slide 4
Technical:
  Low binder content < 10%
  Low W/B ratio < 0.4
  Irregular PSD of aggregates
  Instant demoulding
  Short curing in various conditions (cold)
Introduction
Difficulties to overcome with GGBS
GGBS:
  Slow hydration speed
  Favour desiccation
  Needs to harden faster
GGBS activation
(Fineness)
Thermal
Chemical

## Slide 5
Industrial trials: low GGBS content
= industrial trials with moderate quantity of GGBS
Activation for dry concrete applications has to remain cheap:
Historical activator for non reinforced applications: chlorides
Results from literature + internal works: sulfates (alkali)
Trials in 3 different plants, with several activators
2 ways to add chemical activators
per mass of total binder
per mass of GGBS only
Association to lower Cl- content
NaCl
Na2SO4
NaCl + Na2SO4
The more GGBS, the more activator
Compressive strength measured after 14 days, typical age for testing

## Slide 6
Industrial trials: low GGBS content
Results in Plant ‛A’ and ‛B’ on blocks
Plant ‛A’:
Activator: [1% NaCl + 1% Na2SO4] / total binder
Conservation 2d at 30°C then stockpiled outside
Chemicals allows to enhance GGBS by 10%
Strength of blocks containing GGBS inferior to the
reference (OPC) but over 6 MPa, required by the
producer
Plant ‛B’:
Activator:
Conservation 4d at 28°C then stockpiled outside
50% GGBS without activator = 100% OPC
Impossible to reach good strength with 70+% of
GGBS
2% Na2SO4
0.3% (NaCl + Na2SO4)
1% (NaCl + Na2SO4)
Justifies needs for lab development
Chart: GGBS content (%)
| 30
 | 0.84091
 | 0.86603
 | 1
 | 0.60341 | 0.69296 | 0.63326 | 0.65885

## Slide 7
Industrial trials: low GGBS content
Chart: GGBS content (%)
| 24 | 32 | 40 | 40 | 48 | 50
 | 0.9238 | 0.92083 | 0.90896 | 0.88125 | 0.88521 | 0.83325
 | 1.0709 | 1.0654 | 1.0567
Results in Plant ‛C’ on blocks and curbs
Plant ‛C1’ :Blocks
Activator: [0.4% NaCl + 0.4% Na2SO4] of GGBS content
Conservation 3d at 10-15°C then stockpiled outside
Results were correct up to 48% of GGBS with SAI ≈ 0.9
Plant ‛C2’ :Kerbs
Activator: [0.4% NaCl + 0.4% Na2SO4] of GGBS content
Conservation 1d at 10-15°C then stockpiled outside
Better results than with OPC only

## Slide 8
Already possible to get good results with 50% GGBS with a good curing conditions
Needs for a laboratory development to work on combination of chemicals activation + thermal curing to enhance GGBS content
Industrial trials: low GGBS content

## Slide 9
Laboratory development
Materials
OPC: CEM I 52.5R CE CP2 NF
GGBS: ECOCEM France
Activators: Analytical grade
binder:
aggregates:
Quartz sand
30% 0-2mm + 70% 2-4 mm
Packing favorising some voids
Specific Blaine area (cm²/g) | Density (g/cm3)
4000 | 3.13
4400 | 2.91

## Slide 10
Laboratory development
Methods: 2 phases
    Controled volume + weight
    = controled density
    Blocks density: 1.95 T/m3
    Binder content: 197 kg/m3
Great variability on compressive strength
Switching to phase 2
Vibro-compaction
(10*10*10cm)
ASTM (C90)
(4*4*16cm)
Compressive strength test after 24h

## Slide 11
Laboratory development
Trials at 20°C: effect of chemical activation
Chart: GGBS content (%)
| 90.476190476190482 | 87.962962962962962 | 95.238095238095227 | 95.238095238095227 | 90.476190476190482 | 87.962962962962962 | 95.238095238095227 | 95.238095238095227 | 69.306930693069305 | 91.7 | 91.7 | 89.3 | 88.855721393034827 | 90.476190476190482 | 90.476190476190482 | 69.306930693069305 | 69.306930693069305 | 68.627450980392155 | 68.627450980392155 | 79.207920792079207 | 79.207920792079207 | 71.287128712871279 | 71.287128712871279 | 71.287128712871279 | 71.287128712871279 | 70 | 70 | 69.306930693069305
Without activator | 0.38442
Alkali | 0.506 | 0.998 | 0.48969 | 0.43688 | 0.56708 | 0.77687 | 0.22875 | 0.2225 | 0.54583
Alkali-sulfate | 0.29542 | 0.28604 | 0.35167 | 0.30042 | 0.516 | 0.48167
Cl | 0.50687 | 0.372
Cl-sulfate | 0.416
(OH-,
alkali silicates)
(Na2SO4)
(NaCl,
CaCl2)
(NaCl + Na2SO4)
(NaCl + CaSO4)
Ref: SAI < 0.4
Alkali:
  OH- led to the lowest results
  88%GGBS + 7.4% Sodium silicate = 100% OPC
Other combination: ineffective at 20°C

## Slide 12
Laboratory development
Trials at 30°C: synergy between chemical and thermal activation
Chart: GGBS content (%)
| 90.476190476190482 | 87.962962962962962 | 95.238095238095227 | 95.238095238095227 | 90.476190476190482 | 87.962962962962962 | 95.238095238095227 | 95.238095238095227 | 69.306930693069305 | 91.7 | 91.7 | 89.3 | 88.855721393034827 | 90.476190476190482 | 90.476190476190482 | 69.306930693069305 | 69.306930693069305 | 68.627450980392155 | 68.627450980392155 | 79.207920792079207 | 79.207920792079207 | 71.287128712871279 | 71.287128712871279 | 71.287128712871279 | 71.287128712871279 | 70 | 70 | 69.306930693069305
Without activator | 0.59312
Alkali | 0.64979
Alkali-sulfate | 0.882
Cl | 1.0167 | 0.808
Cl-sulfate | 0.972
Without activator | 0.38442
Alkali | 0.506 | 0.998 | 0.48969 | 0.43688 | 0.56708 | 0.77687 | 0.22875 | 0.2225 | 0.54583
Alkali-sulfate | 0.29542 | 0.28604 | 0.35167 | 0.30042 | 0.516 | 0.48167
Cl | 0.50687 | 0.372
Cl-sulfate | 0.416
 | 1 | 1
Ref: SAI < 0.4 to 0.6
Alkali:
  Low effect of the temperature
Other combination: highlighted synergy between thermal and chemical activation

## Slide 13
Conclusion
With only thermal curing, possible to use 50% of GGBS
To enhance GGBS content over 70%, it is necessary to combine thermal + chemical activation = synergy
Chlorides + Na sulfates combined with temperature is efficient and easy to handle
Alkali-activation could allow to realize Portland cement free concrete, however sodium-silicate is expensive and must be manipulate with precaution

## Slide 14
Perspectives & on going work
2 PhD student currently working on chlorides effect on GGBS blended with OPC binders
  Hydration mechanisms  where do chlorides go in the matrix?
  Durability behaviour  effect on corrosion, releases of chlorides by carbonation?
Would it be possible to include chlorides also in reinforced concrete application without any risks for durability?

## Slide 15
Thank you for your attention!