## Slide 1: EFFECT OF COOLING WATER CHEMISTRY ON HYDRATION OF GRANULATED BLAST FURNACE SLAG
Romain TRAUCHESSEC1, Lyès CHAOUCHE1, Cécile DILIBERTO1, Patrice REEB2, André LECOMTE1, Samyr EL-BEDOUI3, Klaus-Jürgen ARLT2.
1 Institut Jean Lamour, Université de Lorraine, France.
2 Dillinger Hüttenwerke, Germany.
3 Cerema Tomblaine, France.
5th International Slag Valorisation Symposium, 3-5 April 2017, Leuven, Belgium

## Slide 2: INTRODUCTION
Granulated Blast Furnace Slag (GBFS) is commonly used has an hydraulic binder for road construction.
NF EN 14227-2 : Hydraulically bound mixtures — Specifications — Part 2: Slag bound granular mixtures.
Example, base course : 20% GBFS (0/2) + 80% air-cooled blast furnace slag (0/22).
These bounds granular mixtures can be obtained without crushing and without activator (lime, cement).
© Dillinger

## Slide 3: Problematic
Molten blast furnace slag entrance in the granulation system.
Granulated slag storage (0/2) until water content reaches ≈7%.
Vitrified blast furnace slag contains ≈ 7% of quenching water.
Does the chemical composition of this water affects GBFS reactivity ?
© Dillinger
© Dillinger
Quenching with industrial water used in closed circuit.
© J. Alexandre and J.L. Sebilau. Le laitier (1988)

## Slide 4: Experiments
Quenching water chemistry
ICP analysis over 2 weeks.
Two blast furnaces (BF1 and BF2).
GBFS and distilled water mix
Water/Slag = 0.3 or 1.0.
GBFS hydration study
Filtration and interstitial solution analysis (1, 14 and 28 days).
Hydration stopped (isopropanol) then X-ray diffraction after sieving (<100µm).
Electronic microscope observation.
4 samples of GBFS selected
GBFS with similar chemical and physical properties but different cooling water chemistry.

## Slide 5: Results
Chemical composition of the cooling water (mmol/L) |  |  |  |  |  |  |  | 
Sample |  | Ca | Mg |  |  |  |  | 
BF1 | A | 25.1 | 4.0 |  |  |  |  | 
 | B | 24.2 | 3.8 |  |  |  |  | 
 | Average | 24.7 | 3.9 |  |  |  |  | 
BF2 | C | 10.9 | 2.2 |  |  |  |  | 
 | D | 19.6 | 1.8 |  |  |  |  | 
 | Average | 15.2 | 2.0 |  |  |  |  | 
Quenching water chemistry
Chemical composition of the cooling water (mmol/L) |  |  |  |  |  |  |  | 
Sample |  | Ca | Mg |  | Na | K |  | S
BF1 | A | 25.1 | 4.0 |  | 14.6 | 31.7 |  | 23.9
 | B | 24.2 | 3.8 |  | 12.3 | 27.1 |  | 25.4
 | Average | 24.7 | 3.9 |  | 13.5 | 29.4 |  | 24.7
BF2 | C | 10.9 | 2.2 |  | 25.1 | 62.4 |  | 32.6
 | D | 19.6 | 1.8 |  | 18.2 | 49.1 |  | 46.8
 | Average | 15.2 | 2.0 |  | 21.7 | 55.7 |  | 39.7
Cooling water from BF1 contains :
- more calcium and magnesium,
Over 2 weeks of analysis, selection of four representative samples.
- less sodium, potassium and sulfur (= mostly sulfate : chromatography),
- similar quantity of silicon, and chlorine.
Chemical composition of the cooling water (mmol/L) |  |  |  |  |  |  |  | 
Sample |  | Ca | Mg | Si | Na | K | Cl | S
BF1 | A | 25.1 | 4.0 | 0.8 | 14.6 | 31.7 | 61.2 | 23.9
 | B | 24.2 | 3.8 | 0.8 | 12.3 | 27.1 | 55.7 | 25.4
 | Average | 24.7 | 3.9 | 0.8 | 13.5 | 29.4 | 58.4 | 24.7
BF2 | C | 10.9 | 2.2 | 0.7 | 25.1 | 62.4 | 54.9 | 32.6
 | D | 19.6 | 1.8 | 0.8 | 18.2 | 49.1 | 45.8 | 46.8
 | Average | 15.2 | 2.0 | 0.7 | 21.7 | 55.7 | 50.4 | 39.7

## Slide 6: RESULTS
GBFS properties
The four selected samples have similar chemical and physical properties.
GBFS chemical and physical properties |  |  |  |  |  |  |  |  |  | 
Sample |  | Water content (%) | ρ (g/cm3) | Alpha | <80µm (%) | X-ray fluorescence (%) |  |  |  | 
 |  |  |  |  |  | CaO | Al2O3 | SiO2 | MgO | S
BF1 | A | 6.66 | 2.91 | 23 | 1.75 | 41.1 | 11.3 | 38.1 | 6.8 | 0.9
 | B | 6.72 | 2.91 | 19 | 1.51 | 42.2 | 11.4 | 37.3 | 6.8 | 0.9
BF2 | C | 7.27 | 2.91 | 17 | 1.04 | 41.2 | 11.6 | 38.1 | 6.6 | 0.9
 | D | 7.52 | 2.91 | 17 | 2.35 | 41.1 | 12.4 | 37.7 | 6.3 | 1.2
GBFS reactivity :
α ≈ 20 ( )
C x A ≈ 484.

## Slide 7: Results
Chemical composition of the interstitial solution at 14 days (mmol/L) |  |  |  |  |  |  |  |  | 
Sample |  | Ca |  |  |  |  |  |  | 
BF1 | A | 5.7 |  |  |  |  |  |  | 
 | B | 6.1 |  |  |  |  |  |  | 
 | Average | 5.9 |  |  |  |  |  |  | 
BF2 | C | 5.0 |  |  |  |  |  |  | 
 | D | 2.4 |  |  |  |  |  |  | 
 | Average | 3.7 |  |  |  |  |  |  | 
Interstitial water chemistry
Chemical composition of the interstitial solution at 14 days (mmol/L) |  |  |  |  |  |  |  |  | 
Sample |  | Ca |  |  | Na | K |  |  | S
BF1 | A | 5.7 |  |  | 3.8 | 7.3 |  |  | 2.6
 | B | 6.1 |  |  | 5.1 | 9.0 |  |  | 4.3
 | Average | 5.9 |  |  | 4.4 | 8.2 |  |  | 3.5
BF2 | C | 5.0 |  |  | 7.7 | 17.9 |  |  | 9.0
 | D | 2.4 |  |  | 14.3 | 24.3 |  |  | 9.2
 | Average | 3.7 |  |  | 11.0 | 21.1 |  |  | 9.1
less sodium, potassium and sulfur,
Example : interstitial solution composition after 14 days :
The same observations were made after 1 or 28 days of hydration.
pH is between 10.9 and 11.6.
Alike cooling water, interstitial solution for slag from BF1 contains :
more calcium,
- similar quantity of magnesium, silicon, aluminum and chloride.
Chemical composition of the interstitial solution at 14 days (mmol/L) |  |  |  |  |  |  |  |  | 
Sample |  | Ca | Mg | Si | Na | K | Al | Cl | S
BF1 | A | 5.7 | 0.02 | 0.3 | 3.8 | 7.3 | 0.1 | 12.0 | 2.6
 | B | 6.1 | 0.02 | 0.2 | 5.1 | 9.0 | 0.1 | 13.9 | 4.3
 | Average | 5.9 | 0.02 | 0.3 | 4.4 | 8.2 | 0.1 | 13.0 | 3.5
BF2 | C | 5.0 | 0.02 | 0.6 | 7.7 | 17.9 | 0.1 | 15.0 | 9.0
 | D | 2.4 | 0.03 | 0.1 | 14.3 | 24.3 | 0.4 | 12.0 | 9.2
 | Average | 3.7 | 0.02 | 0.4 | 11.0 | 21.1 | 0.2 | 13.5 | 9.1

## Slide 8: Results
Solution composition at 14 days for two Water/Slag ratio (mmol/L) |  |  |  |  |  |  |  |  | 
Sample |  | Ca | Mg | Si | Na | K | Al | Cl | S
BF1 B | W/S=0.3 |  |  |  | 5.1 | 9.0 |  | 13.9 | 
 | W/S=1.0 |  |  |  | 1.5 | 2.7 |  | 4.4 | 
BF2 C | W/S=0.3 |  |  |  | 7.7 | 17.9 |  | 15.0 | 
 | W/S=1.0 |  |  |  | 2.5 | 6.0 |  | 5.0 | 
Solution composition at 14 days for two Water/Slag ratio (mmol/L) |  |  |  |  |  |  |  |  | 
Sample |  | Ca | Mg | Si | Na | K | Al | Cl | S
BF1 B | W/S=0.3 | 6.1 | 0.02 | 0.2 | 5.1 | 9.0 | 0.1 | 13.9 | 4.3
 | W/S=1.0 | 7.2 | 0.01 | 0.5 | 1.5 | 2.7 | 0.0 | 4.4 | 4.7
BF2 C | W/S=0.3 | 5.0 | 0.02 | 0.6 | 7.7 | 17.9 | 0.1 | 15.0 | 9.0
 | W/S=1.0 | 3.8 | 0.01 | 0.7 | 2.5 | 6.0 | 0.1 | 5.0 | 3.5
Water/Slag ratio multiplied by 3.3 = [Cl], [Na] and [K] divided by ≈ 3.3.
Interstitial water chemistry
Interstitial solution composition after 14 days with different Water /Slag ratio :
The same observations were made after 1 or 28 days of hydration or with rinsed GBFS or higher temperature (40°C).
Ca, Si and S are modified but don’t systematically decreased.
Chlorine, sodium and potassium concentrations are linked to the cooling water composition and not the slag dissolution.

## Slide 9: Results
BF1B – 28j – W/S = 0.3
Hydrates (CSH) covering GBFS surface
Ettringite
For these concentrations and pH, hydrates as CSH or ettringite are stable (oversaturation) for all the samples.
Their formation is confirmed by electronic microscopy (SEM and TEM). They are even formed for sample hydrated after elimination of the cooling water (GBFS rinsed).
BF1A - 28d - W/S=0.3 – 20°C
BF2C - 1d - W/S= 1 – 40°C.
BF1A - 28d - W/S=0.3 - GBFS rinsed

## Slide 10: Results
X-ray diffraction analysis of the samples after 28 days of hydration
I Calcite I Ettringite BF1 A BF1 B BF2 C BF2 D
Ettringite and calcite (linked to carbonation of hydrates) are formed in all the samples.
Quantification impossible (<1% of hydrate : thermogravimetric analysis).

## Slide 11: CONCLUSION
BF1B – 28j – W/S = 0.3
Cooling water affects the composition of the interstitial solution during GBFS hydration : it controls K, Na and Cl concentrations.
Ca, Mg, Al, Si and S concentrations can be modified by the quenching water but they are essentially controlled by slag dissolution.
pH and hydrates nature are not significantly modified by the cooling water.
Consequently, influence of cooling water chemical composition on GBFS hydration can only be moderate.

## Slide 12
BF1B – 28j – W/S = 0.3
BF1B – 28j – W/S = 0.3
Thank you for your attention
Do you have any questions?