## Slide 1
INVESTIGATING THE PROPERTIES OF IRON IN INORGANIC POLYMERS WITH 57Fe MÖSSBAUER SPECTROSCOPY
Alexios P. Douvalis
Physics Department
University of Ioannina
Ioannina-Greece

## Slide 2
Outline
Slags and Inorganic Polymers (IP): why 57Fe Mössbauer Spectroscopy.
  Brief introduction and basic parameters.
The state of iron and its properties in synthetic Slags made of binary FeOx-SiO2 (Bi) and ternary FeOx-CaO-SiO2 (Te) oxide systems and the corresponding IPs, as seen by 57Fe Mössbauer Spectroscopy.
  Estimating the valence, atomic environment and structure.
  Identifying the iron-bearing phases.
  Suggesting paths to explain the role of iron in the IP formation.
  Following the evolution of the 57Fe Mössbauer spectra at different reaction stages of the Slag with the activating SiO2/Na2O-H2O/Na2O solution.
    Monitoring the oxidation of Fe2+ to Fe3+.

## Slide 3
Mössbauer spectroscopy “works” only in solids (those that are, or can become under experimental measuring conditions), and only with particular nuclei, not in soft matter (gases/liquids/loosely bound solids), because the process needs to be recoilless.
Eγ
Εg
Ee
Source
Absorber-Sample
Εg
Ee
Ε0
Nuclear Energy Levels
γ
Recoil-free γ-ray nuclear resonant emission and absorption
simply: Mössbauer spectroscopy
ER=Eγ2/2Mc2≈E02/2Mc2
Eγ=E0 - ΕR
Free
Atom
Recoil Energy
M

## Slide 4
57Fe Mössbauer Spectroscopy
γ-rays
Sample-absorption
(different iron spices in the same phase or in different phases, or both, will appear as different contributions in the spectra)
Source-emission
(stable & identical chemical environment)
Εg
Ee
Eγ
γ
Εg
Ee
Ε0
57Co(Rh)
57Fe
Hyperfine Interactions
(multiple transitions)

## Slide 5
Superposition of several contributions
57Fe Mössbauer Spectroscopy
Source velocity modulation
sample
γ ray detector
Electronics/Recording
Transmission geometry
γ-ray energy modulation is required to achieve absorption resonance
1
2
1
1
2
3
6
5
4
1
2
3
6
5
4
QS
IS
IS
IS
IS
Bhf
Bhf
ε
Hyperfine Interactions-Mössbauer Parameters
atomic environment
valence state
coordination
magnetic properties
structure
Isomer Shift (IS)
IS & Quadrupole Splitting QS
IS & Hyperfine Magnetic Field (Bhf)
IS & Bhf &
Quadrupole Shift (2ε)
Fe3+
Fe2+a
Fe2+b
Α(Fe3+):A(Fe2+a):A(Fe2+b)=2:1:1
Absorption
area (A)
Ratios of Absorption Areas of individual components proportional to the ratios of populations of specific Fe atoms or ions in sample

## Slide 6
Fe3+
Fe2+
0.25-0.55
IS* (mm s-1)
0.75-1.50
0 -1.50
0 - 4.00
QS (mm s-1)
Fe3+
Fe2+
0.25-0.55
IS* (mm s-1)
0.75-1.50
100 - 400
450 -550
Bhf (kG)
Expected values of Mössbauer Parameters for high spin Fe3+ (S=5/2) and Fe2+ (S=2) in Oxides
*IS relative to α-Fe @ 300 K
57Fe Mössbauer Spectroscopy
Coordination: IS(Fe3+/2+)tetrahedral< IS(Fe3+/2+)octahedral

## Slide 7
Synthetic binary FeOx-SiO2 (Bi) and ternary FeOx-CaO-SiO2 (Te) Slags and the corresponding IPs
Table 1. (XRF) |  | 
Starting Mixture Components | Bi (wt.%) | Te (wt.%)
FeO | 73 | 48
SiO2 | 27 | 35
CaO | - | 17
Table 2. XRD-Rietveld analyses (external standard-based) |  |  |  |  |  |  | 
wt.% | Fayalite (Fe2SiO4) | Ca-Fayalite (Fe2-xCax)SiO4 | Magnetite (Fe3O4) | Quartz (SiO2) | Wollastonite (CaSiO3) | Wüstite (FeO) | Amorphous
Bi-Slag | 53.7 | - | 1.5 | 0.4 | - | 2.5 | 41.9
Bi-IP | 42.2 | - | 1.2 | 0.0 | - | 2.0 | 54.6
Te-Slag | 0 | 4.3 | - | 0.7 | 0.7 | 0.9 | 93.4
Te-IP | 0 | 4.9 | - | 0.3 | 0.3 | 0.5 | 94.0
Activating solutions with molar ratios SiO2/Na2O=1.2 and H2O/Na2O=22.
Curing ~ 4 weeks.

## Slide 8
Bi samples
Complete analysis

## Slide 9
Bi samples
Complete analysis

## Slide 10
Te samples
Complete analysis

## Slide 11
Te samples
Complete analysis

## Slide 12
R(Fe3+IP)≈4xR(Fe3+Slag)
Bi-Te samples 77 K Mössbauer spectra comparison
Fe2+
IS=1.26
QS=3.05
ΔQS=0.14
A=85%
Fe2+
IS=1.26
QS=3.05
ΔQS=0.13
A=73%
(Fe3+)
IS=0.43
QS=1.04
ΔQS=0.53
A=4%
Fe3+
IS=0.42
QS=0.82
ΔQS=0.41
A=16%
IS, QS, ΔQS in mm/s (±0.02 mm/s)
Fe3+
IS=0.49
QS=1.24
ΔQS=0.32
A=7%
Fe3+
IS=0.48
QS=0.81
ΔQS=0.39
A=27%
Fe2+1
IS=1.28
QS=2.63
ΔQS=0.42
A=39%
Fe2+2
ISSlag=1.12
QSSlag=2.02
ΔQS=0.55
A=51%
Fe2+1
IS=1.28
QS=2.81
ΔQS=0.32
A=28%
Fe2+2
IS=1.12
QS=2.12
ΔQS=0.55
A=40%
R(Fe3+IP)≈4xR(Fe3+Slag)
Γ/2=(0.14 ±0.02) mm/s
Te[R(Fe3+IP)]≈1.5xBi[R(Fe3+IP)]
ΔQS(Fe2+)-Te > ΔQS(Fe2+)-Bi  enhancement of glass phase formation with Ca addition

## Slide 13
Increase of the amount of Fe3+ with Ca addition
Bi
Te
57Fe Mössbauer Spectroscopy

## Slide 14
57Fe Mössbauer Spectroscopy
Weighted average values
Influence of Ca addition to the electronic configuration & coordination of Fe2+/Fe3+
Bi
Te

## Slide 15
Influence of Ca addition to the electronic configuration & coordination of Fe2+/Fe3+
57Fe Mössbauer Spectroscopy
Weighted average values
Bi
Te

## Slide 16
Enhancement of glass phase formation with Ca addition
57Fe Mössbauer Spectroscopy
Weighted average values
Bi
Te

## Slide 17
Suggestions for relative phases hosting Fe2+ and Fe3+ ions
Fe2+ in Slag precursor and IP:
Fayalite-type Fe2+2SiO4 (crystalline & amorphous for Bi)
Ca-Fayalite-type (Fe2+2-zCaz)SiO4 and Ca-Ferrosilite-type (Fe2+2-zCaz)Si2O6 (amorphous for Te)
Fe3+ in Slag precursor and IP:
Ferrifayalite-type (Fe2+2-x□yFe3+x)SiO4 (crystalline & amorphous for Bi)
Ca-Ferrifayalite-type (Fe2+2-x-zCaz□ye3+x)SiO4 (amorphous for Te)
Crystal structure of Fayalite
(olivine-type) Fe2+2SiO4
Crystal structure of Ferrosilite (pyroxene-type) Fe2+2Si2O6
Bi & Te samples
Te samples
Fe3+ in glass structure:
The large drop in QS values from the Slags to the IPs reflect a shift in the coordination (O) number most probable from 6 (nn) to 5 or 4  the ferric ion could behave like silicon in the IP binder, i.e. it could act as a network former.

## Slide 18
1 d
3 d
4 w
7 w
Evolution of the 77K 57Fe Mössbauer spectra at different reaction stages
Activating solutions with molar ratios SiO2/Na2O=1.6 and H2O/Na2O=20.
Starting Mixture Components wt% |  |  |  | 
FeO | SiO2 | CaO | Al2O3 | MgO
47 | 34 | 12 | 5 | 2

## Slide 19
Conclusions
Emphatic appearance of Fe3+ contributions in the IP samples resulting by oxidation of the Fe2+ states existing in the Slags after chemical reaction with the activating solutions.
The amorphous part of the slags is the most active component of the starting Slag material, while the crystalline part is more resistive to oxidation.
The addition of Ca seems to favor the formation of the amorphous-glass phase and enhance the presence of Fe3+ states both in the Slags and, more pronounced, in the IPs.
A shift in the Mössbauer parameters of the ferric ions from the slags to the IPs indicates a change in their O-coordination, suggesting that these ions could act as network formers similar to the role of Si.
The oxidation of Fe2+ to Fe3+ in the curing period of the IPs is fast for the initial 1-3 days, then slower up to 4 weeks and persists further up to at least 7 weeks.

## Slide 20
Arne PEYS
Silviana ONISEI
Yiannis PONTIKES
Collaborators KU LEUVEN

## Slide 21
  Mössbauer Spectroscopy & Physics of Materials Laboratory
  Physics department, University of Ioannina
  http://pml.physics.uoi.gr
Ioannina-Greece