## Slide 1
Alkali activation of slags has over the years been studied widely especially with amorphous slags. However, some crystalline slags have also shown potential in sustainable alkali activated binders. Amongst these crystalline slag is ladle slag, currently an under-utilized residue from steelmaking process, with an estimated annual production of three million tons in Europe. In a previous study by the authors, ladle slag has been shown to possess potential as a sole precursor for alkali-activated binders. Here, we investigate the effects of fine grinding on the properties of alkali activated ladle slag (AALS).
References
1. Shi C (2002) Characteristics and cementitious properties of ladle slag fines from steel production. Cem Concr Res 32:459–462. doi: 10.1016/S0008-8846(01)00707-4
2. Adesanya E, Ohenoja K, Kinnunen P, Illikainen M (2016) Alkali Activation of Ladle Slag from Steel-Making Process. J Sustain Metall 1–11. doi: 10.1007/s40831-016-0089-x
Effect Of Fine Grinding On Alkali Activation Of Ladle Slag
Elijah Adesanya1, Katja Ohenoja1, Päivö Kinnunen1 and Mirja Illikainen1
1Faculty of Technology, Fibre and Particle Engineering Unit, University of Oulu, Finland
Figure 1. Particles size distribution for the mechanically activate ladle slag and the unmilled slag (RW). The d50 for the BM0, BM10, BM30, BM60 and BM120 are 33.84, 24.27, 23.55, 20.80, and 14.19µm respectively.
CaO | Al2O3 | SiO2 | MgO | Fe2O3 | Others | LOI
46.3 | 28.3 | 8.6 | 7.4 | 5.0 | 4.4 | -1.3
Setting time analysis (Figure 2) was done to analyze the effect of particle size due milling on the setting of the activated paste. Both setting times reduced as the slag particles becomes finer due to increased dissolution and hydration of slag.
Five samples were analyzed milled at various milling time 0, 10, 30, 60 and 120 min. The mix
composition for each sample had similar water to binder ratio and binder to standard sand
ratio. The varied ladle slag samples were activated using alkaline solutions of Sodium silicate
(R=3.5) and Potassium hydroxide. The samples were all cured at 60 °C and demolded
after a day and thereafter kept in sealed bags till testing except shrinkage test samples that
were thereafter kept at 50±5 relative humidity and 22±2 °C.
Figure 2. Measured setting time of alkali activated ladle slag with varying milling time
BM60 seems to have the highest compressive strength and BM120 with the lowest. It should be noted that the compressive strength can be redefined with optimized parameters; water-to-binder ratio, increase silicate content using supplementary materials such as silica fume and diatomaceous earth [2]. In this analysis, no supplementary silica was added to the mix.
DURABILITY PROPERTIES
Figure 4. Compressive strength of the various mortars after freeze-thaw and without freeze thaw at the same age.
Figure 5. Length change of AALS mortars
MICROSTRUCTURE
SEM backscattered images (Figure 6a) showed the effects of the coarse particles in the unmilled slag in inhibiting crack propagation acting as aggregates. There exist in the RW microstructure fewer cracks and propagation compare to BM120, these observations are related to the drying shrinkage values in Figure 5.
Figure 6. SEM-Backscattered images showing the microstructure of the AALS mortars (a) RW (b) BM120; partially reacted LS = 1, reacted product =2 and sand aggregates =3
CONCLUSIONS
The setting time of AALS is influenced by the particle size of the slag particles
The drying shrinkage tendency of AALS mortars is influenced also by the particle size distribution of the slag
The AALS mortars showed considerable frost resistance after 25 cycles.
Maximum compressive strength was achieved for BM60 with 48 MPa after 64 days.
Figure 3. Compressive strength of the various milled AALS at 64 days
Chart: Slag milling time (min)
| BM0 | BM10 | BM30 | BM60 | BM120
Initial setting time | 50 | 35 | 30 | 20 | 15
Final setting time | 80 | 60 | 35 | 35 | 30
Chart: UCS (MPa)
| BM0 | BM10 | BM30 | BM60 | BM120
64 days | 38.4735 | 40.1605 | 33.9271 | 47.7711 | 29.7467
56 days
Chart: UCS (MPa)
| BM0 | BM10 | BM30 | BM60 | BM120
Aft F_T | 37.5377 | 41.5531 | 35.7164 | 44.8403 | 31.3829
64 days | 38.4735 | 40.1605 | 33.9271 | 47.7711 | 29.7467
56 days
Chart: Age (days)
| 0 | 1 | 3 | 7 | 14 | 21 | 28 | 45 | 56 | 90
BM0 | 0 | 0.71562 | 1.0212 | 1.2206 | 1.2787 | 1.2981 | 1.3087 | 1.3112 | 1.3131 | 1.3187
BM10 | 0 | 0.66562 | 1.1675 | 1.3906 | 1.4575 | 1.4831 | 1.4944 | 1.4962 | 1.4906 | 1.4981
BM30 | 0 | 0.71937 | 1.4669 | 1.5512 | 1.6644 | 1.7 | 1.7206 | 1.7325 | 1.7338 | 1.7413
BM60 | 0 | 0.7875 | 1.2156 | 1.3925 | 1.4656 | 1.4862 | 1.4987 | 1.5012 | 1.5019 | 1.5081
BM120 | 0 | 0.78187 | 1.23 | 1.405 | 1.4862 | 1.5087 | 1.5237 | 1.5269 | 1.5256 | 1.5331
OPC | 0 | 0.65062 | 0.69562 | 0.70312 | 0.72812 | 0.73937 | 0.73688 | 0.74625 | 0.74375 | 0.74625
Effects of milling was evident on the drying shrinkage tendency with BM0 showing lowest length change. BM30 showed highest length change which Is attributed to it compressive strength in Figure 3. Moreover, BM0 shrinks twice as OPC, though with a lower sand-to-binder ratio than OPC.
According to the durability test undertaken on the samples using freeze-thaw test (Figure 4), all mortar samples showed considerable frost resistance with similar or even higher strength after freezing and thawing. The samples were tested through 25-cycles of freeze-thaw with each cycle lasting a minimum of 6hrs modified according to EN 14617-5
- Frost resistance
- Drying shrinkage
COMPRESSIVE STRENGTH
SETTING TIME
EXPERIMENTAL
BACKGROUND
Chart: Particle size [µm]
Table 1. Chemical composition of the slag used in this study