## Slide 1: Glass forming ability of slags in the FeOx-SiO2-CaO system and properties of inorganic polymers made thereof
Experimental
.
Results and Discussion
J. Van De Sandea, A. Peysa, T. Hertela, S. Oniseia, B. Blanplaina,Y. Pontikesa a KU Leuven Department of Materials Engineering, Kasteelpark Arenberg 44, 3001 Leuven, Belgium
Introduction
Iron silicate precursors receive increasing interest for the synthesis of inorganic polymers (IP). The work herein aspires to, in the long run, the valorisation of slags from non-ferrous metallurgy, e.g. copper slags, towards higher added value applications, e.g. in structural concrete elements.
To achieve this, slags in the FeOx-CaO-SiO2 system are investigated. The influence of silica and calcium oxide on the glass forming ability of the slags is assessed. In the next step, inorganic polymers are synthesized and the relation between slag microstructure and strength evolution of the IP is presented.
Conclusion
In the studied range of FeOx-CaO-SiO2 slags, a lower (FeO+CaO)/SiO2 molar ratio seems to reach higher glass contents. The early strength of the resulting inorganic polymers is mainly influenced by the availability of silica; a higher SiO2/Na2O molar ratio in the activating solution, lower (FeO+CaO)/SiO2 molar ratio and higher glass content in the slag lead to higher compressive strength after 2 days of curing. After 28 days, a maximal compressive strength exceeding 50 MPa was observed for slag S5.
Melting of Fe, Fe2O3, CaO, SiO2 in an induction furnace in a reducing atmosphere
Quenching of the slag, 100 °C above the liquidus temperature, calculated by FactSage 7.0 software
Milling to a specific surface area of 4000 ± 200 cm2/g according to Blaine
Characterisation of the chemical and mineralogical composition of the slag
Synthesis of IP mortar by mixing the synthetic precursor slags with standard CEN sand and an alkaline activating solution (H2O/Na2O = 25, SiO2/Na2O = 1.6-2.0)
The stars represent the chemical compositions of the studied synthetic slags in the ternary phase diagram (axis in wt%), the parallelogram represents lines with constant (FeO+CaO)/SiO2 (≈1.2 and 2) or FeO/CaO (≈ 2 and 5) molar ratios.
Slag | Amorphous phase (wt%)
S1 | 67
S2 | 75
S3 | 95
S4 | 91
S5 | 89
H2O/Na2O = 25, SiO2/Na2O = 1.6
H2O/Na2O = 25, SiO2/Na2O = 2.0
FeO
CaO
SiO2
2d compressive strength (MPa)
The amount of amorphous phase seems to be related to the amount of silica in the precursor slag.
Early strength seems to be influenced by to the availability of silica in the slag and activating solution, higher silica content results in a higher strength.
The maximal compressive strength was reached for slag S5. The highest relative increase in strength is observed for slags with a lower FeO/CaO ratio (S1,S3,S5).
28d compressive strength (MPa)