## Slide 1: AUTOGENOUS SHRINKAGE AND STRENGTH DEVELOPMENT OF ALKAL-ACTIAVTED SLAG/FLY ASH MORTAR BLENDS
Siva UPPALAPATI1, Shiju JOSEPH2, Özlem CIZER3
1, 2, 3 Department of Building Materials & Building Technology, KU Leuven, Belgium
Volume instability
Problem definition:
Early-age cracking
High volume instability of AAS, inducing a higher risk to early-age micro-cracking, which endangering the mechanical and durability performance.
Objectives:
To determine the optimum synthesis of slag and fly ash blended system with best shrinkage performance and strength properties.
Study the effect of the activator-to-binder ratio on shrinkage and strength properties of alkali-activated slag/fly ash system.
Interlink the volume instability of alkali activated slag/fly ash blends with reaction kinetics and microstructure development.
Mineralogical Characterization:
Shrinkage deformation:
The low reactivity of the fly ash made its hydration slower than slag and thus autogenous shrinkage related to chemical shrinkage decreases.
In addition to this, with increase in the fly ash content the Ca+2 ions decreases and contributes to form less denser matrix and thus autogenous shrinkage related to self-desiccation decreases with increase in fly ash content.
Reaction Kinetics:
Fly ash contains more inactive minerals and also its active constituents are mainly hollow glass pearls, which are not as active as glass phase of slag.
With increasing the fly ash content, the acceleration peak intensity decreases and slightly shift to the longer times. Such a significant change in the acceleration peak with fly ash addition is attributed to the diluted of Ca2+ ions dissolved from the surface of slag grains.
Intensity of the acceleration peak increases with decrease in dosage of activator and also slight shift towards the lower time due to lower degree of dilution of slag and fly ash in pore solution.
Increasing Fly ash content, decreases the C-A-S-H phase and increases the N-A-S-H phases .
Two main phases are detected:
  C-A-S-H
  N-A-S-H
Materials:
Ground Granulated Blast Furnace Slag:
    Basicity Coefficient = 1 and Hydraulic Modulus = 1.6
Low calcium Fly ash with mean diameter of 20µm.
Activator: Combination of 50% Sodium hydroxide (5M) and 50% Sodium Silicate (alkali modulus of 3.4)
Strength:
Activator-to-binder ratio of 0.7
Varied Activator-to-binder ratio
Notes: <number>