## Slide 1: ON THE FOAMING KINETICS FOR THE SYNTHESIS OF POROUS INORGANIC POLYMERS
Activating solution
Mixing time
Temperature
The mixing time mainly influences the speed and duration of the foaming. It also improves the stability of the foams
The process temperature influences the starting time, duration and speed of foaming at high SiO2/Na2O ratio and low mixing time.
The SiO2/Na2O ratio influences the starting time and duration of foaming but not the speed.
Kinetics of pore formation
Jos DENISSEN1, Lubica KRISKOVA1, Yiannis PONTIKES1
1 KU Leuven, Department of Materials Engineering, 3001 Heverlee, Belgium
jos.denissen@kuleuven.be, lubica.kriskova@kuleuven.be, yiannis.pontikes@kuleuven.be
Goal: Study the foaming kinetics of IP by heat of reaction (isothermal calorimetry) and kinetics of pore formation (visual recording), to investigate the influence of the activating solution, addition time of the foaming agent and temperature.
Heat of reaction
Fayalite slag
S/L = 3.33
Aluminium powder
0.2 wt%
Activating solution
1.0, 1.2 or 1.4 SiO2/Na2O
Isothermal
Calorimetry
Materials
IP synthesis without aluminium powder showed 3 peaks namely initial heat, dissolution and polymerisation. This process finishes between 2 or 40 hours depending mainly on the temperature and lesser on the activating solution.
Mineralogy | Composition | wt%
Fayalite | Fe2SiO4 | 19
Hercynite | FeAl2O4 | 3
Magnetite | Fe3O4 | 1
Zincite | ZnO | <1
Amorphous/unidentified | / | 76
Element | wt%
FeO | 41
SiO2 | 39
Al2O3 | 8
ZnO | 6
MgO | 3
Fayalite slag, a by-product from secondary copper recycling, is used as precursor with a D50 of 2.5 μm.
10, 20 or 40 ˚C
Activating solutions were prepared by mixing Na-silicate, demi-water and NaOH pellets. The SiO2/Na2O molar ratio varied but all solutions contained 75 wt% of water.
Surfactant was added to improve the foam structure and stability.
Metallic aluminium powder with particle size 1-5 μm was used as foaming agent.
2Al + 6H2O + 2NaOH → 2NaAl(OH)4 + 3H2
The addition of aluminium powder generates additional heat, finishing the IP synthesis within 1 hour for any temperature or activating solution. However, the effect of activating solution and temperature were still visible in lesser extent.
Conclusion: The temperature and SiO2/Na2O ratio mainly influenced the height (total volume) and speed of the foaming while the addition time played an important role in the stability of foams. Maximum foaming was obtained at 40 C using an activating solution with a SiO2/Na2O molar ratio of 1.4 and by adding the Al-powder after 5 minutes of mixing.