## Slide 1
Instituto de Ingeniería,
Universidad Nacional Autónoma de México,
Avenida Universidad 3000, Coyoacán,
04510, México D.F.
B. Alcánter, R. Schouwenaars, R.M. Ramírez Zamora
Departamento de Materiales y Manufactura,
Universidad Nacional Autónoma de México,
Avenida Universidad 3000, Coyoacán,
04510, México D.F.
CO2 Capture at High Temperature Using Slag – Derived Lithium Silicates

## Slide 2: Introduction
  General goal of the research group:
  Waste valorisation for environmental applications
  Examples:
    Recovery of heavy metals using activated carbon produced from high-sulphur petroleum coque.
    Production of zeolites from copper mining tailings.
    Production of zeolites and cellular ceramics from water potabilisation sludge
    Catalysis and photocatalysis by means of copper slag
    Removal of As and B from groundwater by means of iron and steel slag

## Slide 3: Introduction
  CO2 capture at point sources:
    Separation of CO2 from flue gas (capture)
    Recovery of CO2 for sequestration and regeneration of reagents.
  Issues
    Energy balance
    Efficiency
    Lifetime of reagents

## Slide 4: Introduction
  Materials for CO2 capture:
Zeolites
CaO
Alkaline ceramics
Organic-inorganic hybrids
Activated carbons
Hydrotalcites
Slag
Li-silicates produced from slag

## Slide 5: Introduction
  Issues in materials selection:
  Alternative materials proposed for silicate-based materials:
Material | Selectivity | High temperatura capture | Kinetics | Regeneration | Stability | Cost
CaO |  |  |  |  |  | 
Li2ZrO3 |  |  |  |  |  | 
Li4SiO4 |  |  |  |  |  | 
Waste or by product | CO2 capture capacity | Reference
Rice husk ash | High / 15 cycles | Wang, 2011.
Fly ash | High / 10 cycles | Olivares-Marín, 2011.

## Slide 6: Introduction
  Goal of the present work:
    Use CaO present in slag for CO2- capture.
    Evaluate slags as source of silicate material for the production of Li-silicates for CO2- capture.
  Materials used
    S1: Blast furnace slag
    S2: Electric induction furnace slag

## Slide 7: Experimental:
  Slag and product characterisation:
    XRF
    XRD
    Surface area by means of adsorption-desorption of N2 (BET-isotherm)
  Silicate synthesis
    Mixing of Li2CO3 with ground slag at a Li2CO3 /SiO2 ratio of 2:1
    Calcination at 850°C for 8h.

## Slide 8: Experimental:
  Analysis of CO2 capture
    Temperature programmed carbonation
    Temperature programmed decarbonation
    TPC: 100 mg of sorbent placed in He-gas stream with 5 % (molar fraction) of CO2.
    Heating at 5°C/min
    TPD: samples saturated with CO2 at temperatures between 500 and 650°C for 1 h.
    Desorption by 30 mL/min He-flow
    Ramp of 10°C/min up to 850°C

## Slide 9: Results:
  Mineral composition of raw slag
 | Mineralogical phases | Semicuantitative (RIR)
S1 | Aluminite: Al2SO4(OH)4∙7H2O Alite: Ca3SiO5 | 79 21
S2 | Larnite: Ca2SiO4 Brownmillerite: Ca2(AlFe)2O5 Quartz: SiO2 | 75 22 3

## Slide 10: Results:
 | Mineralogical phases | Semicuantitative (RIR)
S1 | Lithium silicate: Li4SiO4 Lime: CaO β Eucryptite: LiAlSiO4 a Eucryptite: LiAlSiO4 Alite: Ca3SiO5 | 47 20 18 8 7
S2 | Acmite: FeLiO6SiO2 α Eucryptite: LiAlSiO4 Pseudoeucryptite: Li0.9AlSiO4 γ Eucryptite: LiAlSiO4 Lithium and manganese oxide | 27 23 17 13 8
  Mineral composition after treatment

## Slide 11: Results:
  N2 adsorption and specific surface area
Raw slag
S1: 4.4 m2/g
S2: 1.2 m2/g
Modified slag
S1: 1m2/g
S2: 1 m2/g

## Slide 12: Results:
  TPC-TPDC

## Slide 13: Discussion:
  Both slags show a conversion point of 595°C
  Slag 1 shows higher CO2 capacity
    Production of Li4SiO4 as compared to more complex silicates in slag 2.
    Presence of CaO
  Both slags show some sintering during synthesis.

## Slide 14: Conclusions:
  Li-based sorbents for CO2 capture could successfully be prepared from steel slag.
  The amount of CO2 removed of material compares favourably with other proposed sorbents
  The inversion temperature of the present material is lower than other lithium and calcium based materials reported in literature.

## Slide 15: Acknowledgement
  The authors acknowledge support to their laboratories under DGAPA grant n° IV100616.