## Slide 1
CONVERTING STEEL SLAG INTO SI-CA BASED BUILDING CERAMICS
Dejian Pei, Yu Li, Daqiang Cang.
Introduction
Research results
A pyroxene based Si-Ca ceramic has been researched. The Si-Ca ceramic is mainly composed of pyroxene group minerals with high content of CaO and Fe2O3, which belongs to a new SiO2-CaO-MgO-Al2O3-Fe2O3 system. It breaks through the limitations of low content of CaO and Fe2O3 in traditional SiO2-Al2O3-Na2O (K2O) ceramics and could convert large amounts of slag with high content of CaO and Fe2O3 into high value added ceramics. Reusing steel slag in ceramics can help to improve utilization level of steel slag in quality and quantity.
High content of slag: Containing 25-65wt.% steel slag (Fig. 1 ) with compositions (wt.%): 44-55 SiO2, 13-28 CaO, 10-20Al2O3, 2-15 MgO
Excellent Mechanicals Performance：Flexural strength of 2-3 times that of national standard (35 MPa) , as shown in Fig. 2.
1) Its main crystals are of pyroxenes minerals (augite, enstatite) , with a crystallization process (800 to 1100 ℃) prior to its densification
process (1150 to 1220 ℃).
2) The pyroxenes played an important role of framework during the densification process, with small particles size (2-5 μm) and dense
structure of crystals which was contributed to its good properties.
Environment friendly: Stable solidification and low leaching behaviors of heavy metal (Fig. 3), such as Mn2+, Cr3+, V3+ , et al.
In pyroxene (M2M1T2O6) crystals, M2 site for Na+, Ca2+, Mg2+ , Fe2+, Mn2+ cations; M1 site for Mg2+ , Fe3+, Mn2+ , Fe2+, Ti4+, Cr3+ , Zr4+
cations; mainly T site for Si4+, followed by Al3+ and Fe3+.
Fig. 2 Si-Ca Ceramics prepared from steel slag (30wt.%). (a) Crystals, water sorption and flexural strength of Si-Ca ceramic under increasing firing temperature, the steel slag based ceramic has excellent properties with flexural strength of 107 MPa and water absorption rate of 0.045%. (b) SEM photographs of the ceramic.
Fig. 6 Related patents and test reports
Application and outlook of Si-Ca based ceramics
yuli@ustb.edu.cn, cangdaqiang@metall.ustb.edu.cn, peidejian1990@126.com
University of Science and Technology Beijing, Beijing 100083, China
Fig. 1 : Simulation of the crystal phases with steel slag content by Factsage
Fig. 3 Flow chart for idea site occupancy of cations between the T, M1 and M2 sites of pyroxenes.
Application:
1) Ceramic was produced from 45 wt.% stainless steel slag which contained 5.7 wt.% of Cr2O3. Results of leaching test of Cr, Pb and Cd in
ceramics were respectively 25.17, 0.01 and 0.01 mg/kg, much lower than requirements of national standard of 100, 20 and 5 mg/kg (Fig.4).
2) Ceramics was also prepared from red mud (proportion of 10-30 wt.% in raw materials) with good mechanical properties,
including high bending strength of 127.39 MPa, low water absorption of 0.07% and good Na+ solidification behavior.
3) As a new technology with proprietary intellectual property rights (Fig. 6), it has been applied into preparing ceramics from different solid
waste, such as steel slag, blast furnace slag, red mud, tailing, fly ash, ferroalloys slag and so on. At present, ceramic tiles from steel slag or
tailing have been produced on an industrial line in Guangdong and Guizhou province, in China (Fig. 5).
Outlook:
1) Effects of trace elements and sintering mechanisms in the ceramics prepared from different solid wastes need to be further researched.
2) New properties of the ceramics from metallurgical solid wastes should be revealed, especially for function ceramics.
Fig. 4 Polished ceramic tiles from 45 wt.% stainless steel slag
Fig. 5 Ceramic tiles produced on an industrial line
107MPa
0.045%
Pyroxenes
(augite, enstatite)
5th International Slag Valorisation Symposium 2017 (KU LEUVEN)
Notes: <number>