## Slide 1: NON- TRADITIONAL SLAG VALORIZATION FOR AGRICULTURE
T. Velea1, Ildiko Anger1, F. Stoiciu1, Eugenia Gament 2, M. Mihalache3, L. Ilie3, Lavinia Popescu4, Fl. Zaman4, Luminita Mara1, V. Predica1
IMNR
NATIONAL RESEARCH-DEVELOPMENT INSTITUTE FOR NON-FERROUS AND RARE METALS – I.M.N.R
.

## Slide 2
1. National R&D Institute for Nonferrous and Rare
Metals, 102 Biruintei Blvd, Pantelimon, Romania
2. National R&D Institute for Soil Science,
Agrochemistry and Environment Protection, 61
Marasti Blvd. sector 1, Bucharest, Romania
3. University of Agronomic Sciences and Veterinary
Medicine of Bucharest, 61 Marasti Blvd. sector 1,
Bucharest, Romania
4. Institute for Metallurgical Research, 39 Mehadiei
sector 6, Bucharest, Romaniastreet,
IMNR

## Slide 3
The ladle furnace (LF) is known as a smaller version of electric arc furnace, having all three graphite electrodes.
The ladle furnace is equipped with :
an argon injection system;
with injection lance for desulfurizing agents and/or
supply system for deoxidizing additives or chemical composition adjustments
IMNR
What metallurgical waste is used?

## Slide 4
The most important components of LF slag are: CaO (40-60%), Al2O3, SiO2 and MgO.
Due the high content of free CaO, this slag is very alkaline.
LF slag can be used as follow:
is reintroduced into the steelmaking unit,
as a substitute for clinker or cement,
for acid mine water treatment,
as a fertilizer (fertilaizăr)in the agriculture,
as a possible chemical trap for CO2.
IMNR

## Slide 5
IMNR
The classification of acid soils using pH is the following:
pH< 5.5 - soil is strongly acid;
pH is 5.5 - 5.9 the soil is medium acid;
pH is 6.0 – 6.4 the soil is slightly acid;
pH is 6.5 – 6.9 the soil is very slightly acid and
when pH is 7.0 the soil is neutral.
The soil acidity can have influence upon soil fertility:
decrease the availability of essential elements,
decrease activity of soil microorganisms ,
increase the solubility and negative influence of toxic
elements (Al, Mn, Fe)
increase prevalence of plant diseases,
decrease of plant production, water uses and competitive
ability of different plant species.
What is an acid soil?

## Slide 6
IMNR
The LF slag composition in oxides (wt. %)
The XRD analysis identified the following crystalline phases:
Calcio-olivine (Ca2(SiO4))- 45% ,
Mayenite (Ca12Al14O32(O,F2))-12%,
Periclase (MgO)-12%,
Calcite(CaCO3)-3-5%,
Fluorite(CaF2)-6% and
Calcium Fluoride Silicate(Ca6-0.5xSi2O10-xFx)-20%.
The LF slag composition used in field experiments
LF slag | SiO2 |  | Al2O3 | Fe2O3 | MnO | MgO | TiO2
 | 19.85 | 55.12 | 6.01 | 1.18 | 0.89 | 9.42 | 0.22
 | K2O | Cr2O3 | F | P2O5 | V2O5 | SO3 | Others
 | 0.031 | 0.055 | 4.31 | 0.034 | 0.062 | 1.11 | 1.89
CaO

## Slide 7
IMNR
The optical microscopy analysis shows that the slag is composed from microcrystalline and vitreous phases
Optical microscopy .N+. Reflected light. V- vitreous phase

## Slide 8
IMNR
The field from Moara Domneasca is situated in the East side of Bucharest, Romania. This area is situated in Vlasia Plain and the soil is Chromic luvisol
In the table are presented some physical and chemical characteristics of acid soil from Moara Domneasca area at two depth (0-20cm and 20-40 cm)
Acid soil texture and chemical characteristics
Depth (cm) | Bulk density (g/cm3) | Total Porosity (%) | Degree of settling (%) | pH (H2O) | Corg (%) | Humus (%) | Nt (%) | PAl (mg/kg) | KAl (mg/kg)
0-20 | 1.48 | 42.42 | 15.28 | 5.51 | 1.21 | 2.08 | 0.147 | 74 | 230
20-40 | 1.63 | 37.19 | 26.39 | 5.55 | 1.23 | 2.12 | 0.158 | 87 | 235
Some physical and chemical characteristics of Chromic luvisol

## Slide 9
IMNR
The influence of LF slag on soil chemical properties
Treatment | pH H2O |  | Corg % |  | Nt % |  | P mg/kg |  | K mg/kg | 
Depth (cm) | 0-20 | 20-40 | 0-20 | 20-40 | 0-20 | 20-40 | 0-20 | 20-40 | 0-20 | 20-40
V1 (soil 0 trm.) | 5.51 | 5.55 | 1.21 | 1.23 | 0.147 | 0.158 | 74 | 87 | 230 | 235
V2(1t LF slag/ha) | 5.68 | 5.77 | 1.35 | 1.31 | 0.157 | 0.153 | 106 | 108 | 225 | 270
V3 (2t LF slag/ha) | 5.80 | 5.92 | 1.28 | 1.23 | 0.153 | 0.155 | 97 | 105 | 298 | 287
V4 (3t LF slag/ha) | 5.78 | 5.95 | 1.25 | 1.21 | 0.151 | 0.157 | 85 | 87 | 299 | 326
V5 (5t LF slag/ha) | 6.01 | 6.35 | 1.32 | 1.25 | 0.157 | 0.132 | 78 | 89 | 311 | 317

## Slide 10
Chart: Treatment
| V1 | V2 | V3 | V4 | V5
N tot | 0.147 | 0.157 | 0.153 | 0.151 | 0.157
C org | 1.21 | 1.35 | 1.28 | 1.25 | 1.32
Humus | 2.086 | 2.3274 | 2.2067 | 2.155 | 2.2757
Chart: 
| V1 | V2 | V3 | V4 | V5
pH | 5.51 | 5.68 | 5.8 | 5.78 | 6.01
IMNR
The influence of LF slag on soil
pH at depth 0-20 cm
The influence of LF slag on soil total N, organic C, Humus at depth 0-20 cm

## Slide 11
IMNR
Chart: Treatment
| V1 | V2 | V3 | V4 | V5
P | 74 | 106 | 97 | 85 | 78
K | 230 | 225 | 298 | 299 | 311
The influence of LF slag on soil mobile phosphorous and mobile K at depth 0-20 cm

## Slide 12
IMNR
Wheat on experimental field Moara Domneasca

## Slide 13
IMNR
Chart: Treatment
| V1 | V2 | V3 | V4 | V5
 | 4630 | 4980 | 5280 | 6070 | 6320
The influence of LF slag on wheat production

## Slide 14
IMNR
The heavy metal content of the wheat grains (ppm)
Treatment | Lead | Copper | Zinc
V1 (soil 0 trm.) | 0 | 0 | 36
V2(1t LF slag/ha) | 0 | 0 | 40
V3 (2t LF slag/ha) | 0 | 0 | 34
V4 (3t LF slag/ha) | 0 | 0 | 41
V5 (5t LF slag/ha) | 0 | 0 | 41

## Slide 15
IMNR
Conclusions
The LF slag from the steel refining can be used for acid soil remediation. The presence of LF slag in soil improves the soil chemical characteristics and increases the crop production.
The wheat grain contains zinc, which is very important for human health.

## Slide 16
Thank You for attention
IMNR