## Slide 1: The carbon cost of Slag production in the blast furnace
April 16th, 2015 4th Slag valorization symposium Leuven
Notes: <number>

## Slide 2: Place of the Blast furnace in the material production Worldwide
16/4/2015
4th Slag valorization symposium Leuven
<number>
Energy (BF gas)
BF slag
The Blast furnace produces 94% of all primary steel worldwide
It produces 3 different streams simultaneously
4 most important materials
94% primary steel with Blast Furnaces
1 process 3 product streams

## Slide 3: Why do we want to know the carbon cost of slag production in the Blast Furnace?
There are basically 4 fundamental reasons why we need to determine the CO2 value/ cost of slag
To measure and compare process performance
To determine the best possible production options & technologies
To decide on the desirability for Society to demand better raw materials quality
To determine the life cycle impact of steel
16/4/2015
4th Slag valorization symposium Leuven
<number>

## Slide 4: Q① Measuring and comparing process performance
There are two parameters that make benchmarking in primary steel making difficult: raw materials quality (can be measured by total BF slag production – granulated or not) and scrap
  Both need to be neutralized for meaningful comparison
  Slag burdens in BF vary from 160kg/tHM to more than 600kg/tHM
  The amount of slag and BF gas needs to be neutralized in order to judge the performance of the BF on hot metal level
    BF produces 3 flows each with their own carbon cost: Hot metal; BF gas and BF slag
      Footprint of BF gas quite simple: natural gas equivalent (best available alternative
      Hot metal footprint = total carbon footprint – BF gas – BF slag
  Example: how to tell Kazakh BF (650kg/t slag) manager how much coke is reasonable compared to the EU peers?
16/4/2015
4th Slag valorization symposium Leuven
<number>

## Slide 5: Q② Determining the best production options & technologies
BF route allows to produce ‘Granulated Blast Furnace slag’
  Other technologies (EAF based) can only produce ‘stones’
Hence for equal performance a BF operation should be preferred
How unequal the performance should become before the non-BF route would become more attractive?
Everything depends on the CO2 cost of GBFS production…
A criterion could be the CO2 cost of technologies to convert non-granulatable slag in granulatable (ZEWA project)
In SA consultants propose to use DRI/EAF as bench for primary steel making
16/4/2015
4th Slag valorization symposium Leuven
<number>
Without the CO2 valorization of slag DRI/EAF would receive undue advantage
Notes: Zero waste project EAF pour refondre les scories pour ajuster l’hydraulicité
laitier granulable et hydraulique
recup de métaux
<number>

## Slide 6: Q③ To decide on the desirability for society to improve raw materials quality
Should the production of granulatable slag be discouraged?
  We can benificiate ores & coal more and produce less slag
  Use pellets instead of sinter
16/4/2015
4th Slag valorization symposium Leuven
<number>

## Slide 7: Subdivision of HM and slag production
Blast Furnace
Blast Furnace
Sinter Plant
Pellet plant
Ore Benefic.
Mine
Mine
Tailings
GBFS
GBFS
HM
HM
16/4/2015
4th Slag valorization symposium Leuven
<number>
2 scenarios to compare: Which is the more desirable?
  Minimize slag volume - increase tailings volume - produce more clinker
  Minimize tailing ponds - use more GBFS - produce less clinker
If CO2 cost of slag production ≤ CO2 of eq. Clinker production no reason to decrease (on the contrary)
If CO2 cost of GBFS < Equivalent clinker production: no need to reduce GBFS

## Slide 8: Q④ To determine the life cycle impact of steel
So far most (WSA etc.) LCA systems use ‘system expansion’ i.e. the CO2 cost for clinker is attributed to GBFS (900kg/tGBFS)
  Over time this is not tenable – a given sector should not have to depend on another for determining its footprint
  Cement can/ will improve its performance = exogenous data are unfit for allocation they change all the time
  If GBFS is more efficient than clinker the benefit should be for the customer not the producer
Using the real impact leaves interest for the user as well as for the producer
  Data analysis showed the value to be extremely robust
16/4/2015
4th Slag valorization symposium Leuven
<number>
Low CO2 values for GBFS should lead to an obligation to use GBFS over clinker for the cement user but also to a decrease of production for the steel maker since the steel footprint is too high

## Slide 9: Methodology
Previous attempts to derive the impact of different slag burdens by correlation studies of different BF operations failed
  Too many other operational variables make the direct measurement of the slag impact on carbon emissions impossible
We considered a «differential approach»: adding a marginal quantity of gangue how much will the carbon input of the BF change?
  The mathematical BF model (MMBF) needs to calculate the new equilibrium (more slag = more carbon-in = also more BF gas)
  The emissions of the sinter plant increase because more gangue requires more limestone/ dolomite to adjust slag basicity – only carbon content needs considering
16/4/2015
4th Slag valorization symposium Leuven
<number>

## Slide 10: Data – Calculations - results
16/4/2015
4th Slag valorization symposium Leuven
<number>
Comparison of standard operation with +50kg/tHM slag
Coke input was allowed to vary (PCI variation is similar)
Flame temperature is required to remain the same
Upstream requirements for additional coke production and limestone consumption are added into iron making plant model

## Slide 11: Results
16/4/2015
4th Slag valorization symposium Leuven
<number>
For 5 different BF the real CO2 impact was calculated using a differential reasoning
Result is remarkably robust and independent of the raw material mix used (sinter, pellets, lump ore)
Application of correction seems to effectively account for the impact of slag quantity

## Slide 12: Conclusion
Present analysis shows 550kgCO2/t slag to be a robust value representing the actual cost for producing slag through the BF
This value is indispensable for benchmarking of BF operations on Hot Metal level
It allows for a reasonable comparison of very different steel making routes (DRI/ EAF)
The value is much lower than the benchmark value for producing grey clinker (766kgCO2/t) =>
  No reason to discourage the production of slag on the condition it is granulated and used as clinker substitute avoiding huge tailing ponds
  It seems reasonable to use this value in LCA evaluations
16/4/2015
4th Slag valorization symposium Leuven
<number>

## Slide 13: Thank you
31/07/26
Confidential
<number>
Notes: <number>