## Slide 1
Cold-Pressing Technique - A New Approach to Recycle Stainless Steel Reductive Slag as Coarse Aggregate
C. T. Tsai, Wei-Sheng Chen*, J. E. Chang
Sustainable Environment Research Laboratories &
Department of Resources Engineering
National Cheng Kung University
17 April, 2015
SERL website:
http://serc.ncku.edu.tw

## Slide 2
Introduction-1
Every year there was approximately 160,000 to 200,000 tons of stainless steel reductive slag generated in Taiwan .
Due to the fact that stainless steel reductive slag has the characteristic of poor volume stability (i.e. stainless steel reductive slag is liable to react with H2O and CO2 to result in expansion), the Industrial Development Bureau, Ministry of Economic Affairs announced that stainless steel reductive slag is only recycled or reused in raw cement materials and concrete products in Taiwan.
1

## Slide 3
In Taiwan the natural resources are rather lack, but recycling resources are quite plentiful.
A new approach, the cold-pressing technique which incorporates the principles of the cement chemistry and composite material was developed to recycle these resources as coarse aggregates.
This paper aims to show that using cold-pressing technique to recycle stainless steel reductive slag as coarse aggregate.
Introduction-2
2

## Slide 4
Experimental Materials-1
Cement：Type I Portland Cement produced by Taiwan Cement Company.
Blast-furnace slag (BF slag) provided by CHC Resources Corporation.
Class F fly ash supplied by Taiwan Power Station.
A carboxylate-based type G superplasticizer was purchased from a local factory.
Stainless steel reductive slag was provided from Ming Hsiang Hsin Co., Ltd.
Glass fibers were recycled from printed circuit board (PCB) wastes.
The cementitious materials and superplasticizer conform to the related ASTM standards.
3

## Slide 5
TCLP results of stainless steel reductive slag (mg/L)
TCLP results of stainless steel reductive slag were below the criteria of general enterprise wastes and green building materials in Taiwan
Experimental Materials-2
 | Cr | Ba | Se | Cd | Pb | Cu | As | Hg | Ag | Cr+6
Stainless steel reductive slag | 0.07 | 0.543 | ND | ND | ND | ND | ND | ND | ND | ND
Criteria of general enterprise wastes | 5.0 | 100.0 | 1.0 | 1.0 | 5.0 | 15.0 | 5.0 | 0.2 | 5.0 | 2.5
Criteria of green building material | - | - | - | 0.3 | 0.3 | 0.15 | 0.3 | 0.005 | 0.05 | 1.5
4

## Slide 6
Glass fibers
Cement, Slag,
Fly ash
Cold-pressing
Technique
Stainless steel
reductive slag
The cement-based composites for making the recycling coarse aggregate is regarded as concrete.
Cement, blast-furnace slag, and fly ash are regarded as binders
Stainless steel reductive slag is as a filler (i.e. aggregate)
Glass fiber is as a reinforcement
Mixture Proportion-1
5

## Slide 7
Mixture Proportion-2
A local mixture proportion method in Taiwan, densified mixture design algorithm (DMDA), is adopted to design and prepare the cement-based composites for making the recycling coarse aggregate.
The water-to-cementitious ratio (w/cm) of mixture proportion is 0.2 and a total of 39.4 kg glass fibers (the volume=0.02 m3) was added to the cement-based composites.
Specifically, the mixture proportions with a low cement amount of 100 kg/m3 was designed .
6

## Slide 8
Mixture Proportion-3
Cement | Pozzolanic materials | Stainless steel reductive slag | Glass fiber | SP+Water
100 (5.00)* | 365 (18.22)* | 1499 (74.81)* | 39.4 (1.97)* | 93
Mixtures of cement-based composites (kg/m3)
Pozzolanic materials: BF slag + Fly ash
*: The percentage by weight of solid composition materials.
The cement-based composite contains approximate 75 % (by weight) of stainless steel reductive slag
7

## Slide 9
Method of Granulation
Three various methods were adopted to granulate the cold-pressing recycling coarse aggregate:
1 | Spirally push method | 
2 | Immediately squeeze out method | 
3 | Press ingot method | 
8

## Slide 10
The forming energy of spirally push method is too small to adequately granulate the recycling aggregates, while the cement-based composite with lower moisture.
This way is inappropriate to granulate the recycling aggregates
Spirally push method
9

## Slide 11
Regardless of the stainless steel reductive slag with moisture, the immediately squeeze out method will cause the water of cement-based composite to be drained out during the process of forming recycling aggregates (like consolidation).
This way is inappropriate to granulate the recycling aggregates
Immediately squeeze out method
10

## Slide 12
Press ingot method-1
1. To fill the mixed cement-based composite into the mold.
2. To set up the pestle into the mold.
3. To press and form the recycling aggregates.
4. To take off the recycling aggregates from the mold.
11

## Slide 13
Press ingot method-2
The press ingot method was developed to successfully granulate the cold-pressing recycling coarse aggregates with five various diameters.
D=24 mm
D=18 mm
D=12 mm
D=8 mm
D=5 mm
12

## Slide 14
Optimum Moisture
The purpose of exploring the optimum moisture of stainless steel reductive slag under granulating aggregate is to avoid two issues:
With lower moisture: the recycling coarse aggregate can not be adequately granulated.
With higher moisture: the redundant water may drain out during the process of forming recycling aggregates (like consolidation in geotechnical engineering) and cause the excessively high water-to-cement ratio (w/c) or water-to-cementitious materials (w/cm) around the surface of the recycling aggregate.
The optimum moisture for granulating recycling coarse aggregate of stainless steel reductive slag was 14.0 % while the stress of granulation by using press ingot method is 35.0 to 42.0 MPa.
13

## Slide 15
Observation of Volume Stability-1
The surface of recycling aggregate had slight splits due to expansive reaction of f-CaO within stainless steel reductive slag before the age of 7 days.
So far, recycling coarse aggregates with stainless steel reductive slag has not generate further expansion, splits, or even rupture for more than four years.
There was a significantly white particle existing in the expansions, splits, or spalls of recycling coarse aggregate and the diameter of the white particle is more than 1.0 mm.
14

## Slide 16
Observation of Volume Stability-2
While the diameter of stainless steel reductive slag was controlled to less than 0.297 mm (below No. 50 sieve), the expansions, splits, or spalls of recycling coarse aggregate were completely improved.
15

## Slide 17
Single particle compressive strength
The single particle compressive strength increases with the increase of curing age due to the fact that the contribution of hydration of cement and pozzlanic reaction.
16

## Slide 18
Basic characteristics of recycling coarse aggregate
Specific gravity (OD) |  | Specific gravity (SSD) |  | Absorption (%) |  | Unit weight (kg/m3) |  | Voids (%) |  | Particle cylindrical crushing strength (MPa) | 
1.70-1.73 |  | 1.98-2.02 |  | 14.09-14.47 |  | 1201-1235 |  | 32.9-33.3 |  | 39.89-41.67 | 
 | Clay lumps and friable particles （%） |  | Material finer than 75-μm （%） |  | Coal and Lignite （%） |  | Abrasion （%） |  | Soundness （%） |  | Cl- （%）
 | ND |  | 0.09 |  | ND |  | 29.8 |  | 5.23 |  | 5.6×10-4
ASTM C33 | 2.0-10.0 |  | 1.0 |  | 0.5-1.0 |  | 50.0 |  | 12.0 |  | 0.012
Basic characteristics of recycling coarse aggregate conform to ASTM C33.
17

## Slide 19
Conclusion-1
The DMDA is appropriate to design the cement-based composite with stainless steel reductive slag and glass fibers recycled from PCB wastes for producing the cold-pressing recycling coarse aggregates.
The optimum moisture for granulating recycling coarse aggregate of stainless steel reductive slag was 14.0 % while the stress of granulation by using press ingot method is 35.0 to 42.0 MPa.
18

## Slide 20
Conclusion-2
The recycling coarse aggregates produced by using the cold-pressing technique can reduce about 65 % CO2 footprint when compared to using the sintering technique. And the prime cost of cold-pressing recycling aggregate is 5 to 6 times lower than sintering recycling aggregate.
Therefore the cold-pressing technique is a new and practicable approach to recycling stainless steel reductive slag in future.
19

## Slide 21
Thank For Your Attention