## Slide 1
Producing bricks from stainless steel slags: an environmental evaluation based on Life Cycle Analysis
Andrea DI MARIA; Muhammad SALMAN; Karel VAN ACKER. Maarten DUBOIS
Notes: versie 15/01/2014

## Slide 2
Industrial symbiosis
“In nature, there is no such thing as waste…”
IS is a system innovation aiming to share services, resources and by-products among different industries
Industrial symbiosis in the steel sector
Flue gas and steam to nearby industries
Blast Furnace Slag (BFS) in cement production
…There is still a need for research focused on the valorisation of other residues whose potential is not explored at present:
Industrial symbiosis in the steel sector

## Slide 3
  Stainless steel production by-products
  300 Kg of SSS each tonne of steel produced
  8,7 Mtons of SSS produced in 2011
  Several types of slags generated:
    Electric Arc Furnace (EAF)→melting
    Argon Oxygen Decarburation (AOD) →refining
    Continuous Casting (CtCs) →final stage
Industrial
Product
Industrial
By-product
SS Slag
Stainless Steel
The Stainless Steel Slag (SSS)

## Slide 4
Average chemical composition (AOD slag)
Oxides | CaO | SiO2 | MgO | Al2O3 | TiO2 | Cr2O3 | Fe2O3 | Others
wt% | 57 | 29 | 8 | 2 | 1 | 0,6 | 0,6 | 1,8
Strengths and Opportunities
  SSS contains high quality oxides (CaO,SiO2,Al2O3,MgO)
Threats
  Hazardous compounds (Cr, Pb, Ni, Cd ). Borates or cement addition to stabilised the slag
  Fine particles (mm÷μm)
The Stainless Steel Slag (SSS)

## Slide 5
Possible end-of-life destinations of SSS
  Reclamation of waste steel and iron
  Utilization in road construction (aggregates substitution)
  Production of binder for construction material
New development
The Stainless Steel Slag (SSS)
  Landfilling
Stabilization required!

## Slide 6
The Alternative…
Use of SSS as binder for the production of new construction material
The project SMARTPRO²
Production of new construction material in the form of masonry blocks (SSS blocks) from fine AOD slag:
AOD slag composition: closer to binder than to aggregates
Fine particles: Avoid energy intensive milling
4 different blocks, 2 different processes applied:
Alkali activation
Carbonation
The StainlessSteelSlag (SSS) blocks: General

## Slide 7
Alkali activators
(sodium silicates)
Alkali Activation
  Chemical process that transforms glassy structures into compact and well cemented composites, through chemical activation with alkali compounds
  Viable alternative to Ordinary Portland Cement (OPC)
  Potential to reach high mechanical strength
AOD Stainless
Steel
Slag
Solid
block
The StainlessSteelSlag (SSS) blocks: General
7
Aggregates

## Slide 8
+ Alkali activators
+ Aggregates
+ Alkali activators
+ Aggregates
+ Aluminum
(Alkali activation)
AOD Stainless
Steel
Slag
Alkali Activation: The block production process
Solid
AA block
Aerated
AA block
The StainlessSteelSlag (SSS) blocks: General
8

## Slide 9
Carbonation
  Method of carbon capture that accelerates the natural weathering of calcium, magnesium and silicon oxides, allowing them to react with CO2 to form stable carbonate
Oxides
Carbonates (Solid)
  Developed mainly as a technique to capture CO2 (carbon sink)
  Arising interest for industrial by-products
  Industrial ecology concept
  CO2 uptaking + Waste reduction + High value end product
The StainlessSteelSlag (SSS) blocks: General
9
Solid
block

## Slide 10
Reactor
2,5 hours
8 bars
80 °C
Chamber
7 days
1,01 bars
22 °C
(Carbonation)
Solid
CR block
AOD Stainless
Steel
Slag
Carbonation: The block production process
Energy required!
Solid
CC block
The StainlessSteelSlag (SSS) blocks: General
10

## Slide 11
reactor
chamber
Carbonation
Alkali activation
Solid
CR block
Solid
AA block
Aerated
AA block
AOD Stainless
Steel
Slag
Production Phase
Disposal Phase
Research question
Is the valorization of AOD slag as SSS blocks beneficial in terms of impacts for the environment?
Solid
CC block
The StainlessSteelSlag (SSS) blocks: General
11

## Slide 12
Comparison of three different scenarios:
SSS valorization through the production of SSS blocks
NO valorization (boric oxide stabilization and use as aggregates)
Production of the alternative to SSS block already available in the market
Solid
CR block
Solid
AA block
Solid
CC block
Concrete
Paver
block
Autoclaved
concrete
block
Aerated
AA block
The StainlessSteelSlag (SSS) blocks: LCA
12

## Slide 13
Goal
and
Scope
Inventory
Analysis
Impact
Assessment
The LCA framework
Functional unit
System boundaries
Data collection
Data treatment
Calculation method
Results analysis
The StainlessSteelSlag (SSS) blocks: LCA
13

## Slide 14
Goal
and
Scope
Inventory
Analysis
Impact
Assessment
The LCA framework
Functional unit
System boundaries
The StainlessSteelSlag (SSS) blocks: LCA
14

## Slide 15
Scope
To assess the environmental impacts of new developed construction blocks made through the activation of AOD slag, in order to evaluate the environmental benefits arising from the application of industrial ecology concepts to steel sector.
Functional unit
Impacts related to the life cycle of 1m² blocks
Volume of 1 block: 25x5x10 cm (1000cm³)
In 1 m² → 50 blocks
Different weight for 1 m² (different density)
  Comparison 1
  AA solid= 111 kg/m² ; CC solid= 107 kg/m²; CR solid= 107 kg/m²; Paver= 134 kg/m²
  Comparison 2
  AA aerated= 58 kg/m² ; Autoclaved= 25 kg/m²
The StainlessSteelSlag (SSS) blocks: LCA
15

## Slide 16
Alkali activation
Carbonation
System Analysis
The StainlessSteelSlag (SSS) blocks: LCA
16

## Slide 17
Traditional blocks
The StainlessSteelSlag (SSS) blocks: LCA
17

## Slide 18
Goal
and
Scope
Inventory
Analysis
Impact
Assessment
The LCA framework
Data collection
Data treatment
The StainlessSteelSlag (SSS) blocks: LCA
The StainlessSteelSlag (SSS) blocks: LCA
18

## Slide 19
Inventory table
 | Scenario 1 AA Solid blocks (Alkali Activated) 1 block= 2,2 kg |  | Scenario 2 AA Aerated blocks (Alkali Activated) 1 block= 1,1 kg | Scenario 3 C-R solid blocks (carbonated react) 1 block= 2,1 kg | Scenario 4 C-C solid blocks (carbonated chamb) 1 block = 2,1 kg | Scenario A Concrete paver blocks 1 block = 2,1 kg | Scenario B Autoclaved concrete blocks 1 block = 0,6 kg
Density (g/cm³) | 2,22 |  | 1,16 | 2,14 | 2,14 | 2,6 | 0,6
Weight of FU (kg) | 111 |  | 58 | 107 | 107 | 134 | 25
INPUT |  |  |  |  |  |  | 
Quantity of slag (kg) |  | 39 | 18 | 101 | 101 | / | /
NaOH (kg) |  | 1,4 | 2,8 | / | / | / | /
Na silicate (kg) |  | 3 | 3,4 | / | / | / | /
River Sand (kg) |  | 60 | 28 | / | / | 108 | 11
Aluminum powder (kg) |  | / | 0,009 | / | / | / | 0,01
Energy (kWh) |  | 0,04 | 0,04 | 62 | / | / | 10
Boric oxide to stabilize |  | 0,7 | 0,3 | 2,1 | 2,1 | / | /
Water (kg) |  | / | / | 19 | 19 | 7 | 10
CO2_input (kg) |  | / | / | 17 | 17 | / | /
Portland Cement (kg) |  | / | / | / | / | 20 | 4
Limestone (kg) |  | / | / | / | / | / | 3
The StainlessSteelSlag (SSS) blocks: LCA
19

## Slide 20
Goal
and
Scope
Inventory
Analysis
Impact
Assessment
The LCA framework
Calculation method
Results analysis
The StainlessSteelSlag (SSS) blocks: LCA
20

## Slide 21
Raw Materials
Land use
CO2
VOC
P
SO2
NOx
CFC
PAH
DDT
Ozone depletion
Human toxicity
Radiation
Ozoneformation
Particules form.
Climate change
Terr. ecotox
Terr. acidif.
Agr. land occ.
Urban. land occ.
Nat. land transf
Marine ecotox.
Marine eutr.
Freshwater eutr.
Freshw. Ecotox.
Fossil fuel cons
Mineral cons.
Water cons.
Damage
Damage
Damage
Human Health
(Daly)
Ecosystems
(Species yr.)
Resources
(Cost)
Calculation methodology
Single
Score
Substances
Midpoints
Endpoints
Uncertainty
ReCiPe
The StainlessSteelSlag (SSS) blocks: LCA
21
Impact category | Total | Unit
Climate change | 4,041874 | kg CO2 eq
Ozone depletion | 2,96E-07 | kg CFC-11 eq
Terrestrial acidification | 0,017053 | kg SO2 eq
Freshwater eutrophication | 0,003442 | kg P eq
Marine eutrophication | 0,001289 | kg N eq
Human toxicity | 3,274149 | kg 1,4-DB eq
Photochemical oxidant formation | 0,010805 | kg NMVOC
Particulate matter formation | 0,005966 | kg PM10 eq
Terrestrial ecotoxicity | 0,000379 | kg 1,4-DB eq
Freshwater ecotoxicity | 0,019231 | kg 1,4-DB eq
Marine ecotoxicity | 0,022642 | kg 1,4-DB eq
Ionising radiation | 2,547385 | kBq U235 eq
Agricultural land occupation | 0,122318 | m2a
Urban land occupation | 0,052585 | m2a
Natural land transformation | 0,00107 | m2
Water depletion | 26,3019 | m3
Metal depletion | 0,171878 | kg Fe eq
Fossil depletion | 1,149028 | kg oil eq

## Slide 22
The StainlessSteelSlag (SSS) blocks: LCIA
The StainlessSteelSlag (SSS) blocks: LCA Results (1)
Comparison 1: Solid AA/CC/CR vs Concrete paver
Environmental points
22

## Slide 23
Environmental points
23
The StainlessSteelSlag (SSS) blocks: LCA Results (1)
Comparison 2: Aerated AA vs Aerated Concrete

## Slide 24
Positive:
Saving energy
Alkali activated and carbonated (in chamber) SSS blocks lower the energy consumption (electricity or fossil fuels), which is the highest impact for conventional concrete blocks (during production of cement and binders).
Negative:
Alkali production
CO2 stream required
Energy consumption in the reactor
In terms of industrial symbiosis
SSS valorization scenarios have higher impact that current no valorization scenario
Looking at a long term, the substitution of traditional concrete with new material from SSS reduces the total environmental impact
Industrial symbiosis presents advantages, but also limitations ( the case of carbonation in reactor)
The StainlessSteelSlag (SSS) blocks: Conclusions
24

## Slide 25
The StainlessSteelSlag (SSS) blocks: Conclusions
25
Multidisciplinary paper
Construction materials from stainless steel slags: Technical aspects, environmental benefits and economic opportunities; Journal of industrial ecology; 2015
Muhammad Salman, Maarten Dubois, Andrea Di Maria, Karel Van Acker, Koen van Balen
Technical aspect
Is it possible to make bricks from slags which fulfil the current normative requirements in terms of shear stress and bearing capacity?
Environmental Aspect
Looking at the whole life cycle, what are the environmental benefits of using these new bricks compared to traditional bricks?
Economic aspect
What is the economic potential for such technologies and their strong and weak points in a view of a possible market introduction?
Innovation
- Multidisciplinary approach; - Industrial ecology concept application; -

## Slide 26
Thank you
for
your attention!
andrea.dimaria@kuleuven.be