## Slide 1: Influence of chemistry of vitrified residues on the properties of blended inorganic polymers with calcined kaolinitic clay
E. François1,2, J. Elsen1, Y. Pontikes2 & L. Machiels2
1KU Leuven, Department of Earth and Environmental Sciences, 3001, Leuven, Belgium
2KU Leuven, Department of Materials Engineering, 3001, Leuven, Belgium

## Slide 2: GOAL
Replace GGBFS in a GGBFS-metakaolin based inorganic polymer (IP) by alternative glassy precursors:
  Limited availability and high price of GGBFS
  Designing glass chemistry to have optimal properties
Three different glass chemistries:
 | GGBFS | GGBFS-glass | Mg-glass | K-glass
SiO2 | 36.0 | 34.0 | 27.1 | 28.2
Al2O3 | 14.5 | 10.4 | 13.4 | 8.9
Fe2O3 | 0.4 | 14.2 | 14.1 | 13.7
CaO | 39.9 | 32.3 | 31.7 | 30.5
MgO | 6.9 | 1.7 | 8.1 | 2.3
K2O | 0.7 | 0.8 | 0.6 | 8.5
Na2O | 0.2 | 2.4 | 3.6 | 4.8
Others | 1.6 | 4.4 | 1.3 | 3.2

## Slide 3: Reactivity
Based on:
  Particle size distribution
  Specific surface area
  Amorphous content
  Chemical composition
Similar for the glasses
GGBFS-glass | Mg-glass | K-glass
0.84 | 1.09 | 1.24

## Slide 4: Results and conclusion

## Slide 5: First hours
 | Initial setting time (hours)
GGBFS | 1.2
GGBFS-glass | 2.6
Mg-glass | 1.2
K-glass | 0.8
Setting time measured with vicat testing apparatus
Heat flow over time obtained with calorimetry
GGBFS-glass | Mg-glass | K-glass
0.84 | 1.09 | 1.24

## Slide 6: After several days of curing
BSE image of a representative inorganic polymer sample
Flexural strengths at 28 days
Compressive strengths at 33 days

## Slide 7: Conclusion
During first hours: chemical composition has strong influence on IP properties
Glass with highest network-modifying to network-forming cations ratio reacts the fastest
After several days similar microstructures are observed and equal flexural and compressive strengths are obtained
Glass chemistry can be controlled to modify the setting time (0.8 to 2.6 hours) without affecting the final properties (strength, microstructure)

## Slide 8: Thank you for your attention