## Slide 1: Dimitra ZAHARAKI, Antigoni VLACHOU, Kostas KOMNITSAS School of Mineral Resources Engineering, Technical University of Crete, 73100, Chania, Greece
CO-UTILIZATION OF SLAGS WITH CONSTRUCTION WASTES OR RED MUD FOR GEOPOLYMER PRODUCTION

## Slide 2: Objective
Contents
Geopolymerization
Materials and experimental methodology
Compressive strength of geopolymers
XRD and FTIR analyses
Conclusions
Investigation of the co-geopolymerization potential of ferronickel slags with construction/demolition wastes or red mud

## Slide 3: Geopolymer or inorganic polymer
Geopolymers are inorganic materials formed by the alkali activation of aluminosilicates at relatively low temperatures
Partially or fully amorphous polymeric structures consisting of Si-O-Al bonds
The tetrahedral AlO4 and SiO4 units are built in three dimensional structures

## Slide 4: Geopolymer or inorganic polymer
The structure and mechanical properties of geopolymers are affected by several parameters such as chemical composition and particle size of the raw materials
Various wastes such as fly ash and slag have been extensively investigated as potential raw materials for the synthesis of geopolymers
Geopolymerisation of other wastes and especially construction and demolition wastes (CDW) still remains a great challenge
Raw materials
[aluminosilicate materials or industrial by-products]
Activating solution
[ΚΟΗ or ΝaOH and Na2SiO3]

## Slide 5: Materials
Electric arc furnace slag from the “LARCO S.A” ferronickel plant, Greece
CDW (tiles, bricks and concrete)
Red mud from “Aluminium of Greece”

## Slide 6: Materials
All materials were dried and pulverized using a FRITSCH-BICO pulveriser (slag: <120 μm and d50 12 μm, tiles: <140 μm and d50 14 μm, bricks: <140 μm and d50 6.6 μm, concrete: <190 μm and d50 10 μm, red mud: <76 μm and d50 4 μm)
Material | Fe2O3 | SiO2 | Al2O3 | CaO | Na2O | K2O | MgO | TiO2 | LOI | SUM
Slag (S) | 43.83 | 36.74 | 9.32 | 3.73 | - | - | 2.76 | - | - | 96.4*
Concrete (C) | 0.75 | 5.81 | 1.49 | 65.42 | 0.57 | 1.26 | 4.21 | 0.03 | 21.59 | 101.1
Bricks (B) | 6.00 | 57.79 | 14.95 | 8.79 | 1.03 | 2.80 | 4.75 | 0.85 | 1.89 | 98.9
Tiles (T) | 5.39 | 70.54 | 9.80 | 8.78 | - | 1.37 | 4.46 | 0.77 | - | 101.1
Red mud (R) | 41.65 | 9.28 | 15.83 | 10.53 | 2.26 | 0.21 | - | 4.73 | 16.77 | 101.3
Table 1: Chemical composition (%) of raw materials
LOI: Loss on ignition after heating the material at 1050 oC for 4 h, *Cr2O3: 2.82 %

## Slide 7: Experimental methodology
The activating solution consists of NaOH or KOH anhydrous pellets, distilled water and sodium silicate solution
Raw materials were then mixed with the activating solution (8-10 M NaOH or KOH)
The specimens produced (5 cm edge) were heated at 80 °C in a laboratory oven for 7 days and then subjected to compressive strength testing using an MTS 1600 load frame
X-ray diffraction (XRD) of the final products using a Bruker D8 Advance diffractometer
Fourier transform infrared spectroscopy (FTIR) on KBr pellets using a Perkin–Elmer Spectrum 1000 spectrometer

## Slide 8
Geopolymers from concrete, bricks and tiles (left to right)
5 cm
5 cm
5 cm
Slag-red mud geopolymer
Slag-CDW geopolymer

## Slide 9: Results and discussion

## Slide 10: Figure 1: Compressive strength of geopolymers prepared by mixing slag with (a) CDW (eg. 50-20-20-10: % w/w 50 S-20 T-20 B-10 C) and (b) red mud (eg. 90-10: % w/w 90 S-10 R)
Slag-CDW geopolymers prepared with 10 M NaOH acquired higher compressive strength
The percentage of each CDW component in the initial mixture affects the compressive strength at 10 M NaOH
The compressive strength decreases gradually with increasing red mud %

## Slide 11: Table 2: Molar ratios of oxides
 | S | T | B | C | R | Geopo-lymer 50-10-10-30 | Geopo-lymer 25-30-30-15 | Geopo-lymer 50S-50R
SiO2/Al2O3 | 7.33 | 12.67 | 6.84 | 9.86 | 1.33 | 8.26 | 8.86 | 3.53
H2O/(Na2O+K2O) | 8.30 | 9.03 | 8.32 | 6.62 | 8.11 | 6.96 | 6.10 | 6.66
SiO2/(Al2O3+CaO) | 4.03 | 4.81 | 3.30 | 0.12 | 0.60 | 1.18 | 2.21 | 1.70
Strength, MPa | 76.1 | 57.8 | 39.4 | 7.8 | 2.5 | 59.2 | 78.4 | 38
S: slag, T: tiles, B: brick, C: concrete, R: red mud, eg. 50-10-10-30: % w/w 50 S-10 T-10 B-30 C

## Slide 12: Figure 2: XRD patterns of geopolymers synthesized from slag, CDW and red mud (T: tiles, C: concrete, B: bricks, S: slag, R: red mud, G1:25-30-30-15% w/w S-T-B-C, G2: 50-50% w/w S-R)

## Slide 13: Figure 3: FTIR spectra of selected geopolymers (T: tiles, C: concrete, B: bricks, S: slag, G1:25-30-30-15% w/w S-T-B-C)

## Slide 14: Conclusion
Slag can be successfully co-utilized with various by-products/wastes such as CDW and red mud
Production of geopolymers with compressive strength between 37 and 80 MPa using 10 M NaOH or KOH as alkali activator
The presence of the major fingerprints of the aluminosilicate geopolymeric matrix was revealed by XRD and FTIR analysis

## Slide 15: Thank you
Technical University of Crete
School of Mineral Resources Engineering Research unit “Management of Mining/Metallurgical Wastes and Rehabilitation of Contaminated Soils” http://www.mred.tuc.gr/3020.html
Acknowledgements
The present study has been co-funded by the European Commission (European Regional Development Fund) and by national funds through the Operational Programme “Competitiveness and Entrepreneurship” (OPCE ΙΙ 2007 - 2013), National Strategic Reference Framework – Research funded project: “Recycling of quarry dust and construction and demolition wastes for the production of novel ecological building elements”, DURECOBEL 11SYN_8_584, in the framework of the Action COOPERATION 2011– Partnerships of Production and Research Institutions in Focused Research and Technology Sectors.
Project website: http://www.durecobel.gr/