## Slide 1: Influence of solid phases on BOF slag viscosity
<number>
<number>
Zhuangzhuang Liu, Bart Blanpain, Muxing Guo
Department of Materials Engineering
KU Leuven, Belgium
17/04/2015

## Slide 2
[1]M. Kühn et al. "Treatment of liquid steel slags". In 2nd European slag conference, 2000, Düsseldorf, Germany,. pp. 123-135 (2000).
<number>
Introduction – stabilization principles
BOF slag hot stage engineering
How does the solid phase influence BOF slag viscosity?
The ejection is blocked due to high viscosity of slag
Notes: By co-injecting oxygen, the slag is stirred and FeO in the slag is oxidised to Fe2O3, generating the required heat to dissolve the SiO2. Viscosity is a key factor to keep the production running smoothly.
For this project, too high viscosity can lead to serious problems:
Block the stabilization operation:
The standard hot stage stabilisation process can only be applied for 10% of its BOF slag due to the high slag viscosity
Lower iron recovery yield:
Slag viscosity significantly affects the size and distribution of entrained metallic iron particles in the slag and the sedimentation of metallic Fe particles (or droplets) to the slag pot bottom, also the agglomeration of small iron droplets in the slag during hot stage.
Final slag product is stockpiled
The final slag product is the so called LD gravel which is currently stockpiled.
The dissolution of additives.
Slag viscosity affects the dissolution speed of the compositional modifiers and fluidizers.
For other metallurgical processes, it is a crucial parameter for metallurgical reaction kinetics:
The ability to tap the slag from the reactor
The efficiency of separation of slag from the metal phases
The extent of slag foaming
The performance of continuous-casting fluxes
The kinetics of metal smelting and refining reactions
......

## Slide 3
<number>
<number>
Compositions of BOF slag
Materials
Atmosphere: Ar, 0.4~0.8Nm3/h;
Temperature: 1400~1650℃;
Sampler: stainless steel rod (d=10mm)
 | CaO | SiO2 | T.Fe | MnO | Al2O3 | MgO | Cr2O3 | V2O5 | TiO2 | S
wt.% | 48.48 | 14.21 | 17.73 | 4.33 | 2.83 | 0.975 | 0.826 | 1.22 | 1.02 | 0.101
Experimental
Conditions
Experimental set-up
Mo crucible

## Slide 4
<number>
Results and discussion
1650℃
1600℃
1500℃
1400℃
More and larger size of solids are present in slag quenched at lower temperature
Size and distribution of precipitates in slag sample quenched at different temperature
SEM-BSE analysis of sample

## Slide 5
<number>
Volume fraction of solid precipitates
Results and discussion
Calculation via FactSage
Quenching + Image processing
Difference between two methods are
within experimental deviation

## Slide 6
<number>
Results and discussion
Volume fraction of solids
Viscosity increases dramatically when volume fraction of solids >10%
Comparison between calculated viscosity with Urbain model and Einstein-Roscoe model

## Slide 7
<number>
Solid precipitates influence slag viscosity dramatically when the solid volume faction is larger than 10%
The solid volume faction is larger than 10% at temperature lower than 1500℃ for the BOF slag.
Conclusions

## Slide 8
Thank you for your attention!