## Slide 1
Solidification of metallurgical slags for higher added value applications
- Separation of FeO and P2O5 from steelmaking slags by solid phase precipitation -
Takahiro MIKI, Tohoku University (Japan)

## Slide 2
Annual Worldwide Metal Production
Fe : 1606.9 million tonnes
Al : 47.3 million tonnes
Cu: 17.9 million tonnes
Zn: 13.5 million tonnes
Pb: 5.4 million tonnes
Minerals Commodity Summaries (2014)
Production amount of Fe is very large

## Slide 3
Chart: 
| China | Japan | United States | India | Russia | South Korea | Germany | Turkey | Brazil | Ukraine | Other Countries
 | 779 | 111 | 87 | 81 | 69 | 66 | 43 | 35 | 34 | 33 | 269
Production of steel
Chart: 
| Asia | European Union | C.I.S | Other Europe | North America | South America | Middle East | Africa | Oceania
 | 1136 | 169 | 106 | 38 | 121 | 45 | 28 | 15 | 5
Worldsteel (2014)
Countries
Region

## Slide 4
Slag and Steel production in Japan
Blast furnace(BF) slag : 24.6 million tonnes/yr
Steelmaking slag : 14.4 million tonnes/yr
Hot metal(HM): 83.8 million tonnes/yr
Steel : 111.5 million tonnes/yr
Nippon Slag Association(FY 2013)
Blast furnace slag : 294kg-slag/t-HM
Steelmaking slag : 129kg-slag/t-steel
・Annual production
・Slag production per t-HM and t-steel

## Slide 5
CaO
Iron ore
Coke
BF slag
De-S Slag
De-P Slag
De-Si Slag
De-P Slag
De-Si,P Slag
De-C Slag
Product
BOF steel production process
Beside this process, there is EAF steel production process using steel scraps as an iron source.

## Slide 6
Blast furnace(BF) slag usage in Japan
Cement – 72%
Road Building – 15%
Concrete Aggregate – 9%
Others – 2%
Typical Composition of BF slag
42mass%CaO-34mass%SiO2-13mass%Al2O3-7mass%MgO
mass%FeO<0.5, mass%P2O5<0.1
BF slag has established a stable position for cement industry

## Slide 7
■ Civil
■ Road
■ Recycling
■ Soil improvement
■ Cement
■ Land fill
■ Fertilizer
■ Other
Uses of steelmaking slag in Japan.
Chart: 
 | 4344 | 2873 | 1647 | 1226 | 550 | 276 | 84 | 859
14.4 million ton/yr
Steelmaking slag
The FeO and P2O5 in the slag is wasted in such applications.
These materials need to be put to better use.
Typical Composition of Steelmaking slag
46mass%CaO-17.4mass%FeO-11mass%SiO2-6mass%MgO
-1.7mass%P2O5

## Slide 8
Blast Furnace
Slag
De-P
De-P slag
Slag
CaO
Iron ore
Coal
Molten iron
BF slag
Raw materials
Steel products
Slag
Steelmaking slag
Dephosphorization
Converter
Flow chart of steelmaking process
Si
P
S
(Si,P,S,C)
Phosphorus in steelmaking slag

## Slide 9
Matsubae et al. Chemosphere (2011)
Phosphorus flow in Japan

## Slide 10
 | CaO | SiO2 | T-Fe | MgO | Al2O3 | S | P2O5 | MnO
BOF | 45.8 | 11 | 17.4 | 6.5 | 1.9 | 0.06 | 1.7 | 5.3
EAF | 22.8 | 12.1 | 29.5 | 4.8 | 6.8 | 0.2 | 0.3 | 7.9
Compositions of Basic Oxygen Furnace(BOF) and Electric Arc Furnace(EAF) slag.
 | CaO | SiO2 | T-Fe | MgO | Al2O3 | S | P2O5 | MnO
BOF | 45.8 | 11 | 17.4 | 6.5 | 1.9 | 0.06 | 1.7 | 5.3
EAF | 22.8 | 12.1 | 29.5 | 4.8 | 6.8 | 0.2 | 0.3 | 7.9
2CaO･SiO2
Nippon Slag Association.
Background
CaO – FeO – SiO2 ternary system.
Main components： CaO-FeO-SiO2
Steelmaking slag
BOF(Basic Oxygen Furnace) slag
EAF(Electric Arc Furnace) slag

## Slide 11
 | CaO | SiO2 | T-Fe | MgO | Al2O3 | S | P2O5 | MnO
BOF | 45.8 | 11 | 17.4 | 6.5 | 1.9 | 0.06 | 1.7 | 5.3
EAF | 22.8 | 12.1 | 29.5 | 4.8 | 6.8 | 0.2 | 0.3 | 7.9
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
FeO
FeO
FeO
FeO
FeO
FeO
Background
Compositions of Basic Oxygen Furnace(BOF) and Electric Arc Furnace(EAF) slag.
Nippon Slag Association.
Main components： CaO-FeO-SiO2
Steelmaking slag
BOF(Basic Oxygen Furnace) slag
EAF(Electric Arc Furnace) slag
FeO
Solidification model
FeO
FeO
FeO
Molten slag(including FeO and P2O5)
Liquid slag(FeO rich)
2CaO・SiO2 (P2O5 rich)
P2O5 tends to distribute in 2CaO･SiO2

## Slide 12
 | CaO | SiO2 | T-Fe | MgO | Al2O3 | S | P2O5 | MnO
BOF | 45.8 | 11 | 17.4 | 6.5 | 1.9 | 0.06 | 1.7 | 5.3
EAF | 22.8 | 12.1 | 29.5 | 4.8 | 6.8 | 0.2 | 0.3 | 7.9
FeO
FeO
FeO
FeO
Background
Compositions of Basic Oxygen Furnace(BOF) and Electric Arc Furnace(EAF) slag.
Nippon Slag Association.
Main components： CaO-FeO-SiO2
Steelmaking slag
BOF(Basic Oxygen Furnace) slag
EAF(Electric Arc Furnace) slag
Solidification model
Liquid slag(FeO rich)
2CaO・SiO2 (P2O5 rich)
P2O5 tends to distribute in 2CaO･SiO2
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
FeO
FeO
FeO
FeO
FeO
FeO

## Slide 13
 | CaO | SiO2 | T-Fe | MgO | Al2O3 | S | P2O5 | MnO
BOF | 45.8 | 11 | 17.4 | 6.5 | 1.9 | 0.06 | 1.7 | 5.3
EAF | 22.8 | 12.1 | 29.5 | 4.8 | 6.8 | 0.2 | 0.3 | 7.9
FeO
FeO
FeO
FeO
Background
Compositions of Basic Oxygen Furnace(BOF) and Electric Arc Furnace(EAF) slag.
Nippon Slag Association.
Main components： CaO-FeO-SiO2
Steelmaking slag
BOF(Basic Oxygen Furnace) slag
EAF(Electric Arc Furnace) slag
Solidification model
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
FeO
FeO
FeO
FeO
FeO
FeO
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
FeO
FeO
FeO
FeO
FeO
FeO
FeO
FeO
FeO
If these are able to be separated, they can be used more effectively.
P2O5 rich 2CaO・SiO2
FeO rich liquid slag
Reuse as an iron-making material
Fertilizer and chemical industry
For example :

## Slide 14
FeO
FeO
FeO
FeO
Background
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
FeO
FeO
FeO
FeO
FeO
FeO
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
P2O5
FeO
FeO
FeO
FeO
FeO
FeO
FeO
FeO
FeO
P2O5 rich 2CaO・SiO2
FeO rich liquid slag
Separation
Investigate the possibilities of separating the 2CaO･SiO2 solid phase from the liquid phase of steelmaking slag.
The purpose of this study

## Slide 15
Experiment B：Addition of sintered CaO to slag.
Separation of the FeO-rich liquid and P2O5-rich 2CaO･SiO2 by absorption of FeO-rich liquid to sintered CaO.
Experiment A : floatation of 2CaO・SiO2
Separation of FeO-rich liquid and P2O5-rich 2CaO･SiO2
by density difference between liquid slag and 2CaO･SiO2

## Slide 16
Cooling water
Gas outlet
Gas inlet
Cooling water
Sample slag(8 g)
Composition：45.8 mass%CaO – 43.1 mass%FeO
– 8.1 mass%SiO2 – 3.0 mass%P2O5
Crucible：MgO crucible
Atmosphre：Ar(100 ml/min)
Experimental temperature：1523、1573、1623、1673 K
Holding time：4 hours
Experimental condition
Apparatus and Procedure
Experiments
slag
(8 g)
MgO crucible

## Slide 17
Procedure and principles.
v
v
v
v
v
v
v
Sample slag(8 g)
Composition：45.8 mass%CaO – 43.1 mass%FeO
– 8.1 mass%SiO2 – 3.0 mass%P2O5
Crucible：MgO crucible
Atmosphre：Ar(100 ml/min)
Experimental temperature：1523、1573、1623、1673 K
Holding time：4 hours
Experimental condition
1673 K
1623 K
1573 K
1523 K
4 hours
1 hour
quench
1823 K
200 K/hour
melting
solid-liquid coexistance
Experimental
temperature

## Slide 18
Photo of the vertical section of the sample at 1623 K.
10 mm
1673 K
1623 K
1573 K
1523 K
4 hours
1 hour
quench
1823 K
200 K/hour
melting
solid-liquid coexistance
1623 K
Sample slag(8 g)
Composition：45.8 mass%CaO – 43.1 mass%FeO
– 8.1 mass%SiO2 – 3.0 mass%P2O5
Crucible：MgO crucible
Atmosphre：Ar(100 ml/min)
Experimental temperature：1523、1573、1623、1673 K
Holding time：4 hours
Experimental condition
SEM-EDS analysis

## Slide 19
500 μm
50 μm
50 μm
50 μm
SEM images of the sample of 1623 K
1623 K

## Slide 20
Temp.1623 K | Composition (mass%) |  |  |  | 
Phase | CaO | FeO | SiO2 | MgO | P2O5
Initial | 45.8 | 43.1 | 8.1 | 0 | 3.0
CaO | 88.5 | 10.1 | 0.2 | 1.2 | 0.0
2CaO･SiO2 | 59.7 | 3.2 | 27.9 | 0.1 | 9.1
Liquid | 34.7 | 62.7 | 1.0 | 1.3 | 0.3
(Mg,Fe)O | 1.6 | 27.6 | 0.2 | 70.5 | 0.1
Observed phases
- CaO solid.
2CaO･SiO2 solid.
(Mg,Fe)O solid.
Liquid.
▲Initial
◆CaO
◆2CaO･SiO2
◆Liquid
2CaO･SiO2
CaO
(Mg,Fe)O
Liquid
50 µm
Composition of Phases
Composition of each phase

## Slide 21
Temp.1623 K | Composition (mass%) |  |  |  | 
Phase | CaO | FeO | SiO2 | MgO | P2O5
Initial | 45.8 | 43.1 | 8.1 | 0 | 3.0
CaO | 88.5 | 10.1 | 0.2 | 1.2 | 0.0
2CaO･SiO2 | 59.7 | 3.2 | 27.9 | 0.1 | 9.1
Liquid | 34.7 | 62.7 | 1.0 | 1.3 | 0.3
(Mg,Fe)O | 1.6 | 27.6 | 0.2 | 70.5 | 0.1
▲Initial
◆CaO
◆2CaO･SiO2
◆Liquid
2CaO･SiO2
CaO
(Mg,Fe)O
Liquid
50 µm
Composition of Phases
Composition of each phase
・This result is good agreement with the phase diagram.
・FeO was concentrated in liquid phase
・P2O5 was clearly distributed in 2CaO･SiO2

## Slide 22
Temp.1623 K | Composition (mass%) |  |  |  | 
Phase | CaO | FeO | SiO2 | MgO | P2O5
Initial | 45.8 | 43.1 | 8.1 | 0 | 3.0
CaO | 88.5 | 10.1 | 0.2 | 1.2 | 0.0
2CaO･SiO2 | 59.7 | 3.2 | 27.9 | 0.1 | 9.1
Liquid | 34.7 | 62.7 | 1.0 | 1.3 | 0.3
(Mg,Fe)O | 1.6 | 27.6 | 0.2 | 70.5 | 0.1
2CaO･SiO2
CaO
(Mg,Fe)O
Liquid
50 µm
Composition of Phases
Composition of each phase
These 4 phases were also observed in the other areas of sample.
▲Initial
◆CaO
◆2CaO･SiO2
◆Liquid

## Slide 23
1 mm
50 μm
50 μm
50 μm
SEM images of one sample
2CaO･SiO2
CaO
(Mg,Fe)O
Liquid
Solid phase
Be concentrated
Very little

## Slide 24
▲ Initial
● Upper
● Lower
500 μm
Composition by area.
Results
Temp.1623 K | Composition (mass%) |  |  |  | 
Area | CaO | FeO | SiO2 | MgO | P2O5
Initial slag | 45.8 | 43.1 | 8.1 | 0 | 3.0
Upper area | 47.4 | 28.9 | 15.6 | 3.7 | 4.4
Lower area | 38.5 | 50.8 | 4.9 | 4.5 | 1.3
Compositions of each areas.

## Slide 25
▲ Initial
● Upper
● Lower
500 μm
Results
Temp.1623 K | Composition (mass%) |  |  |  | 
Area | CaO | FeO | SiO2 | MgO | P2O5
Initial slag | 45.8 | 43.1 | 8.1 | 0 | 3.0
Upper area | 47.4 | 28.9 | 15.6 | 3.7 | 4.4
Lower area | 38.5 | 50.8 | 4.9 | 4.5 | 1.3
Composition by area.

## Slide 26
FeO and P2O5 mass ratio
 | 1523 K | 1573 K | 1623 K | 1673 K
 | 0.67 | 0.61 | 0.57 | 0.62
 | 2.4 | 3.6 | 3.4 | 2.2
The results for the other temperatures.
Chart: 
| 1523 K | 1573 K | 1623 K | 1673 K
 | 0.67 | 0.613 | 0.568 | 0.62
Chart: 
| 1523 K | 1573 K | 1623 K | 1673 K
 | 2.4 | 3.6 | 3.4 | 2.2
No clear temperature dependence was observed.

## Slide 27
Brief summary of experiment A
The floatation method had serious limitations because it was not possible to successfully retrieve the FeO or P2O5.
Even though the sample changed quite dramatically in appearance, analysis showed little change in the composition from top to bottom

## Slide 28
Experiment B：Addition of sintered CaO to slag
Separation of the FeO-rich liquid and P2O5-rich 2CaO･SiO2 by absorption of FeO-rich liquid to sintered CaO.
Experiment A : floatation of 2CaO・SiO2
Separation of FeO-rich liquid and P2O5-rich 2CaO･SiO2
by density difference between liquid slag and 2CaO･SiO2

## Slide 29
Gas outlet
Gas inlet
Silicon rubber seal
Cooling water
slag
(0.165g or 0.680 g)
MgO crucible
CaO crucible：1.58 g (sintered at 1773K)
Slag：0.680 g, 0.165g
Sample held at 1623K for 4hrs
CaO crucible
(1.58g)
1823 K
1 hour
200 K/hour
200 K/hour

## Slide 30
slag
0.165g
slag
0.680 g
CaO crucible
Remained slag
Easily separated

## Slide 31
0.11g of liquid phase was absorbed in CaO crucible
73% of P2O5 and 92% of FeO were recovered

## Slide 32
Gas outlet
Gas inlet
Silicon rubber seal
Cooling water
Sintered CaO ball
Experimental condition
Sintered CaO：0.74 g
Slag：0.15 g
Compositions：45.8 mass%CaO – 43.1%FeO
– 8.1 mass%SiO2 – 3.0 mass%P2O5
Crucible：MgO crucible
Atmosphere：Ar(100 ml/min)
Holding time：1 hour
Procedure
CaCO3
Calcinated
at 1473 K
CaO
Sintered CaO
Pressed into tablet shape (10 MPa)
Sintered 12 hours at 1773 K
Preparation of sintered CaO
same as experiment A

## Slide 33
Gas outlet
Gas inlet
Silicon rubber seal
Cooling water
Sintered CaO ball
Sintered CaO：0.74 g
Slag：0.15 g
Compositions：45.8 mass%CaO – 43.1%FeO
– 8.1 mass%SiO2 – 3.0 mass%P2O5
Crucible：MgO crucible
Atmosphere：Ar(100 ml/min)
Holding time：1 hour
Procedure
Experiments
slag
(0.15 g)
MgO crucible
same as experiment A
Experimental condition

## Slide 34
Procedure and Principle
Experiments
1823 K
1 hour
1 hour
Addition of CaO
1773 K
15 min
Slag tablet
2CaO・SiO2
Sintered CaO ball
Absorption
Sintered CaO：0.74 g
Slag：0.15 g
Compositions：45.8 mass%CaO – 43.1%FeO
– 8.1 mass%SiO2 – 3.0 mass%P2O5
Crucible：MgO crucible
Atmosphere：Ar(100 ml/min)
Holding time：1 hour
same as experiment A
Experimental condition
200 K/hour

## Slide 35
Photo image taken from top of the crucible.
Sintered CaO
Results. (i)
Slag
SEM-EDS analysis

## Slide 36
50 μm
2CaO･SiO2
Liquid
SEM image of sintered CaO
SEM observation of ball.
Results
CaO
Observed phase
・CaO
・2CaO・SiO2
・Liquid
Located in the CaO voids
2CaO・SiO2 was precipitated from liquid phase during cooling to R.T.

## Slide 37
2CaO･SiO2
Liquid
SEM image of separated slag
100 μm
SEM observation of slag.
Results
Observed phases
・2CaO･SiO2
・Liquid―(in the 2CaO･SiO2 voids)
Most of the liquid was absorbed to sintered CaO ball.
MgO Crucible

## Slide 38
43.1mass%
10.1mass%
FeO
3.0 mass%
6.4 mass%
P2O5
x2
Change in composition
P2O5 composition was twice of initial slag.
FeO composition was 1/4 of initial slag
 | Composition (mass%) |  |  |  | 
 | CaO | FeO | SiO2 | MgO | P2O5
Initial slag | 45.8 | 43.1 | 8.1 | 0 | 3.0
Separated slag | 56.7 | 10.1 | 25.1 | 1.7 | 6.4
Sintered CaO | 90.7 | 5.3 | 2.4 | 1.1 | 0.5
87% of P2O5 and 90% of FeO were recovered

## Slide 39
Comparison of both methods.
▲Initial slag
◆Separated slag
◆Sintered CaO
 | Composition (mass%) |  |  |  | 
 | CaO | FeO | SiO2 | MgO | P2O5
Initial slag | 45.8 | 43.1 | 8.1 | 0 | 3.0
Separated slag | 56.7 | 10.1 | 25.1 | 1.7 | 6.4
Sintered CaO | 90.7 | 5.3 | 2.4 | 1.1 | 0.5
▲
◆
◆

## Slide 40
Comparison of experiment .
 | Composition (mass%) |  |  |  | 
 | CaO | FeO | SiO2 | MgO | P2O5
Initial slag | 45.8 | 43.1 | 8.1 | 0 | 3.0
Separated slag | 56.7 | 10.1 | 25.1 | 1.7 | 6.4
Sintered CaO | 90.7 | 5.3 | 2.4 | 1.1 | 0.5
At 1623 K | composition (mass%) |  |  |  | 
area | CaO | FeO | SiO2 | MgO | P2O5
Initial slag | 45.8 | 43.1 | 8.1 | 0 | 3.0
Upper area | 47.4 | 28.9 | 15.6 | 3.7 | 4.4
Lower area | 38.5 | 50.8 | 4.9 | 4.5 | 1.3
Experiment A upper area
Experiment B separated slag
Experiment B was more successful than experiment A
▲Initial slag
◆Separated slag
◆Sintered CaO
●Experiment A
▲
◆
◆

## Slide 41
Summary
In this study, two possible methods for the separation of 2CaO･SiO2 and the liquid phase of steelmaking slag with the aim of finding the best way to recover valuable FeO and P2O5 are investigated.
The floatation method had serious limitations because it was not possible to successfully retrieve the FeO or P2O5. Even though the sample changed quite dramatically in appearance, analysis showed little change in the composition from top to bottom.
The addition of sintered CaO allowed for the successful separation of both FeO and P2O5 from steelmaking slag. This technique has the potential to be applied by industry so that valuable resources can be retrieved from slag and reused.

## Slide 42
On site separation of FeO and P2O5 by use of Capillary effect

## Slide 43: Separation using capillary effect
Absorber+ Fe rich liquid
P2O5 containing 2CaO・SiO2
P2O5 enriched 2CaO・SiO2
Molten steel
Molten slag
Absorber
Converter
P source for fertilizer
Fe source for blast furnace
Absorber+ Fe rich liquid
Absorber
+ Fe rich liquid
P2O5 containing 2CaO・SiO2
Capillary effect

## Slide 44
Magnetic Separation
Magnetic Separation of Phosphorus Enriched Phase from Multiphase Dephosphorization Slag : Hironari Kubo, Kazuyo Matsubae-Yokoyama, Tetsuya Nagasaka, ISIJ International, 50 (2010), 59-64.
Dissolution into Aqueous Solution
Dissolution Behavior of Dicalcium Silicate and Tricalcium Phosphate Solid Solution and other Phases of Steelmaking Slag in an Aqueous Solution : Takuya Teratoko, Nobuhiro Maruoka, Hiroyuki Shibata, Shin-ya Kitamura, High Temperature Materials and Processes, 31(2012), 329–338.
Other possible ways to separate FeO and P2O5

## Slide 45
Slag : Glass-like by-product left over after a desired metal has been separated from its raw ore
Slag is By-product, not Waste!
Meaning of Slag

## Slide 46
Thank you for your kind attention!