## Slide 1: Valorisation of stainless steel slag by selective Cr recovery and carbonation of the matrix material
E.Kim1,2, J.Spooren1, K.Broos1, L.Horckmans1, P.Nielsen1, M.Quaghebeur1
1Flemish Institute for Technological Research, VITO
2Department of Bioengineering, University of Antwerpen

## Slide 2: Goals
selectively recover Cr from a low grade (secondary) ore by hydrometallurgical method
safely reuse the matrix material after removal of Cr

## Slide 3: Proposed process flow
Compress strength: 38MPa
25mm(D)x11mm(H)
1
2
3

## Slide 4: Carbonation of the residue

## Slide 5: Conclusions
The leaching efficiency of Cr under alkaline oxidizing conditions increased with temperature and MA time.
Optimal reaction condition: 240 °C, 6hr, MA 30min, 1M NaOH, 8.4 bar pO2.
After Cr leaching by APL and MA the matrix material can be used after a subsequent washing step for the production of building materials through a carbonation step.