## Slide 1: Treatment and recycling of Electric Arc Furnace slag processing water
B. Wendler * M. Kozariszczuk
VDEh-Betriebsforschungsinstitut GmbH, Sohnstr. 65, 40476 Düsseldorf

## Slide 2: Aim of research project
Research project SLACON
Work is part of a European research project co-ordinated by FEhS
Project aim is improvement of slag quality defined by eluate tests
Slag production in electric arc furnace
Eluate
test
Slag
Slag for utilisation in the construction industry
Slag
Water
Process development for water treatment and recycling
Slag processing: cooling, washing, sizing
Adsorption treatment
for water recycling
Process development for improved slag quality

## Slide 3: Treatment of slag processing water
Investigation of water treatment for recycling
For water recycling, leached elements (Vanadium, Molybdenum, Fluoride) have to be removed from water from slag processing - without input of substances that might accumulate in the water cycle
Slag processing water is highly alkaline, with high total ion concentration - a selective process for removal of leached elements is needed
Laboratory tests
Precipitation with Fe2(SO4)3
Adsorption on iron hydroxide based adsorbent
On-site tests
In the on-site test of adsorption 80 m³ of water have been treated
Very low residual concentrations have been obtained, Vanadium 1 µg/l, Molybdenum 2 µg/l

## Slide 4: Treatment of slag processing water
Outlook
A national research project is planned, investigating
Consequences of new legislation in Germany (Ersatzbaustoffverordnung)
An adapted slag washing process with integrated water treatment
For more information and discussion you are welcome at our poster !
Contact
barbara.wendler@bfi.de +49 211 6707 - 982
matthias.kozariszczuk@bfi.de +49 211 6707 - 494