## Slide 1
Towards Red mud Valorisation:
EAF Smelting process for iron recovery and slag design for use as precursor in the construction industry
B. Xakalashe, B. Friedrich
Slag Valorisation Symposium
Mechelen 02. April. 2019

## Slide 2: Bayer Process – Generation of Red Mud
Digestion
Clarification
Precipitation
Calcination
Production:
>150 x 106 Mt/year
Stock: 4 x 109 Mt
Bauxite ores
30-54% Al2O3
Alumina

## Slide 3: Red Mud – Resource and Challenges
Components | Fe2O3 | Al2O3 | CaO | SiO2 | TiO2 | Na2O
Typical range (wt.%) | 5- 60 | 5-30 | 2-14 | 3-50 | 0.3-15 | 1-10
Trace elements: As, Be, Cd, Cr, Cu, Ga, Hg, K, Mn, Pb, REEs, Sc, Th,
U, V, Zn, REEs
Potential resource of valuable elements
Challenges:
Generation of residue during extraction
Low reactivity
Leaching of heavy metals
UP

## Slide 4: Zero Waste Valorisation of Red Mud
Horizon 2020: MSCA–ETN Redmud
“European Training Network for Zero-waste Valorisation of Bauxite Residue (Red Mud)“
http://etn.redmud.org/
Alumina
IME

## Slide 5: EAF Smelting Process
Red Mud (MYTILINEOS Aluminium of Greece)
Component | Fe2O3 | Al2O3 | CaO | SiO2 | TiO2 | Na2O | Cr2O3 | V2O5
Wt.% | 43.5 | 24.0 | 10.2 | 5.5 | 5.6 | 2 | 0.4 | 0.1
3C + Fe2O3 = 2Fe + 3CO
Silica fluxing
lime fluxing
RM
Fe recovery to metal phase
High melting slag
Lower operating temperatures
Fluid slag
Silica sand: aluminosilicate, vitreous slag
(Inorganic polymer)
Lime: calcium aluminate, crystalline slag
(cement clinker)
Fluxing

## Slide 6: Experimental Procedure – EAF Smelting
100 kW DC furnace
Operated (3-6kW)
Batch mass:1.5kg Red Mud
Lignite Coke: 0.1 x Red Mud
(Reducing agent)
Silica sand: 0.2 x Red Mud
Lime: 0.4 x Red Mud
Operating Temperature: 1500 – 1550oC
Holding Time: 1 hour
Slag cooling: Slow - 30oC/min
UP
Pig Iron
(Fe)
slag

## Slide 7: Silica Fluxed Slag
Components | Fe2O3 | Al2O3 | CaO | SiO2 | TiO2 | Na2O
RM (wt.%) | 43.5 | 24.0 | 10.2 | 5.5 | 5.6 | 1.8
Slag (wt.%) | 1.2 | 36.8 | 15.3 | 38.0 | 7.3 | 2.4
Fe removal achieved
Vitreous slag achieved UP
Silica fluxed slag
Red Mud
Intensity (A.U.)

## Slide 8: Lime Fluxed Slag
Components | Fe2O3 | Al2O3 | CaO | SiO2 | TiO2 | Na2O
RM (wt.%) | 43.5 | 24.0 | 10.2 | 5.5 | 5.6 | 1.8
Slag (wt.%) | 0.6 | 31.5 | 53.9 | 8.9 | 6.2 | 0.5
Fe removal achieved
Crystalline slag achieved UP
Silica fluxed slag
Red Mud
Intensity (A.U.)

## Slide 9: Metal Analysis
Component | Fe | C | Si | Ti | Cr | V | P | S
Silica fluxed | 91.8 | 5 | 1.7 | 0.3 | 0.5 | 0.2 | 0.1 | 0.03
Recovery | high | - | low | low | high | high | - | -
Lime fluxed | 93 | 5.1 | 0.1 | 0.3 | 0.5 | 0.2 | 0.2 | 0.01
Recovery | high | - | low | low | high | high | - | 
High recovery of Fe, Cr, V achieved (cleaning)
Low Si and Ti recovery
Pig iron can be used in secondary steel making
Pig iron caUP

## Slide 10: Synergistic Waste Treatment with Red Mud
MSWI BA: Municipal Solid Waste Incineration bottom ash
Waste produce around all EU
20 million tonnes/year
It’s a SiO2-CaO-Al2O3 acid slag (rich in silica ~50%)
BOF: Basic Oxygen Furnace Slag (from Steel making)
Waste produce around all EU
10 million tonnes/year
It’s mainly CaO-FeO basic slag (rich in CaO ~40%)

## Slide 11: Synergistic waste treatment with Red Mud
Acidic slags
Basic slags
RM
MSWIBA
BOF
Highly amorphous
Vitrified MSWI Bottom Ash
Amorphous
Low melting point
Highly crystalline
Low melting point and low viscosity
Combined recovery of Iron (BOF+RM)

## Slide 12: Conclusions
Red mud was successfully smelted for iron recovery and conditioning of slag
Cleaning of the mineral phase (slag) was achieved
Production of a vitreous slag under silica fluxing was achieved
Production of a crystalline slag enriched in calcium aluminate phases was demostrated
Utilisation of the produced mineral phase in the construction industry could lead to zero waste valorisation of red mud
UP