## Slide 1: Utilization of slags for development of fire resistant geopolymers
Prof. D. Panias
Dr. K. Sakkas
Dr. I. Giannopoulou
Slag Valorization Symposium 2019
National Technical University of Athens
School of Mining and metallurgical engineering
Laboratory of metallurgy

## Slide 2
Research Motives
Utilization of slags produced from two different European metallurgical companies as precursors for production of Fire Resistant Geopolymers for passive fire protection of concrete constructions

## Slide 3
What’s the fire effect on concrete constructions?
Dehydration of concrete
380oC
500oC
(a) pore pressure rising due to evaporating water
(b) compression of the heated surface due to a thermal gradient
(c) internal cracking due to difference in thermal expansion between aggregate and cement paste;
(d) cracking due to difference in thermal expansion/deformation between concrete and reinforcement rebars
(e) strength loss due to chemical transitions
Concrete Spalling

## Slide 4
What’s the fire effect on steel rebars?
Substantial loss of mechanical strength due to heating caused by fires
Effect of temperature on mechanical strength
of hot rolled structural steel
Design Strength

## Slide 5
Collapse of concrete constructions due to fire events
Mont Blanc tunnel fire, 1996
Eastern Attica, Greece summer Fire - 2018

## Slide 6
How does a fire resistant materials work ?
Concrete
Structural steel rebars
Fire Resistant Lining
≤ 380oC

## Slide 7
Specifications for fire resistant geopolymers
Density 800-1400 kg/m³
To resist either to ISO-834 cellulosic fire or to RABT simulated fire incidents
Compressive strength > 2MPa

## Slide 8
Market Size of Fire Resistant Materials
Worldwide passive fire protection market is expected to reach 7.13 billion US dollars by 2022
According to numerous studies the annual revenues of the European passive fire protection market follows a steady growing rate expected to reach 1.57 billion US dollars by 2022

## Slide 9
RAW MATERIAL-1: Slag from BOLIDEN
Component | %
FeO | 44,51
Al2O3 | 3,30
SiO2 | 39,88
TiO2 | 0,82
Na2O | 0,60
CaO | 4,08
SO3 | 1,19
P2O5 | 0,21
Cr2O3 | 0,25
ZnO | 1,77
MgO | 1,47
Totally amorphous Fayalitic slag

## Slide 10
Synthesis Conditions for ISO-834 fires
Synthesis Conditions | 
Activator | KOH – 8M
Slag/Activator Ratio | 6 g/mL
Foaming Agent | Al powder – 0,23% w/w
Setting at ambient Temperature
The paste sets at ambient temperature after 3,5 hours

## Slide 11
Materials Properties
Apparent Density = 1060 kg/m³
Compressive strength = 3 MPa
Fire Resistance Test (EFNARC Guidelines)
Composite Specimen
40cm
40cm
15cm
2cm
Concrete Substrate
Rectangular Specimen
40 x 40 cm
with Thickness 15cm
Geopolymer Lining
Rectangular Specimen
40 x 40 cm
with Thickness 2cm
Fire Resistant Anchors
Temperature gradient : 44 °C/mm
Max temperature at the concrete/geolopolymer interface is 160 °C which is lower than the test success limit of 180 °C
After Fire Test
No Damages
Only a small superficial crack

## Slide 12
RAW MATERIAL-2: Slag from Metallo
Component | %
FeO | 41,65
Al2O3 | 8,47
SiO2 | 31,77
TiO2 | 0,82
Na2O | 2,22
CaO | 4,63
SO3 | 0,92
P2O5 | 1,71
Cr2O3 | 1,38
ZnO | 1,14
MgO | 1,46
Totally amorphous Fayalitic slag
C
C
F
F
F: Fayalite Fe2SiO4
C: Clinoferrosilite FeSiO3

## Slide 13
Synthesis Conditions for RABT fires
Synthesis Conditions | 
Activator | KOH – 9M
Slag/Activator Ratio | 3,6 g/mL
Foaming Agent | Al powder – 0,09% w/w
Fluxes added | Al2O3 – 20% w/w
The paste sets at ambient temperature after 3 hours
Setting at ambient Temperature

## Slide 14
Materials Properties
Apparent Density = 1080 kg/m³
Compressive strength = 5 MPa
Composite Specimen
40cm
40cm
15cm
3,5cm
Concrete Substrate
Rectangular Specimen
40 x 40 cm
with Thickness 15cm
Geopolymer Lining
Rectangular Specimen
40 x 40 cm
with Thickness 3,5cm
Before Fire Test
Temperature gradient : 33 °C/mm
Temperature gradient :
30 °C/mm
Max temperature at the concrete/geolopolymer interface is 200 °C which lower than the test success limit of 380 °C
After Fire Test
Magnification at high contrast
No Damages
No cracks

## Slide 15
Competition & Procurement Cost of Materials
Companies dominating the market of fire resistant materials |  |  | 
Promatect®T | PassiveTec® Pro | Aestuver T® | Tecbor®
Geopfire
22 – 42 €/m2
10 – 18 €/m2

## Slide 16
Conclusions
Both slags as well as any Fayalitic slag from other metallurgical sectors such as ferroalloys production are very good precursors for production of Fire Resistant Geopolymers for passive fire protection of concrete constructions
Both slags give excellent materials for protection of concrete from cellulosic fires (ISO-834)
The Metallo slag after modification (doping with alumina) gave excellent material for protection of concrete from more severe fire scenarios like the RABT one
The same can happen with the Boliden slag after chemical modification applying the proprietary methodology of GEOVALIN, a Greek Spin-off established for commercializing fire resistant geopolymers