## Slide 1
Recovering chromium from stainless steel slag and ferrochrome slags
Frantisek Kukurugya, Liesbeth Horckmans, Jeroen Spooren
VITO NV
6th International Slag Valorization Symposium
Mechelen
02-04/04/2019

## Slide 2: CHROMIC (H2020 project)
New recovery processes for critical and valuable metals
Smart combinations of existing methods and new technological innovations to extract valuable and critical metals from slags
SS FeCr
SS FeCr
Nb Cr Mo V
Nb Cr
Mo V
Nb Cr
Dillute Leachate
Mo V
To Metal Products
Metal Depleted Stream
Metal Depleted Stream
efﬁcient mineral processing
Selective Leaching
ﬁne metals to production
Regenerated Leaching Solution
Selective Material Recovery
Use as construction materials
Current System
Primary Ores
Scrap
Metal Production
CS, SS, FeCr
By-product: Slag
Slag
Cr
Nb
Mo V
CHROMIC
Use as construction materials

## Slide 3: Chemical and mineralogical composition
XRF |  | CS slag | SS slag | LC FeCr slag | HC FeCr slag
Al2O3 | wt.-% | 10.0 | 4.2 | 6.5 | 17.9
CaO | wt.-% | 22.8 | 45.1 | 45.9 | 2.5
Fetot | wt.-% | 28.2 | 0.6 | 0.18 | 6.4
MgO | wt.-% | 3.7 | 11.0 | 12.6 | 14.9
MnO | wt.-% | 6.0 | 1.1 | 0.11 | 0.20
SiO2 | wt.-% | 10.6 | 30.8 | 28.8 | 12.6
Cr | wt.-% | 2.6 | 2.5 | 3.2 | 11.5
Mo | mg/kg DM | 47 | 40 | <LLD | <LLD
Nb | mg/kg DM | 245 | 617 | <LLD | <LLD
V | mg/kg DM | 744 | 516 | 448 | 424
Material | Main minerals | Cr-rich phases
CS Slag | Ca-silicates (larnite, gehlenite), Fe-oxides (wuestite), spinel (Fe3O4, MgFe2O4) | Spinel (MgCr2O4)
LC FeCr/HC FeCr | Ca-silicates (merwinite, bredigite, larnite, gehlenite), spinel (MgAl2O4; MgCr2O4) | Ferrochrome particles, spinel MgCr2O4
SS slag | Ca-silicates (merwinite, bredigite, gehlenite, cuspidine), calcite | Spinel (MgCr2O4)
CS slag
(carbon steel slag)
SS slag
(stainless steel slag)
LC FeCr slag
(low carbon ferrochrome slag)
HC FeCr slag
(high carbon ferrochrome slag)
Challenges: low grade ores, spinel structure
Focus: Cr

## Slide 4: Introduction

## Slide 5
Mineral processing

## Slide 6: Mineral processing
Magnetic separation
LIMS & HIMS
0.15T & 1T
WLIMS & WHIMS
0.1T & 1T
WHIMSe
0-2T
Density separation
CS slag
SS slag
LC FeCr slag
HC FeCr slag

## Slide 7: Magnetic separation – CS slag
(70% Fe recovery)

## Slide 8: Magnetic separation – SS slag
D90 = 150 µm
Delivered as a fine powder – no need to crush or mill
31% Cr recovery

## Slide 9: Magnetic separation – LC FeCr slag
FeCr
To use WHIMS(e) material needs to be milled <125 µm = extra costs

## Slide 10: Magnetic separation – HC FeCr slag
50 – 75% Cr recovery in M(Ferrite) fractions

## Slide 11: Density separation – HC FeCr slag
stroke speed = 250 rpm
washing water = 1000 L/h
feed water = 250 L/h
5 output fractions
Fraction 1
(56.0 wt.%)
Fraction 2
(32.4 wt.%)
Fraction 3
(11.3 wt.%)
Fraction 4
(0.2 wt.%)
Fraction 5
(0.1 wt.%)
35% Cr recovery
45% Fe recovery
1% Cr recovery
2% Fe recovery

## Slide 12
Selective leaching

## Slide 13: Selective leaching
Using MW heating = fast, selective and effective heating
Alkaline leaching was selected to avoid of matrix dissolution
Microwave assisted leaching => 100 – 200°C
Microwave assisted roasting followed by water leaching => ≥200 °C
FlexiWave – MW assisted leaching
PyroWave – MW assisted roasting

## Slide 14: MW assisted leaching – CS slag
Effect of alkaline source (NaOH) addition
728 mg/L Cr
455 mg/L Cr
Results
44% Cr extraction after 1h MW treatment + 1h washing
dissolution of Al and Ca below 1%
<7.5mg/L V; <10 mg/L Mo, <40 mg/L Si, <100 mg/L Al,

## Slide 15: MW roasting and water leaching – SS slag
Results
95% Cr extraction was achieved with limited dissolution (<100 ppm) of Al, Ca and Mn
Cr content in solid residue decreases from 2% to 0.2%
Conventional roasting : 400°C for 2h (heating rate 120°C/h)
or
MW roasting: 400°C for 30 min. (+ heating time 10 min)
Water leaching: 50°C, L/S=10, 1h
Analysis (XRF, ICP-OES)

## Slide 16: MW assisted roasting and water leaching – SS slag
Sample description:
1 - 3g sample + 2g NaOH
2 - 3g sample + 2g NaOH + 0.2g NaNO3
3 - 3g sample + 1.5g NaOH + 0.2g NaNO3
4 - 3g sample + 1g NaOH + 0.2g NaNO3
5 - 3g sample + 0.5g NaOH + 0.2g NaNO3
MgCr2O4 + 4NaOH + O2(g) = MgO + 2Na2CrO4 + 2H2O
After roasting
Leachate
(after washing)
Solid residue
(after washing)
50-180 mg/L Al; 40-150 mg/L Mn 70-230 mg/L Si
50-90 mg/L Ca; 10-12 mg/L V
90%

## Slide 17: MW assisted roasting and water leaching
Is it possible to reduce roasting temperature?
90% Cr
200°C
300°C
400°C
Mixing with small amount of water ensure proper contact of reagents with Cr-spinel
Reaction with KOH has more negative ΔG values
No additional oxidant needed when KOH is used
MgCr2O4 + 4NaOH + O2(g) = MgO + 2Na2CrO4 + 2H2O
MgCr2O4 + 4KOH + O2(g) = MgO + 2K2CrO4 + 2H2O

## Slide 18: Conclusion
Physical separation
By applying magnetic or density separation, Cr content can be increased by factor more than 3
Summary of the physical separation |  |  |  |  | 
Slag sample | Technique | Initial Cr [%] | Cr content after separation [%] | Yield [%] | Cr recovery [%]
LC FeCr | WHIMSe | 3.2 | 7.3 | 2.5 | 25
HC FeCr | LIMS | 11.5 | 27.6 | 20 | 50
SS | WHIMS | 2.5 | 8.8 | 7 | 31
HC FeCr | WST | 10.1 | 32.8 | 12 | 46
Selective leaching
MW heating show potential in recovering Cr from Cr-containing slags
More than 40% of Cr can be selectively extracted from CS slag by MW assisted leaching
More than 90% of Cr can be selectively extracted by MW roasting followed by water leaching

## Slide 19: Thank you for your attention fero.kukurugya@vito.be