## Slide 1
“Thermodynamics of conditioning MSWI bottom ash using SAF for usage in minerals products”
H. Lucas, B. FRIEDRICH
Slag Valorisation Symposium
01-05 April 2019

## Slide 2: Outline
Introduction
Thermal treatment of IBA
Mechanisms of IBA decomposition
Conclusions

## Slide 3: Introduction
MSW
Mass reduction > 60% wt.
Landfill
IBA
Aggregates
and/or

## Slide 4: Introduction
MSW
Mass reduction > 60% wt.
Landfill
IBA
Aggregates
 | L/S dependence test (L/S = 10 l/kg) |  |  | pH dependence test (L/S = 10 l/kg) | 
 | Close to the limit | Partially exceeding | Consistently exceeding | Partially exceeding | Consistently exceeding
IBA | Cd, Se, Zn | Cr, Mo, Ni, Pb, Sb, SO4 | Cl, Cu | Cd. Cr, Ni, Pb, Se, Zn | Cl, Cu, Mo, Sb, SO4
H. Saveyn, P. Eder, E. Garbarino, L. Muchova, O. Hjelmar, H. van der Sloot, R. Comans, A. van Zomeren, J. Hyks, A. Oberender. Study on methodological aspects regarding limit values for pollutants in aggregates in the context of the possible development of end-of-waste criteria under the EU Waste Framework Directive
and/or

## Slide 5
Thermal treatment of IBA
Glass
Recover Metal
Metal
9-12% IBA
Slag
65-70% IBA
Slag: ~100% amorphous
45-50%
18-21%
16-20%
Others:
.
Recovered Metal
75-90 % Fe
5-15 %Cu
Others (Cr, Ni, Ag, Au)

## Slide 6
Thermal treatment of IBA
Glass
Recover Metal
“Vitrified slag free of hazardous elements
(Cr, Mo, Co, Pb, Zn, etc.)
Metal
9-12% IBA
Slag
65-70% IBA
Slag: ~100% amorphous
45-50%
18-21%
16-20%
Others:
Recovered Metal
75-90 % Fe
5-15 %Cu
Others (Cr, Ni, Ag, Au)
Crystalline
Amorphous

## Slide 7: Thermal treatment of IBA
wt.% | SiO2 | CaO | Al2O3 | Na2O | Fe2O3 | ZnO | CuO | PbO | SO3 | Cl | C
IBA | 39.1 | 23.70 | 8.18 | 3.00 | 7.95 | 0.95 | 0.53 | 0.26 | 2.77 | 1.62 | 5.55
Slag | 48.3 | 22.60 | 18.51 | 3.73 | 0.76 | 0.01 | 0.14 | 0.01 | 1.48 | 0.02 | 0.11
Al2O3
Fe
C
CaO
S
P
SiO2
Cu
Zn

## Slide 8: Thermal treatment of IBA
wt.% | SiO2 | CaO | Al2O3 | Na2O | Fe2O3 | ZnO | CuO | PbO | SO3 | Cl | C
IBA | 39.1 | 23.70 | 8.18 | 3.00 | 7.95 | 0.95 | 0.53 | 0.26 | 2.77 | 1.62 | 5.55
Slag | 48.3 | 22.60 | 18.51 | 3.73 | 0.76 | 0.01 | 0.14 | 0.01 | 1.48 | 0.02 | 0.11
Charging
Al2O3
Fe
C
CaO
S
P
SiO2
Cu
Zn

## Slide 9: Thermal treatment of IBA
wt.% | SiO2 | CaO | Al2O3 | Na2O | Fe2O3 | ZnO | CuO | PbO | SO3 | Cl | C
IBA | 39.1 | 23.70 | 8.18 | 3.00 | 7.95 | 0.95 | 0.53 | 0.26 | 2.77 | 1.62 | 5.55
Slag | 48.3 | 22.60 | 18.51 | 3.73 | 0.76 | 0.01 | 0.14 | 0.01 | 1.48 | 0.02 | 0.11
Charging
Al2O3
Fe
C
CaO
S
P
SiO2
Cu
Zn

## Slide 10: Thermal treatment of IBA
wt.% | SiO2 | CaO | Al2O3 | Na2O | Fe2O3 | ZnO | CuO | PbO | SO3 | Cl | C
IBA | 39.1 | 23.70 | 8.18 | 3.00 | 7.95 | 0.95 | 0.53 | 0.26 | 2.77 | 1.62 | 5.55
Slag | 48.3 | 22.60 | 18.51 | 3.73 | 0.76 | 0.01 | 0.14 | 0.01 | 1.48 | 0.02 | 0.11
Charging
Al2O3
Fe
C
CaO
S
P
SiO2
Cu
Zn

## Slide 11: Thermal treatment of IBA
wt.% | SiO2 | CaO | Al2O3 | Na2O | Fe2O3 | ZnO | CuO | PbO | SO3 | Cl | C
IBA | 39.1 | 23.70 | 8.18 | 3.00 | 7.95 | 0.95 | 0.53 | 0.26 | 2.77 | 1.62 | 5.55
Slag | 48.3 | 22.60 | 18.51 | 3.73 | 0.76 | 0.01 | 0.14 | 0.01 | 1.48 | 0.02 | 0.11
Charging
Conditioning
Al2O3
Fe
C
CaO
S
P
SiO2
Cu
Zn

## Slide 12: IBA Decomposition
Al2O3
SO3
Fe2O3
Cl
C
CO2
SO2
ZnO
CuO
PbO
CO

## Slide 13: IBA Decomposition
Al2O3
SO3
Fe2O3
Cl
C
CO2
SO2
1st phase
2st phase
3rd phase
ZnO
CuO
PbO
CO

## Slide 14: IBA Decomposition
Unburnt
Al2O3
SO3
Fe2O3
Cl
C
CO2
SO2
Carbonates
1st phase
2st phase
3rd phase
ZnO
CuO
PbO

## Slide 15: IBA Decomposition
Al2O3
SO3
Fe2O3
Cl
C
CO2
SO2
1st phase
2st phase
3rd phase
ZnO
CuO
PbO
CO

## Slide 16
H: Hematite
M: Magnetite
A: Anhydryte
W: Wurtzite
Ca: Calcite
Cr: Cristobalite
Q: Quartz
Co: Corundum
Me: Melilite
Wo: Wollastonite
P: Pseudo-
wollastonite

## Slide 17
H: Hematite
M: Magnetite
A: Anhydryte
W: Wurtzite
Ca: Calcite
Cr: Cristobalite
Q: Quartz
Co: Corundum
Me: Melilite
Wo: Wollastonite
P: Pseudo-
wollastonite

## Slide 18: IBA Decomposition
Al2O3
SO3
Fe2O3
Cl
C
CO2
SO2
1st phase
2st phase
3rd phase
ZnO
CuO
PbO

## Slide 19
H: Hematite
M: Magnetite
A: Anhydryte
W: Wurtzite
Ca: Calcite
Cr: Cristobalite
Q: Quartz
Co: Corundum
Me: Melilite
Wo: Wollastonite
P: Pseudo-
wollastonite

## Slide 20: Outlook/ Conclusions
IBA doesn’t need addition of reductants or fluxing agents to reduce the melting point.
Commercial glass (SiO2-Na2O-CaO matrix) + CaO (decomposition of CaCO3) favours the dissolution of high melting point minerals (quartz, rutile, corundum, etc.).
The range between 800 and 1.300˚C is crucial to cleaning IBA from potentially contaminating pollutants (Cl, Zn, Pb, Cu, Co, Mo).
High temperatures allow to homogenize and separate metals from the slag.
Due to its high silica content, once IBA re-melted, it presents an amorphous and chemically stable structure.

## Slide 21
hlucas@ime-aachen.de
IME Process Metallurgy and Metal Recycling
RWTH Aachen University
Prof. Dr.-Ing. Dr. h.c. Bernd Friedrich
www.ime-aachen.de