## Slide 1: A STUDY ON THE LEACHABILITY OF METALS FROM MODIFIED COPPER SLAG FOR ADDED VALUE APPLICATIONS.
Jakob Kero
Jakob.kero@ltu.se
Ph.D. student in Process Metallurgy,
Luleå University of technology, Sweden

## Slide 2: Outline
Background
Methodology
Results
Summary

## Slide 3: Background - the project IQ slag
Project aims:
Broaden the application areas of copper slag
Quality assurance of the slag product/s
Slag modification
Lime, CaO
Compositions 2FeO-SiO2 to CaO-FeO-SiO2
Slag products
Composition
Leaching behaviour
Up to 25 wt. %
Process conditions
Cooling conditions
Parameters:
Flux
Innovative quality assured fayalite slag products

## Slide 4: Background - the project IQ slag
Project aims:
Broaden the application areas of copper slag
Quality assurance of the slag product/s
Slag modification
Lime, CaO
Compositions 2FeO-SiO2 to CaO-FeO-SiO2
Slag products
Up to 25 wt. %
Parameters:
Process conditions
Cooling conditions
Composition
Leaching behaviour
Flux
Innovative quality assured fayalite slag products

## Slide 5: Background – process overview
Pyrometallurgical copper extraction
Slag former SiO2 , air, heat
Pyrometallurgical processes
Smelting – converting - refining
Cu-conc.
Cu-Fe-S
Electrorefining
Slag, FeO-SiO2
SO2- gas
Slag modification
Slag products
Cu-recycling
CaO
Secondary Cu-conc.
Cu-metal
Sulphuric acid

## Slide 6: Scope of slag modification
Slag modification
CaO up to 25 %
Slag products
Analysis of slag products
Smelting
Semi-slow cooling
Lab-scale trials - slag modification
Characterisation of the crystalline slag samples Investigation of leaching behavior
Feasibility study for industrial full-scale trials
Aims: Investigate possible process modifications - Amount of lime addition - Liquidus temperatures Lowering content and leachability of critical environmental elements in slag product

## Slide 7: Methodology
Smelting conditions
6 Samples CaO : 3.7 (0), 5, 10, 15, 20 and 25 wt. % Temp: 1250 °C Time: 2.0 hours Argon-atmosphere Al2O3- crucibles Cooling time: 4 hrs 24 min
Leaching conditions
Batch leaching test, EN12467-2 Remelted samples Liquid/solid: 10 Time: 24 hours Filtration of eluate: 0.45µm filter
Evaluation methods
Evaluation
Lab-scale trials
Smelting
Slag products
Characterisation
Slag sample
Leaching test EN12467-2
XRD powder diffraction
ICP-OES Element analysis of eluate
SEM-EDS
Chemical analysis

## Slide 8: Results - Characterisation

## Slide 9: Results – Chemical analysis
Main element distribution, >1 wt.% | Cu, Zn, As, Pb contents
Main trends with increasing CaO content: Content of: CaO increases Content of : Fe, SiO2, decreases | Main Trends with increasing CaO content: Content of: Zn, Pb decreases Content of: Cu, As fluctuates (decreases)
Chart: Normalised main element distribution
| Original | C0 | C5 | C10 | C15 | C20 | C25
Fe, % | 32.034 | 30.4253 | 29.5161 | 29.8658 | 26.9981 | 25.4594 | 25.5293
SiO2, % | 38.1 | 33.7 | 33.3 | 32.9 | 31.5 | 27.9 | 26.6
CaO, % | 3.77 | 3.89 | 4.85 | 10.6 | 13.9 | 19.3 | 23
MgO, % | 1.52 | 1.55 | 1.56 | 1.73 | 1.37 | 1.41 | 1.26
Al2O3, % | 4.65 | 6.21 | 6.06 | 5.74 | 5.57 | 5.03 | 5.78
Chart: Minor elements
| Original | C0 | C5 | C10 | C15 | C20 | C25
Cu, mg/kg | 9610 | 19000 | 8210 | 5890 | 8080 | 5610 | 7140
Zn, mg/kg | 10300 | 8660 | 8330 | 8200 | 8590 | 7720 | 6370
As, mg/kg | 290 | 312 | 164 | 110 | 247 | 117 | 183
Pb, mg/kg | 59.1 | 145 | 43.2 | 42.1 | 41.6 | 33.7 | 25.1

## Slide 10: Results – SEM-EDS
Sample C5 | Sample C15 | Sample C25
Main phases: 1. Fe, Si, Mg, O 2. Si, Ca, Fe, Al, O – (Cu, S, Sb, As) Inclusions | Main phases: 2. Si, Ca, Fe, Al, O - (Cu, S, Sb, As) 3. Fe, Si, Ca, Mg, O 4. Fe, O | Main phases: 2. Si, Ca, Fe, Al, O - (Cu, S, Sb, As) 4. Fe, O 5. Ca, Si, Fe, Mg, O
1
2
5
4
3
4
2
2

## Slide 11: Results – X-ray diffraction
Mineral phases identified | 
1. Fe2SiO4 | Fayalite
2. Fe3O4 | Magnetite
3. CaFeSi2O6 | Hedenbergite
4. CaFeSiO4 | Kirschstenite
5. Ca2FeSi2O7 | Åkermanite
Increasing CaO content

## Slide 12: Results - Leaching

## Slide 13: Results – Batch leaching test
pH | Conductivity
pH increases from 9.6 to 10.5 increasing amounts of available Ca. | Conductivity increasing to 62 µS/cm Generally low values, below tap water. < 2500 µS/cm
Chart: pH
| C0 | C5 | C10 | C15 | C20 | C25
Average | 9.64 | 9.785 | 9.89 | 10.035 | 10.215 | 10.465
Chart: µS/cm
| C0 | C5 | C10 | C15 | C20 | C25
Average | 39.4 | 29.55 | 46.5 | 47 | 55.1 | 62.4

## Slide 14: Results – Batch leaching test
Copper | Antimony | Arsenic
Copper decrease: ~56 % | C15: ~3 times C0 | C15: ~3 times C0
Chart: mg/L
| Blk | C0 | C5 | C10 | C15 | C20 | C25
Cu | 0.0045852 | 0.091148 | 0.071875 | 0.04676 | 0.05585 | 0.04563 | 0.040594
Chart: mg/L
| Blk | C0 | C5 | C10 | C15 | C20 | C25
As | 0 | 0.011147 | 0.011949 | 0.020968 | 0.034471 | 0.029435 | 0.015266
Chart: mg/L
| Blk | C0 | C5 | C10 | C15 | C20 | C25
Sb | 0.00043258 | 0.042557 | 0.040762 | 0.074463 | 0.12004 | 0.034009 | 0.022682

## Slide 15: Summary
CaO addition changed the slag mineralogy of crystalline slag samples
  Fe2SiO4  CaFeSi2O6 (transition area) CaFeSiO4
Leachability of Cu decrease from the slag product.
The leaching of Sb and As was highest at the transition area, CaFeSi2O6
Iron oxide precipitates in slag with higher CaO addition (20-25 wt.%).

## Slide 16: Acknowledgements
Project partners:
Luleå University of technology
Boliden Mineral AB
PEAB Anläggning AB
Xore AB
Nordkalk AB

## Slide 17: Thank you for your attention!
Contact details:
Jakob Kero
Jakob.kero@ltu.se
Ph.D. student in Process Metallurgy,
Luleå University of technology, Sweden