## Slide 1
Optimizing the use of EAF
stainless steel Slag to
neutralize acid baths
Mattia De Colle
Pär Jönsson
Andrey Karasev
Alicia Gauffin

## Slide 2
high alloyed
stainless steel Slag to neutralize acid baths
Optimizing the use of EAF
coming from the pickling process

## Slide 3
Chart: 
| Blast Furnace | Low Alloyed EAF | High Alloyed EAF
% Landfilled | 0 | 0.2 | 0.8
*Jernkontoret:
Use of slag in Sweden (2010)
Why so niche

## Slide 4
Changing perspective
By-Product
Incidential & secondary
Recycling
Converting waste into new products
Slag
Tool
Carries out specific functions
Re-use
Increasing the life span

## Slide 5
Waste Hierarchy
Reduce
Recover
Dispose
Recycling
Reuse
+ Desirable
- Desirable
*Brochure: The EU’s approach
to waste management (2008)

## Slide 6
Extending slag lifespan
Neutralization
Waste
Waters
EAF Steelmaking
Landfill
Natural
world
Slag builders
Saturated Lime
Slag
Lime
H2O
Saturated Slag
1st trials

## Slide 7
Neutralization Setup
Slag Properties
Mass
Particle size
Mineral content
Origin
WW Properties
Volume
pH, Cr, Ni, F, Fe, Mo
(before and after)
t
pH

## Slide 8
Chart: time (min)
| 0 | 2 | 5 | 10 | 15 | 20 | 25 | 30 | 40 | 50 | 60
S4 15g | 1.18 | 4.16 | 5.59 | 6.06 | 6.25 | 6.34 | 6.38 | 6.33 | 6.36 | 7.15 | 8.33
S4 20g | 1.14 | 6.26 | 6.57 | 6.68 | 6.84 | 7.04 | 7.62 | 8.12 | 8.44 | 8.61 | 9.03
S4 23g | 1.15 | 6.51 | 7.12 | 8.29 | 8.53 | 8.73 | 8.88 | 8.96 | 9.05 | 9.09 | 9.18
SL 5,0g | 1.21 | 6.03 | 9.59 | 9.95 | 9.97 | 9.93 | 9.91 | 9.92 | 9.87 | 9.91 | 9.94
Mass dependent (slag<63 µm)
Lime (5g, 15 µm)
Slag (15g)
Slag (20g)
Slag (23g)

## Slide 9
Chart: time (min)
| 0 | 2 | 5 | 10 | 15 | 20 | 25 | 30 | 40 | 50 | 60
S4 23g | 1.15 | 6.51 | 7.12 | 8.29 | 8.53 | 8.73 | 8.88 | 8.96 | 9.05 | 9.09 | 9.18
S4 48,5 | 1.35 | 5.44 | 6.39 | 6.94 | 7.26 | 7.87 | #N/A | 9.05 | 9.54 | 9.76 | 9.88
Particle size dependent

## Slide 10
Composition dependent (slag<63 µm)
Chart: time (min)
| 0 | 2 | 5 | 10 | 15 | 20 | 25 | 30 | 40 | 50 | 60
S4 23g | 1.15 | 6.51 | 7.12 | 8.29 | 8.53 | 8.73 | 8.88 | 8.96 | 9.05 | 9.09 | 9.18
O1 39g | 1.46 | 6.21 | 6.94 | 8.02 | 8.63 | 8.69 | 8.81 | 8.97 | 9.04 | 9.11 | 9.13

## Slide 11
 | Cr | Ni | Fe | Mo | F
Before Neutralization | 434.00 | 358.00 | 664.00 | 42.00 | 1230.00
Lime Neutralization | 0.08 | 0.27 | 0.12 | 8.93 | 5.53
Slag Neutralization | 0.13 | 0.32 | 0.05 | 7.83 | 9.03
Threshold allowed | 0.50 | 0.50 | 1.00 | 10.00 | .
WW
Composition
(mg/L)

## Slide 12
What’s
Next?
Up-Scale trial
SEM, XRD
Process analysis
LCA
analysis
Pilot line
Mineral
Design

## Slide 13
Thank you!