## Slide 1: An effective equilibrium reaction model for the submerged plasma fuming process using ChemApp
Zhongfu Cheng, Bart Blanpain, Muxing Guo

## Slide 2
Research background
Model development
Modeling case
Results and discussion
Conclusion
2

## Slide 3: Backgrounds
Post
combustion
Premixed feed
Secondary air
Compressed air
Plasma torch
Compressed air+NG
Tuyere
  Off gas
Slag bath
Slag bath
Slag Matte
1
2
3
4
5
6
  Cooler
Technical advantages:
Recover considerable amounts of valuable metals;
Allow valorization potential of slags;
Produce clean slag for novel inorganic polymer.
Existing works:
crucible-scale experiments
industrial measurements
mathematical models
thermodynamic analysis
effective equilibrium reaction zone
computational fluid dynamics simulation
……
Plasma fuming:
Develop a kinetics model for plasma fuming process to fully understand the influence of parameters on the kinetics of metal fuming, allowing optimization of process variables
3

## Slide 4
R0 – Start slag melt
R1 – Plasma generation
R2 – LPG gas combustion
R3 – Feed raw material melt
R4 – Coal-slag reaction
R5 – Slag mixing
R6 – Gas-slag reaction
R7 – Reacted slag homogenization
R8 – Off gas removal from slag bath
R9 – Electrical heating of slag
R10 – Heating loss
R10
R1
R2
R3
R7
R4
R6
R8
R9
R0
Air
Feeding raw materials
LPG
R5
Cooling
Upper plasma generator
lower plasma generator
Reaction zones of plasma fuming process
4

## Slide 5
Model structure for plasma fuming process
Start slag
Feeding materials
Air stream
Natural gas
Coal stream
Combusted gas
Mixed slag
Unreacted slag
Reacted gas
Reacted slag
Off gas
Homogenized slag
Equilibrated slag
R0
Premixed slag
R4
R2
R5
R7
Slag-gas equilibrium
R6
Power input
R1
Elements input
R3
R8
Unreacted gas
Reaction kinetics
R9
R10
5

## Slide 6
Kinetics model--Effective equilibrium reaction zone (EERZ) model
Equilibrium
Bulk slag
Off gas
Equilibrated slag
Unreacted slag
Bulk gas
Injection gas
Continuous feeding
Short circuiting gas
Reactive gas
Reaction level;
Mass transfer coefficient solving the amount of reactive slag:
Fitting with experimental data;
The influences of process variables are incorporated in the mass transfer coefficient
Fitting
Reactive slag
6
Notes: This figure shows the details of my kinetics model. It is developed based on the EERZ model. Specifically, for a given time step, a certain amount of slag and gas will reach equilibrium, and the equilibrated slag will return to the bulk slag, and the gas products will return to the bulk gas, forming the off gas, and finally flow out of the reactor. The reaction level is determined by the amount of reactive slags. The reactive slag was calculated by the first order mass transfer equation, so the key parameter is the mass transfer coefficient. It was solved by fitting with experimental data. Obviously, the influence of process variables are incorporated in this coefficient.

## Slide 7
Reaction interface area A is a function of foaming slag height, evaluated based on the numerical results.
Slag volume fraction
Numerical simulation of fuming furnace
(Gas velocity 50 m/s, t=10s)
Short circuiting gas
Reaction interface
7

## Slide 8: ChemApp-based fuming model
Equilibrium calculation;
Effective equilibrium reaction zone (EERZ) model for kinetics;
Time step concept.
Model structure
Reasonable kinetics model
Thermodynamic calculation
Three key steps
a
b
c
Reaction kinetics model
8

## Slide 9
Incorporate all the reaction zones
Define global variables
Initialize chemApp and calculation conditions
Read input data
Write results
Connect transfer streams
Call the kinetics model
Definite all the reaction streams
Store reacted streams
10. Calculate equilibriums
Model implement
ChemApp
9
Highly modular
Notes: This model was implemented by ChemApp as shown this figure. At the same time, the database of Factsage was imported into ChemApp to calculate the equilibriums. My ChemApp code model includes 10 parts of subroutines. It allows to use separate input and output files.

## Slide 10
Great flexibility to design and implement FactSage calculation;
Customized reaction kinetics;
3) Flexible input
4) Powerful output
5) Controllable computational efficiency
Model characteristics
10
Notes: I also give a short instruction of my model characteristics.1. The current ChemApp-based model provides great flexibility to design and implement FactSage calculation. 2. It allows to customize reaction kinetics; 3. It provides flexible input, any process parameters you want to consider can be input the calculation, such as temperature, gas flow rate, slag compositions, gas compositions. It even allows to use elements as input; 4. It has powerful output. Any variables you are interested can be set as an output. 5. In addition, in order to improve the computation efficiency, I also optimize the calculation methods. So the calculation efficiency becomes controllable. It allows to run in your personal computer.

## Slide 11
Modelling case
11

## Slide 12
Start slag melting
Raw material feeding
Reducing
Air/LPG=r2
Air/LPG=r1
Air/LPG=r3
Air/LPG=4
Coal amount=s1
I
II
III
Start slag melting
Raw material feeding
Reducing
Coal amount=s2
r1>r2>r3>r4
s1<s2
Modelling case
12
Notes: The ChemApp-based model was applied to simulate the plasma fuming process. In the current modelling case, the fuming was divided into three stages, namely, start slag melting, raw material feeding and reducing. Every stage has its individual operation parameters. The modelling results are shown on the next page.

## Slide 13
Species | Terminal amount (wt%) | 
 | Experiment | Prediction
ZnO | 0.5788 | 0.3930
PbO | 0.0273 | 0.0257
Start slag
Feeding
Air/LPG=r2
Reducing
Air/LPG=r4
Comparison between the simulation results and the experimental data for the concentration profiles of ZnO and PbO
Results and discussion
13

## Slide 14
Start
slag
Feeding
Air/LPG=r2
Reducing
Air/LPG=r4
Comparison between the simulation results and the experimental data for the concentration profiles of slag components
Results and discussion
14
Notes: Obviously, the predictions show good agreement with the experimental data. The residual concentrations of zinc oxide and lead oxide in different stages are well predicted. The target values of residual zinc and lead are also consistent with the measurements.

## Slide 15
An effective equilibrium reaction zone model has been developed to describe the plasma fuming process.
ChemApp was applied in this model to design the model and implement the simulation.
This model can be further extended to investigate the influence of process parameters on the fuming efficiency.
PbO in the slag below 300 ppm.
Conclusions
15

## Slide 16: Thank You
16