## Slide 1: Valorised slags under risk assessment obligations: iron silicate risk assessment
Federica Iaccino

## Slide 2
Slags in the European Legislative Framework

## Slide 3: Iron silicate under EU legislation
Iron silicate is a final slag extracted during the copper production
Produced as stones, granules or powders
As final slag, it contains lowest levels of metals and is used in further applications as in concrete, abrasive blasting,river embankement, road constructions….
REACH Regulation sets up rules for putting substances on the European market in volumes higher than 1 ton/year
  Perform risk assessment
  Prove safe use along the substance life cycle
  Present results in a chemical safety report

## Slide 4
REACH requires to develop risk assessments, based on an increasing level of testing data depending on the volume of the substance to assess
REACH dossiers are based on the following milestones:
REACH Dossier in a nutshell
Substance Identity
Classification
Hazard Assessment
Exposure Assessment
Risk Assessment
Analytical testing to provide unanbiguous mineralogical composition
Phys chem – Environmental & Human Health
Testing strategy or Read Across from structural similar substances
Substance exposure estimated/measured concentrations
Ratio exposure/hazard threshold < 1

## Slide 5
REACH Dossier on Iron Silicate
Iron silicate, as other slags, is an inorganic UVCB (iUVCB): substance of Unknown or Variable composition, Complex reaction products or Biological materials
  It is a complex material typically composed by several metals, metals compounds and minerals with variable concentrations
Challenge: how to comply with REACH requirements for such complex materials?
  In 2012 Eurometaux and its non-ferrous metals consortia launched a project to develop a scientific and pragmatic alternative assessment strategy for iUVCBs

## Slide 6
REACH requires to develop risk assessments, based on an increasing level of testing data depending on the volume of the substance to assess
REACH dossiers are based on the following milestones:
REACH Dossier in a nutshell
Substance Identity
Classification
Hazard Assessment
Exposure Assessment
Risk Assessment
Analytical testing to provide unanbiguous mineralogical composition
Phys chem – Environmental & Human Health
Testing strategy or Read Across from structural similar substances
Substance exposure estimated/measured concentrations
Ratio exposure/hazard threshold < 1
iUVCBs Issues:
No PNEC/DNEL available for the UVCB substance due to high variability; No exposures available for the UVCB substance due to complexity

## Slide 7
Non-ferrous metals inorganic side products risk assessment approach

## Slide 8: Background inorganic UVCBs
Elemental composition is
  known and available
  can present high variability
Speciation/mineralogical composition is:
  can be unknown or uncertain
Complicates toxicity testing: realistic worst-case composition?

## Slide 9: Testing approach
Major
constituents
Minor
constituents
Physico-chemical
endpoints
Substance Identity
Ecotoxicological
endpoints
Systemic
toxicological
endpoints
Substance based
testing approach
Constituent based
testing approach
Local
toxicological
endpoints
Data-rich
Data-poor
Composition: constituents

## Slide 10
Iron Silicate Risk Assessment

## Slide 11: Identification of the Iron Silicate

## Slide 12: Classification of the Iron Silicate (1)
www.meclas.eu
INCREASING CONSERVATISM
INCREASING KNOWLEDGE
TIER 2 Classification based on TDp or Bioaccessibility correction
TIER 0
Classification of worst case assumption on constituents
TIER 1
Classification based on speciation of constituents
TIER 3 Classification based on measured toxicity response (testing)
  Inorganic UVCB classification is derived following mixture rules
  Variability for each constituent is assessed using their maximum concentration (maximum of Typicals)
  Uncertainty in speciation is tackled assuming worst-case speciation for classification endpoints
Releases of metals from the slags are derived using transformation dissolution data

## Slide 13
Classification of the Iron Silicate (2)

## Slide 14: Hazard Assessment of Iron Silicate
  Substance constituents are assessed:
  in their known speciation or
  in the worst-case speciation for the specific hazard endpoint
  Substance specific testing:
  Bioelution (gastric test)
  Acute toxicity via oral route
  Acute toxicity via dermal route
  Skin and eye irritation
  Bacterial gene mutation test
  Long term outdoor aquatic mesocosm study (freshwater NOEC; Hommen et al, 2012).

## Slide 15: Exposure Assesment of Iron Silicate
Manufacturing
On site assessment of exposure during production includes metal releases related to production of slags & of all associated copper intermediates
Downstream uses
Exposure during final uses is related to metal releases from slags only
Validation for critical use (river embankments) from mesocosm study

## Slide 16: Combined Risk Assessment of Iron Silicate
Risk Characterization Ratio=
Measured metal exposures during production and uses
PNECs/DNELs metals (Cu, Pb, Ni, Zn)
RCR=
RCR=
RCR mix=
RCR mix=
∑
∑
< 1
< 1

## Slide 17: Iron Silicate assessment’s conclusions
Iron silicate “constituents approach” methodology provides:
A scientific sound and pragmatic risk assessment
Compliance with the European REACH Requirements
Increasing of multi-metallic methodological approach & development of ad hoc tools, as the Eurometaux multimetallic database (MMD)
REACH ‘regular’ Registration Dossiers for complex slags would lead to several difficulties, as:
Validation of the respresentativness of the tested sample
Exposure assessment difficulties
Extended time (costs) for testing

## Slide 18
Thank you!
Wendy Wellens
Violaine Verougstraete
Frederik Verdonck
Koen Oorts